Supplementary Material

Facile synthesis of KOH and ball milling co-modified wheat straw-derived biochar for the efficient adsorption of methylene blue in aqueous solution

Huaiyan Li 1, Kongyong Ouyang 1, Xinrui Weng 1, Lei Wu 2, Xinshun Li 1, Yanhong Shi 1, Ningyuan Zhang 3, Yunhua Zhang 1*, Hui Li 1*

1 Anhui Province Key Laboratory of Farmland Ecological Conservation and Pollution Prevention, College of Resources and Environment, Anhui Agricultural University, Hefei 230026, China;

2 Anhui Provincial Academy of Eco-environmental Science Research, Hefei 230061, China

3 Hefei NO.1 High School, Hefei 230601, China;

* Correspondence: zhpaper@126.com (Hui Li), yunhua9681@163.com (Yunhua Zhang)

This supplementary information contains:

Table S1 Elemental composition on the SEM-EDS of Biochar, KOH-Biochar, BM-Biochar and KOH-BM-Biochar

Table S2 Weber-Morris intraparticle diffusion model in the adsorption process of MB onto Biochar, KOH-Biochar, BM-Biochar and KOH-BM-Biochar

Table S3 Thermodynamics parameters for the adsorption of MB onto KOH-BM-Biochar

Figure S1. KOH-BM-Biochar prepared route with the two-step KOH activated pyrolysis and ball milling co-modified method

| Element |  | Biochar | KOH-Biochar | BM-Biochar | KOH-BM-Biochar |
| --- | --- | --- | --- | --- | --- |
| C | Wt(%) | 53.31 | 83.53 | 34.63 | 80.42 |
|  | μ | 0.58 | 0.31 | 0.38 | 0.31 |
|  | Atomic(%) | 64.04 | 87.47 | 45.76 | 85.44 |
| N | Wt(%) | 0.42 | - | 0.68 | - |
|  | μ | 0.48 | - | 0.33 | - |
|  | Atomic(%) | 0.42 | - | 0.77 | - |
| O | Wt(%) | 30.31 | 15.16 | 39.49 | 16.53 |
|  | μ | 0.49 | 0.31 | 0.32 | 0.31 |
|  | Atomic(%) | 27.32 | 11.96 | 39.23 | 13.19 |
| Si | Wt(%) | 15.77 | 0.93 | 25.04 | 2.72 |
|  | μ | 0.19 | 0.04 | 0.19 | 0.05 |
|  | Atomic(%) | 8.13 | 0.42 | 14.17 | 1.24 |
| Atomic ratio O/C |  | 0.43 | 0.14 | 0.86 | 0.15 |

Table S1 Scanning electron microscopy-energy dispersive X-ray energy spectroscopy (SEM-EDS) of Biochar, KOH-Biochar, BM-Biochar and KOH-BM-Biochar

| Adsorbent | Weber-Morris |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Kp1(mg·g-1·min-0.5)) | C1 | (R1)2 | Kp2(mg·g-1·min-0.5)) | C2 | (R2)2 | Kp3(mg·g-1·min-0.5)) | C3 | (R3)2 |
| Biochar | 0.043 | 16.468 | 0.0071 | 0.022 | 14.994 | 0.0026 | 0.174 | 20.002 | 0.8226 |
| KOH-Biochar | 1.409 | 84.943 | 0.5415 | 0.956 | 87.722 | 0.9648 | 0.105 | 103.127 | 0.6878 |
| BM-Biochar | 1.909 | 30.633 | 0.8282 | 0.054 | 48.166 | 0.0091 | 2.217 | 34.360 | 0.9981 |
| KOH-BM-Biochar | 2.333 | 129.728 | 0.7548 | 1.650 | 138.408 | 0.9146 | 1.562 | 137.169 | 0.8701 |

Table S2 Weber-Morris intraparticle diffusion model in the adsorption process of MB onto Biochar, KOH-Biochar, BM-Biochar and KOH-BM-Biochar

| Temperature(oC) | KF(L·mg-1) | Keo | ΔGo (kJ·mol-1) | ΔHo (kJ·mol-1) | ΔSo (J·mol-1·K-1) |
| --- | --- | --- | --- | --- | --- |
| 25 | 49.61 | 18549179 | -41.46 | 19.72 | 205.46 |
| 35 | 68.02 | 25432678 | -43.66 |  |  |
| 45 | 81.73 | 30558847 | -45.57 |  |  |

Table S3 Thermodynamics parameters for the adsorption of MB onto KOH-BM-Biochar

Figure S1. KOH-BM-Biochar prepared route with the two-step KOH activated pyrolysis and ball milling co-modified method