Table 1 Slope of MSD curve of composite film components

Table 2 Bond and nonbond energies of film liquids and films with different water content

Table 3 Mechanical properties of composite film components

Table 4 Experimental values of T and permeability of the composite films to four substances

Table 1 Slope of MSD curve of composite film components

| Slope | P10S0 | P8S2 | P6S4 | P4S6 | P2S8 | P0S10 |
| --- | --- | --- | --- | --- | --- | --- |
| γ-PGA | 0.0152 | 0.0127 | 0.0108 | 0.0108 | 0.0125 | - |
| St | - | 0.0102 | 0.0106 | 0.0097 | 0.0083 | 0.0112 |
| Gly | 0.0310 | 0.0351 | 0.0278 | 0.0313 | 0.0266 | 0.0291 |

-: No substance

Table 2 Bond and nonbond energies of film liquids and films with different water content

| Sample | EBond/(kJ·mol−1) | EAngle/(kJ·mol−1) | ETorsion/(kJ·mol−1) | EInversion/(kJ·mol−1) | Evdw/(kJ·mol−1) | Ecoulomb/(kJ·mol−1) | Ehbond/(kJ·mol−1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2396 | 3893 | 1111 | 120 | 2057 | −6001 | −2155 |
| 2 | 2407 | 3662 | 1112 | 115 | 2163 | −4575 | −1697 |
| 3 | 2387 | 3660 | 1073 | 117 | 2020 | −4292 | −1629 |
| 4 | 2408 | 3739 | 1072 | 120 | 1740 | −4042 | −1407 |

1, 2, 3, and 4 represent the moments of 100, 20, 10, and 1 g water during the film-forming process, respectively.

Table 3 Mechanical properties of composite film components

| Elastic coefficient | P10S0 | P8S2 | P6S4 | P4S6 | P2S8 | P0S10 |
| --- | --- | --- | --- | --- | --- | --- |
| C11 | 12.0329 | 12.5337 | 12.228 | 15.407 | 13.7814 | 14.0692 |
| C12 | 4.7394 | 4.4309 | 4.4196 | 6.4247 | 5.3135 | 5.3325 |
| C13 | 4.9749 | 5.3542 | 4.8598 | 5.8797 | 5.4462 | 4.7804 |
| C15 | −0.0788 | 0.0419 | 0.9585 | −0.1674 | −0.1726 | 0.1265 |
| C22 | 11.7342 | 11.4393 | 13.2822 | 14.9091 | 14.5533 | 12.9518 |
| C23 | 4.8701 | 6.0907 | 5.4211 | 5.7453 | 5.2182 | 5.1847 |
| C25 | −0.3119 | 0.1303 | 0.4959 | −0.036 | −0.5518 | −0.0788 |
| C33 | 12.5996 | 15.321 | 11.242 | 12.6228 | 14.2183 | 14.9611 |
| C35 | −0.084 | 0.252 | 0.8829 | −0.3991 | −0.2255 | 0.2665 |
| C44 | 4.6613 | 4.1664 | 2.8595 | 4.4494 | 4.4022 | 4.7596 |
| C46 | 0.0307 | −0.1085 | 0.2389 | 0.0608 | −0.1969 | 0.1606 |
| C55 | 4.3946 | 4.4129 | 4.7067 | 4.4516 | 4.4733 | 4.891 |
| C66 | 3.3128 | 4.3945 | 6.3592 | 4.3229 | 5.3028 | 4.5811 |
| K /GPa | 7.266 | 7.779 | 7.234 | 8.674 | 8.217 | 8.034 |
| G /GPa | 3.882 | 4.108 | 4.056 | 4.276 | 4.581 | 4.601 |
| Y /GPa | 9.285 | 9.844 | 9.316 | 10.66 | 11.23 | 11.19 |
| v | 0.2869 | 0.2919 | 0.2839 | 0.2957 | 0.2707 | 0.2682 |
| C12-C44 | 0.3136 | 1.1878 | 2.0003 | 1.4303 | 1.044 | 0.0208 |

Table 4 Experimental values of T and permeability of the composite films to four substances

|  | T/GPa | / (mg/(cm2·d) | WVP/ (g·mm/(m2·d·kPa)) | / (g/d) | Poil/(g·m/(m2·d)) |
| --- | --- | --- | --- | --- | --- |
| P10S0 | 10.6824 ± 1.6844a | 0.5986 ± 0.0123d | 12.0225 ± 2.9212a | 0.0585 ± 0.0042b | 38.3490 ± 3.2636b |
| P8S2 | 10.9801 ± 0.5759b | 0.5383 ± 0.0552b | 10.0092 ± 1.2683b | 0.0281 ± 0.0064c | 24.0565 ± 0.8649c |
| P6S4 | 6.7672 ± 0.4588a | 0.6011 ± 0.0672b | 11.3507 ± 1.0086b | 0.0193 ± 0.0069a | 15.0626 ± 0.7963c |
| P4S6 | 3.6869 ± 0.22083c | 1.0018 ± 0.1376b | 10.6203 ± 2.0080a | 0.0163 ± 0.0026c | 1.1637 ± 0.07070c |
| P2S8 | 3.8114 ± 0.8403b | 1.0871 ± 0.3173a | 8.1295 ± 0.8199b | 0.0093 ± 0.0013a | 0.4289 ± 0.0910b |
| P0S10 | 10.5978 ± 0.6442b | 0.0161 ± 0.0047c | 3.7496 ± 0.1315d | 0.0126 ± 0.0025b | 0.2783 ± 0.0423a |

Superscripts a, b, c, and d indicate significant differences (P < 0.05).