Synthetic poly (4-hydroxybutyrate) as reinforcing additive to manufacture high-performance and fully biodegradable PBAT composites for foaming applications

Jinyun Cui, Huaping Wang, Xinyi Chen, Ze Kan*, Zhibo Li*

Key Laboratory of Biobased Polymer Materials, Shandong Provincial Education Department, College of Polymer Science and Engineering, Qingdao University of Science and Technology, Qingdao, China

Figure S1 Tan δ (a) and storage modulus (b) of PBAT, P4HB and PBAT/P4HB blend.

Figure S2 SEM images of the cryo-fractured surface for PBAT/P4HB (a15000× , a210000×).

Table S1 Mechanical properties of PBAT, P4HB and PBAT/P4HB/ P4HB-g-GMA blends.

| Sample | Yield strength (MPa) | Tensile breaking strength (MPa) | Elongation at break (%) | Izod notched impact strength (kJ/m2) |
| --- | --- | --- | --- | --- |
| PBAT | 5.9±0.8 | 21.8±2.8 | 689±63 | 23.8±1.4 |
| P4HB | 16.4±1.0 | 52.4±3.0 | 466±21 | 50.1±2.3 |
| PBAT/P4HB | 4.7±0.2 | 17.8±1.0 | 482±49 | 14.1±0.3 |
| PBAT/P4HB/G1 | 7.4±1.1 | 20.4±1.7 | 564±61 | 22.6±0.8 |
| PBAT/P4HB/G2 | 8.4±0.4 | 23.4±1.6 | 641±47 | 23.6±0.2 |
| PBAT/P4HB/G4 | 8.7±2.1 | 25.3±3.0 | 656±51 | 23.8±0.9 |
| PBAT/P4HB/G6 | 9.4±1.3 | 27.5±2.1 | 635±71 | 31.9±1.6 |
| PBAT/P4HB/G8 | 12.1±0.3 | 29.2±1.3 | 588±31 | 30.3±1.9 |

Table S2 DSC data of PBAT/P4HB/P4HB-g-GMA blends.

| Sample | ΔHm (PBAT) (J/g) | Xc (PBAT) (%) | Tm (PBAT) (℃) | Tc (PBAT) (℃) | ΔHm (P4HB) (J/g) | Tm (P4HB) (℃) | Tc (P4HB) (℃) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PBAT/P4HB | 5.9 | 7.5 | 122.9 | 73.9 | 10.1 | 60.5 | -12.9 |
| PBAT/P4HB/G1 | 6.3 | 7.9 | 122.8 | 76.7 | 12.5 | 60.4 | 22.8 |
| PBAT/P4HB/G2 | 7.0 | 8.8 | 122.2 | 77.4 | 13.5 | 60.4 | 23.3 |
| PBAT/P4HB/G4 | 7.2 | 9.0 | 123.4 | 78.6 | 15.3 | 61.3 | 24.9 |
| PBAT/P4HB/G6 | 7.0 | 8.9 | 122.7 | 76.2 | 14.7 | 60.6 | 25.2 |
| PBAT/P4HB/G8 | 7.5 | 9.4 | 122.4 | 77.2 | 15.7 | 60.1 | 25.3 |