
Supplementary
Regulating the asymmetric diffusion channel in MnCo2O4 spinel enables accelerated hydrogen bond reaction kinetics of ammonia ion batteries
Kang Xiao,1, ‡ Bo-Hao Xiao,1, 2 ‡ Jian-Xi Li,1 Shunsheng Cao2 and Zhao-Qing Liu, 1, *
1School of Chemistry and Chemical Engineering/Institute of Clean Energy and Materials/Key Laboratory for Clean Energy and Materials, Guangzhou University, Guangzhou 510006

2School of Materials Science & Engineering, Jiangsu University, Zhenjiang 212013, China

‡K. X. and B. H. X contributed equally to this work.

*Corresponding authors. E-mail: lzqgzhu@gzhu.edu.cn
1. Supplementary Figures
[image: image1.png]



Figure S1. SEM image of (a) MCO/CNTs and (b) Ro-MCO/CNTs.
[image: image2.png]e

Mg

_

o
¥ &





Figure S2. (a) TEM image with corresponding (b) HRTEM image of MCO/CNTs. (c) TEM image with corresponding (d) HRTEM image of Ro-MCO/CNTs.
[image: image3.png]a Mn 2p b Co 2p c O1s
MCO/CNTs

_ E 5

S S S

8 > 2

= 2 2

Z 3 15

2 V,-MCO/CNTSs = =

=
MCO/CNTs

660 655 650 645 640 805 798 791 784 777 536 534 532 530 528 526

Binding Energy (eV) Binding Energy (eV) Binding Energy (eV)




Figure S3. (a) Mn 2p, (b) Co 2p, and (c) O 1s XPS spectra of MCO/CNTs, Vo-MCO/CNTs, and Ro-MCO/CNTs.
[image: image4.png]Transmittance (a.u.)

400

R,-MCO/CNTs

V_,-MCO/CNTSs

600 800 1000 1200

Wavenumber (cm™)




Figure S4. FT-IR of MCO/CNTs, Vo-MCO/CNTs, and Ro-MCO/CNTs.
[image: image5.png]Valence

3.04 Mnsite 9
2.5-
2.0+ od

. Red
1.51 @ Mn-foil

' /o @ V,-MCO
1.0 il

_ , @ MCO
0.5' l’, ° Mno

] 2 R,MCO
004 o @ Mn,0,

6540 6542 6544 6546

Photon energy (eV)

Valence

3.0 Cosite 9
r 'w,
2.5+ 4
. &
2.0- - X
1.5- @ Co-foi
' @ Co0
1.0 @ V,MCO
0.5. @ MCO
. L 2 R-MCO
0.04 o @ Co,0,4
7710 7712 7714 7716

Photon energy (eV)

7718




Figure S5. (a) The average oxidation states of Mn sites in Mn foil, Vo-MCO/CNTs, MCO/CNTs, MnO, Ro-MCO/CNTs, and Mn2O3, respectively. (b) The average oxidation states of W sites in Co foil, CoO, Vo-MCO/CNTs, MCO/CNTs, Ro-MCO/CNTs, and Co2O3, respectively.
[image: image6.png]7(R)I (A%

Mn-O-Mn

MCO/CNTSs
——V,-MCO/CNTSs

——R_,-MCO/CNTSs

2 4 6

Radial disance (A)

O

2(R)I (A

——MCO/CNTs
——V,_-MCO/CNTs

——R,-MCO/CNTSs

Radial disance (A)




Figure S6. (a) FT-EXAFS spectra of Mn and (b) Co.
[image: image7.png]k® x(k) (A®)

1 Mn K-edge
10 1
04—
107 mco
| ——V_-MCO
5p] —ReMCO
Mn-foil
0 2 4
k (A)

k® x(k) (A)

404 CoK-edge
20 -
0 ]
-20 1
——MCO
| ——v,Mmco
407 R,-MCO
' Co-foil
-60 - . : : . .

k (A)




Figure S7. (a) Mn K-edge EXAFS oscillation function of MCO, Vo-MCO, Ro-MCO, Mn foil, MnO, and Mn2O3, respectively. (b) Co K-edge EXAFS oscillation function of MCO, Vo-MCO, Ro-MCO, Co foil, CoO, and Co2O3, respectively.
[image: image8.png]I —&—MCO/CNTs-1
¥ —a— MCO/CNTs-2
—&—MCO/CNTs-3

—O0—O0—Q—¢- :
LE)) O-Q.O--v-g& |m
N
O—0—0—¢g—o-
© O—0—0-0-0-0 00y}
- T
a (wyo) ,z-
- N ™ 5
b o O -~
E E E i
zZ Z Z o
QQQ j
SRele 82
O O O T
= = = I
] 5 2
(2N
=
(@)
5 ®
. tg 8
o) @)
<
- |, e
s |8 %
@
o
)
Ne)

®

. _ _
S S8 o S8 3 o
= < S o < <

(308 'sA A) [enusiod




Figure S8. (a) GCD curves at 0.1 A g−1 and (b) EIS of MCO/CNTs-1, 2 and 3.
[image: image9.png]2
—
Z
&
o)
O
=

|

O

_

d

—&—V_-MCO/CNTSs

&
Q/

-MCO/CNTs

—&—R,

Z' (ohm)




Figure S9. EIS spectra of MCO/CNTs, Vo-MCO/CNTs, and Ro-MCO/CNTs.
[image: image10.png])

Potential (V vs. SCE)

0.9
0.6
— 1%t cycle
0.31 2" cycle
3 cycle
0.0+
-0.3-
01Ag"
-0.6 T T T T T
0 60 120 180 240

Specific Capacity (mAh g™

(on

Potential (V vs. SCE)

o
[(e}
1

o
o
1

©
w
1

o
o
1

-0.31

0 60 120 180
Specific Capacity (mAh g™')

240

o

Current Density (A g™

0.4

0.2+

0.0+

0.2 Capacitive Cc;ntrolled

-0.4 0.2mVs
06 03 00 03 06 09

Potential (V vs. SCE)





Figure S10. (a) GCD curves at 0.1 A g−1. (b) GCD curves at different current densities. (c) Capacitive contribution of Vo-MCO/CNTs.
[image: image11.png]Q

Potential (V vs. SCE)

@

Current Density (A g™

b
0.9 0.9+
ﬂ it: A -1
0_6- O 06_ \ Unit g
« w | 0.1
1% cycle g) \ 0.2
0.3 7 2nd Cycle > 0.3 T 03
3" cycle T_“/ — 05
0.0 1 = 0.0 0.7
[0)
-0.3- g -0.3-
' 0.1Ag” '
-0.6 1 -0.6 1
0 50 100 150 200 0 40 80 120 160
Specific Capacity (mAh g™) Specific Capacity (mAh g™)
= d
0.6 2 ® Peakt 3 1201 [ | Diffusion Controlled
AL Peaka o~ o 1 [ | Capacitive Controlled
5 -0.6 0’::,/;/” ;\;
03430l 7 ieew o
= te-oss ©
S %5 <6 04 w02 00 (n'd
Log v (Scan Rate, mV s™) cC
0.0+ , O
Unit mvVs™ 5
0.2 -g
0.3 045
— 0.6 (@)
i Y
-0.6 1 v 1 v 1 M 1 N 1 N 1 - v
-06 -03 00 03 06 09 0.2 04 0.6 0.8 1

Potential (V vs. SCE)

Scan Rate (mV s™)





Figure S11. (a) GCD curves at 0.1 A g−1. (b) GCD curves at different current densities. (c) CV curves at different scan rates from 0.2 to 1.0 mV s−1. Inset is the log i versus log v plots based on the CV curves at four different oxidation/reduction states. (d) Capacitive contribution of MCO/CNTs.

[image: image12.png]Q

Potential (V vs. SCE)

(@)

Current Density (A g™')

0.9-
0.6
0.3-
0.0-
-0.31
-0.6 1
0 30 60 90 120
Specific Capacity (mAh g™)
00 <afsimy 4
9] o Peak3 _ .-g°
3-06 ) /; ’;’
O3 T e
> -~ -b3=050
S o8 06 w04 02 00
Log v (Scan Rate, mV s™')
0.0 Unit: mV s™
0.2
—04
-0.3 - 086
H I _08
3 2 —1.0
-0.6 1 v 1 v 1 T 1 v 1 T 1 T
-06 -03 00 03 06 0.9

Potential (V vs. SCE)

O

Potential (V vs. SCE)

o

Contribution Ratio (%)

0.9+
Unit: A g™
0.6 - \;\\ 0.1
e ——0.2
0.3 — 03
——05
0.0 ——07
—1.0
-0.3 1
-0.6 1
30 60 90 120
Specific Capacity (mAh g™)
120 [ Diffusion Controlled
[ Capacitive Controlled
100 -
80 -
60 -
40-
204
0 i

0.2

0.4
Scan Rate (mV s™)

0.6 0.8 1





Figure S12. (a) GCD curves at 0.1 A g−1. (b) GCD curves at different current densities. (c) CV curves at different scan rates from 0.2 to 1.0 mV s−1. Inset is the log i versus log v plots based on the CV curves at four different oxidation/reduction states. (d) Capacitive contribution of Ro-MCO/CNTs.
[image: image13.png]Q

Potential (V vs. SCE)

MCO/CNTs

--9

F-12
OQQQ%OQQ &)

e
--15
®

--18
® LogD (cm?s™)
Potential (V vs. SCE)

- -21

0 2x10* 4x10* 6x10* 8x10* 1x10°

Time (s)

Log[D (cm2 s-1)]

(o)

Potential (V vs. SCE)

R,-MCO/CNTSs

ce

® LogD (cm?s™)

Potential (V vs. SCE)

--12

--15

18

0 1x10%

2x10*  3x10% 4x104
Time (s)

)

(2]

Log[D (cm?




Figure S13. GITT profiles and the calculated NH4+ diffusion coefficient of (a) MCO/CNTs and (b) Vo-MCO/CNTs.
[image: image14.png]R,-MCO/CNTs

—©—308.15 K

201 _a_ 30315k

15] —=—313.15K

T
o
-

(wyo) ,z-

V,-MCO/CNTs
—=—303.15K
—&—308.15K
—=—-313.15K

323.15K
—©—333.15K

—_—

20+

15

MCO/CNTs

—&—308.15K

313.16 K
323.15K
—©—333.15K

—
e

204 —®—303.15K

o

~

(wyo) ,z-

5

1

Z' (ohm)

Z' (ohm)

Z' (ohm)




Figure S14. EIS spectra at different temperatures of the (a) MCO/CNTs, (b) Vo-MCO/CNTs, and (c) Ro-MCO/CNTs.
[image: image15.png](wyo) ,.z-

©
-

D

O
|

D)
|

—&— After 100" cycle
—&— After 200! cycle

Z' (ohm)




Figure S15. EIS spectra of the Vo-MCO/CNTs during cycle stability test.
[image: image16.png]Q

Intensity (a.u.)

(oé
Intensity (a.u.)

665 658 651 644 637 536 534 532 530 528

Binding Energy (eV) Binding Energy (eV)




Figure S16. Ex-suit XPS of (a) Mn 2p and (b) O 1s for Vo-MCO/CNTs at different state.
[image: image17.png]



Figure S17. SEM images of Vo-MCO/CNTs at different state in the GCD cycle.
[image: image18.png]d

Hydrogen bond

Hydrate NH,* (3.31 A)

MnCo,0, Spinel




Figure S18. Schematic diagram of (a) hydrate NH4+ and N–H···O bonds, (b) intercalation sites for hydrate NH4+ in MnCo2O4 spinel.
[image: image19.png]/N

) .99 ¢
0 7\ \ W, N
WO ¥ W

W/ W/ \ W, W,

L % \\

\Zaa\ Zea\ /2

MCO

AW

D Z20\ 720\ Zaa\ 7/

N
¢
\
Z,

N/

/8

AW

N\,
\ 720\ Zao\ Zaa\. /

N/

/8





Figure S19. Schematic diagram of three MnCo2O4 samples with different metal–O bond lengths.
[image: image20.png]Q

Current Density (A g")

02mvs’
0.4
0.0
-0.4-
0.8 1%t cycle
—— 2" cycle
3 cycle
_1 .2 T T T T T
-0.9 -0.6 -0.3 0.0 0.3
Potential (V vs. SCE)

(ox

Potential (V vs. SCE)

0.3+

0.0+

-0.3

-0.64

0.1Ag"

1%t cycle

2" cycle

39 cycle

40 80
Specific Capacity (mAh g™')

120

-Z" (ohm)

T
)
I
)
|
)
|
)
|
)
I
s
J
s
<
s

~L

1 2
Z' (ohm)





Figure S20. (a) CV curves, (b) GCD curves, and (c) EIS spectra of PTCDI.
[image: image21.png]Current (mA)

0.04

O
o
N

0.00

-0.02

-0.04

0.0

0.5 1.0
Voltage (V)

1.5

2.0




Figure S21. CV curves of Vo-MCO/CNTs//1 M (NH4)2SO4//PTCDI full cell at 0.2 mV s–1.
[image: image22.png])

(ohm

ZI




Figure S22. EIS spectra of Vo-MCO/CNTs//1 M (NH4)2SO4//PTCDI full cell at 0.2 mV s–1.
2. Supplementary tables

Table S1. Elemental content of Vo-MCO/CNTs
	Element
	C
	Mn
	Co
	O

	Content (%)
	43.5
	12.2
	21.5
	22.8


Table S2. Comparison of representative electrode materials for AIBs
	Host material
	Electrolyte
	V vs. SCE
	Capacity (mAh g–1)
	Ref.

	VOPO4·2H2O
	1 M (NH4)2SO4
	–0.2 — 1.1 V
	154.6 mAh g–1 (0.1 A g–1)
	

1



	Mn3Al1-LDH
	0.5 M (NH4)2SO4
	–0.2 — 1.0 V
	183.7 mAh g–1 (0.1 A g–1)
	2


	PBAs
	21 M NH4TFSI
	0 — 1.2 V
	101.2 mAh g–1 (0.1 A g–1)
	3


	MnOx
	0.5 M NH4Ac
	0 — 0.8 V
	176.0 mAh g–1 (0.1 A g–1)
	4


	h-MoO3
	1 M NH4Cl
	–0.5 — 0.6 V
	115.0 mAh g–1 (0.1 A g–1)
	

5



	V2O5
	0.5 M (NH4)2SO4
	–0.2 — 0.8 V
	119.0 mAh g–1 (0.1 A g–1)
	6


	Vo-MCO/CNTs
	2 M (NH4)2SO4
	–0.5 — 0.9 V
	219.2 mAh g–1 (0.1 A g–1)
	This work


Table S3. Fitted EIS component values of the MCO/CNTs, Vo-MCO/CNTs, and Ro-MCO/CNTs
	Sample
	Temperature (K)
	Solution resistance (Ω)
	Charge transfer resistance (Ω)
	Warburg impedance (Ω)

	MCO/CNTs
	303.15
	4.59
	6.31
	24.8

	
	308.15
	4.33
	5.51
	22.7

	
	313.15
	4.32
	4.69
	18.5

	
	323.15
	3.71
	3.70
	15.2

	
	333.15
	3.82
	2.86
	13.6

	Vo-MCO/CNTs
	303.15
	2.65
	11.2
	9.36

	
	308.15
	2.61
	10.29
	9.19

	
	313.15
	2.28
	9.72
	7.35

	
	323.15
	2.33
	7.83
	6.63

	
	333.15
	2.70
	6.56
	7.51

	Ro-MCO/CNTs
	303.15
	5.64
	4.67
	20.7

	
	308.15
	5.68
	3.61
	15.7

	
	313.15
	5.41
	3.30
	14.7

	
	323.15
	5.15
	1.94
	9.40

	
	333.15
	4.45
	1.26
	6.45


Reference
1.
Ye F, et al. Reversible Ammonium Ion Intercalation/de-intercalation with Crystal Water Promotion Effect in Layered VOPO4·2H2O. Angew Chem Int Ed 62, e202303480 (2023).

2.
Liu Q, et al. MnAl Layered Double Hydroxides: A Robust Host for Aqueous Ammonium-Ion Storage with Stable Plateau and High Capacity. Adv Energy Mater 13, 2202908 (2022).

3.
Chen L, et al. How Prussian Blue Analogues Can Be Stable in Concentrated Aqueous Electrolytes. ACS Energy Lett 7, 1672−1678 (2022).

4.
Song Y, et al. Ammonium-Ion Storage Using Electrodeposited Manganese Oxides. Angew Chem Int Ed 60, 5718−5722 (2021).

5.
Liang G, et al. Initiating Hexagonal MoO3 for Superb-Stable and Fast NH4+ Storage Based on Hydrogen Bond Chemistry. Adv Mater 32, e1907802 (2020).

6.
Dong S, et al. Ultra-fast NH4+ Storage: Strong H Bonding between NH4+ and Bi-layered V2O5. Chem 5, 1537−1551 (2019).



S20

