Supplementary Information

Single Ru site dispersed Cu nanocluster dual sites enables outstanding photocatalytic CO2 reduction

Lizhen Liu,1,2† Jingcong Hu,3† Yuan Sheng,4 Hossein Akhoundzadeh,2 Wenguang Tu,5 Wei Jian Samuel Siow,2,6,7 Hongwei Huang,1* Rong Xu2,8*

1Engineering Research Center of Ministry of Education for Geological Carbon Storage and Low Carbon Utilization of Resources, Beijing Key Laboratory of Materials Utilization of Nonmetallic Minerals and Solid Wastes, National Laboratory of Mineral Materials, School of Material Sciences and Technology, China University of Geosciences (Beijing), Beijing 100083, China

2School of Chemistry, Chemical Engineering and Biotechnology, Nanyang Technological University, Singapore 637459, Singapore

3Beijing Key Laboratory of Microstructure and Properties of Solids, Faculty of Materials and Manufacturing, Beijing University of Technology, Beijing 100124, China

4College of Chemical Engineering, Zhejiang University of Technology, Hangzhou 310014, China

5School of Science and Engineering, The Chinese University of Hong Kong (Shenzhen) Guangdong 518172, China

6Singapore Membrane Technology Centre, Nanyang Environment and Water Research Institute, Nanyang Technological University, Singapore 637141, Singapore

7Nanyang Environment and Water Research Institute, Interdisciplinary Graduate Programme, Nanyang Technological University, Singapore

8C4T CREATE, National Research Foundation, CREATE Tower 1 Create Way, Singapore 138602, Singapore

†These authors contributed equally to this work.

*Corresponding author: hhw@cugb.edu.cn (Hongwei Huang); rxu@ntu.edu.sg (Rong Xu)

Supplementary Text

Fig. S1. XRD patterns of BTO, BTOCux (x = 1, 2, 5, 10) and BTOCuyRu0.5 (y = 2, 10).

The detailed information about the purity and crystallinity of the samples is obtained by XRD analysis. The diffraction peaks of BTO coincide with the standard peaks of Bi4Ti3O12 (PDF#72-1019). The strong peaks indicate good crystallinity. In addition, no other phases can be found in the series of BTO samples, indicating that the introduction of Cu and Ru loading does not produce impurities or change the crystal structure.

Fig. S2. SEM images of a BTO, b BTOT, c-f BTOCux (x = 1, 2, 5, and 10) and g-h BTOCuyRu0.5 (y = 2 and 10) (the scale bar is 100 nm).

Fig. S3. TEM images of a BTO, b the enlarged area in a, c BTOT, d-g BTOCux (x = 1, 2, 5, 10) and h-i BTOCuyRu0.5 (y = 2, 10).

Fig. S4. Size distribution histograms of metal clusters obtained from TEM images (Fig. 3).

Fig. S5. HAADF-STEM images and corresponding elemental mapping of a-b BTOCu2, c-d BTOCu10 and e-f BTOCu10Ru0.5.

Fig. S6. Fitting results of FT spectrum of a Cu foil, b Cu2O and c CuO at Cu K-edge.

Fig. S7. Fitting results of FT spectrum of a Ru foil and b RuO2 at Ru K-edge.

Fig. S8. XPS spectra: a survey, b Bi 4f, c Ti 2p and d O 1s of BTO, BTOCu2, BTOCu10, BTOCu2Ru0.5 and BTOCu10Ru0.5.

XPS spectra of Bi 4f and Ti 2p of BTO, BTOCu2, BTOCu10, BTOCu2Ru0.5 and BTOCu10Ru0.5 show no obvious difference. O 1s of BTOCu2, BTOCu10, BTOCu2Ru0.5 and BTOCu10Ru0.5 differs from that of BTO, which indicates that Cu nanocluster successfully anchors on BTO surface and Cu atoms adjacent to the surface coordinate with surface O atoms. O 1s at 529.7 eV is associated with O in lattice Bi-O. O 1s of lattice Ti-O is up-shifted from 531.3 eV to 531.6 eV, which shows that Cu-O coordination influences the Ti-O coordination, confirming Cu atoms adjacent to the surface coordinate with surface O atoms.

Fig. S9. GC curves during gas sample analysis over BTOCu2Ru0.5.

Fig. S10. GC curves during gas sample analysis over BTOCu2Ru0.5.

Fig. S11. Control experiments: CO production from CO2 photoreduction over BTO, BTOCux (x = 1, 2, 5, 10) and BTOCuyRu0.5 (y = 2, 10) samples (15 mg) without a CO2 (Ar atmosphere) and without b CO2 and acetonitrile (Ar atmosphere and ultra-pure water as solvent).

Fig. S12. a HAADF-STEM images and b-d corresponding element mapping of BTOCu2Ru0.5 after 12 h of reaction time.

Fig. S13. XPS spectra: a Bi 4f, b Ti 2p, c O1s, d Cu 2p and e Ru 3d of BTOCu2Ru0.5 before and after reaction.

Fig. S14. GC-MS curves during gas sample analysis.

Fig. S15. In situ FTIR spectra for dark adsorption over a BTOCu2Ru0.5 and b BTOCu10 before illumination (data collected at 1, 2, 3, 4, 5, 10 and 20 min from bottom to top).

Fig. S16. In situ FTIR spectra for CO2 photoreduction process under 300 W Xe lamp over a BTOCu2Ru0.5 and b-d BTOCu10 (data collected at 2, 4, 6, 8, 10, 20, 30, 40, 50 and 60 min from bottom to top).

Fig. S17. DRS spectra of BTO, BTOT, BTOCux (x = 1, 2, 5, 10) and BTOCuyRu0.5 (y = 2, 10).

Fig. S18. PL spectra of BTO, BTOCu2, BTOCu10, BTOCu2Ru0.5 and BTOCu10Ru0.5.

Fig. S19. CO2 TPD curves of BTO, BTOCu2 and BTOCu2Ru0.5.

Fig. S20. Calculated structures of CO2 adsorbed on a BTO, b BTOCu2 and c site 1, d site 2, e site 3 of BTOCu2Ru0.5.

Table S1. EXAFS fitting parameters of the Cu K-edge.

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor | S02 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cu foil | Cu-Cu | 12 | 2.550±0.010 | 0.01022 | 5.86 | 0.0068 | 0.92 |
| Cu2O | Cu-O | 2 | 1.862±0.023 | 0.00415 | 7.07 | 0.0048 | 0.67 |
|  | Cu-Cu | 12 | 3.019± 0.016 | 0.03986 |  |  |  |
| CuO | Cu-O | 4 | 1.946± 0.006 | 0.00532 | -1.11 | 0.0152 | 0.79 |
|  | Cu-Cu | 12 | 2.960±0.027 | 0.02571 |  |  |  |
| BTOCu2Ru0.5 | Cu-O | 2.2 | 1.946± 0.107 | 0.00429 | 0.41 | 0.007 | 0.80 |
|  | Cu-Cu | 1.2 | 2.688± 0.069 | 0.01749 |  |  |  |
|  | Cu-Ru | 2 | 3.918±0.224 | 0.02043 |  |  |  |

aCN, coordination number; bR, the distance to the neighboring atom; cσ2, the Mean Square Relative Displacement (MSRD); dΔE0, inner potential correction; R factor indicates the goodness of the fit. Fitting range: 3.0 ≤ k (/Å) ≤ 10.0 and 1.0 ≤ R (Å) ≤ 3.0 (Cu foil); 3.0 ≤ k (/Å) ≤ 10.0 and 1.0 ≤ R (Å) ≤ 3.5 (Cu2O); 3.0 ≤ k (/Å) ≤ 10.0 and 1.0 ≤ R (Å) ≤ 3.0 (CuO); 3.0 ≤ k (/Å) ≤ 8.0 and 1.0 ≤ R (Å) ≤ 4.0 (BTOCu2Ru0.5). A reasonable range of EXAFS fitting parameters: 0.700 < Ѕ02 < 1.000; CN > 0; σ2 > 0 Å2; |ΔE0| < 15 eV; R factor < 0.02.

Table S2. EXAFS fitting parameters of the Ru K-edge.

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Ru-foil | Ru-Ru | 12* | 2.674±0.004 | 0.0030±0.0007 | 3.0±0.9 | 0.0089 |
| RuO2 | Ru-O | 6.0±0.4 | 1.962±0.001 | 0.0017±0.0007 | 0.2±0.5 | 0.0082 |
|  | Ru-Ru | 10.4±0.9 | 3.141±0.001 | 0.0101±0.0001 | -1.2±0.6 |  |
|  | Ru-Ru | 4.4±0.3 | 3.585±0.001 | 0.0004±0.0001 | 8.0±0.7 |  |
| BTOCu2Ru0.5 | Ru-O | 5.2±0.2 | 2.014±0.001 | 0.0045±0.0006 | 0.7±0.3 | 0.0021 |
|  | Ru-Cu | 2.5±0.1 | 2.498±0.001 | 0.0089±0.0008 | 3.7±0.4 |  |
|  | Ru-Ru | 3.1±0.3 | 2.713±0.001 |  |  |  |

aCN, coordination number; bR, the distance to the neighboring atom; cσ2, the Mean Square Relative Displacement (MSRD); dΔE0, inner potential correction; R factor indicates the goodness of the fit. S02 was fixed to 0.728, according to the experimental EXAFS fit of Au foil by fixing CN as the known crystallographic value. * This value was fixed during EXAFS fitting, based on the known structure of Au. Fitting range: 3.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.0 (Ru foil); 3.0 ≤ k (/Å) ≤ 12.0 and 1.0 ≤ R (Å) ≤ 3.8 (RuO2); 3.0 ≤ k (/Å) ≤12.0 and 1.0 ≤ R (Å) ≤ 3.0 (BTOCu2Ru0.5). A reasonable range of EXAFS fitting parameters: 0.700 < Ѕ02 < 1.000; CN > 0; σ2 > 0 Å2; |ΔE0| < 15 eV; R factor < 0.02.

Table S3. Comparison of the CO2 photoreduction activity of BTOCu2Ru0.5 with selected dual sites, Cu site and bismuth-based photocatalysts reported in the literature.

| Photocatalysts | Light source |  | Reaction system |  | Production (µmolg-1h-1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| BTOCu2Ru0.5 | A 300 W Xe lamp |  | Without photosensitizer and sacrificial reagent |  | CO: ~180.7 | This work |
| Cu-ZnTCPP/g-C3N4 hybrid | A 300 W Xe lamp (λ: 360-800 nm; 150 mW/cm2) |  | As above |  | CO: 92.0 | 1 |
| C–TiO2–Cu | A 300 W Xe lamp (λ = 320–780 nm) |  | As above |  | CO: 53.4 | 2 |
| Cu1N3@PCN | Visible light |  | As above |  | CO: 49.8 | 3 |
| Cu-substituted ZnIn2S4 | A 300 W Xe lamp with an AM 1.5G filter (112 mW/cm2) |  | As above |  | CO: 47.2 | 4 |
| Cu nanoclusters modified TiO2 with oxygen vacancies | A 300 W Xe lamp |  | As above |  | CO: 40.3 | 5 |
| Cu1.95S@CuS | A 300 W Xe lamp with an AM 1.5G filter |  | As above |  | CO: 28.6 | 6 |
| CoRu-HCNp | A 300 W Xe lamp |  | As above |  | CO: 27.3 | 7 |
| Bi4O5I2–Fe30 | A 300 W Xe lamp |  | As above |  | CO: 23.77; CH4: 4.98 | 8 |
| TOC/Cu-MOF | A 300 W Xe lamp |  | As above |  | CO: 23.01 | 9 |
| SrBi4Ti4O15 | A 300 W Xe lamp |  | As above |  | CO: 19.8 | 10 |
| Bi2MoO6 | A 300 W Xe lamp |  | As above |  | CO: 14.38 | 11 |
| Cu/C3N4 | A 350 W Xe lamp |  | As above |  | CO: 9.89 | 12 |
| Au/Co loaded CdS NPs |  | A 300 W Xe lamp with 400 nm filter |  | As above | CO: 9.16; CH4: 1.1 | 13 |
| SrBi2Nb2O9 | A 300 W Xe lamp |  | As above |  | CH4: 8.75 | 14 |
| Cu-CCN | A 300 W Xe lamp |  | As above |  | CO: 3.086 | 15 |
| Ru@Cu-HHTP | A Xe lamp (λ > 400 nm; 100 mW/cm2) |  | TEOA as the sacrificial reagent |  | CO: 130(5)000 | 16 |
| Isolated square-planar Cu center in boron imidazolate nanocages | Visible light |  | [Ru(bpy)3]Cl2 as the photosensitizer; TEOA as the sacrificial reagent |  | CO: 3334 | 17 |
| CoNi-COF-3 | A 300 W Xe lamp with a 420 nm cutoff filter |  | TEOA as the sacrificial agent; [Ru(bpy)3]Cl2·6H2O as the photosensitizer |  | CO: 2567 | 18 |
| Cu-cobalt carbonate hydroxide | A 300 W xenon lamp a 420 nm cutoff filter |  | TEOA as the sacrificial agent; Ru(bpy)32+(bpy=2,2’-bipyridine) as the photosensitizer |  | CO: 1627.58 | 19 |
| P/Cu SAs@CN | A 300 W Xe lamp |  | TEOA as the sacrificial agent |  | C2H6: 616.6 | 20 |
| PCN-224(Cu)/TiO2 | A 300 W Xe lamp (λ > 300 nm) |  | Poly(3, 4-ethylenedioxythiophene)/poly(styrenesulfonate) (PEDO/TPSS) aqueous solution |  | CO: 37.21 | 21 |
| InCu/PCN | A 300 W Xenon lamp) at 1 W/cm-2 light intensity |  | DMF as the sacrificial agent |  | Ethanol: 28.5 | 22 |
| Cu2O@Cu@UiO-66-NH2 | A long-pass filter (λ ≥ 400 nm) |  | TEOA as the sacrificial reagent |  | CO: 20.9 | 23 |
| PCN-RuCu | A 300 W Xe lamp |  | TEOA as the sacrificial agent |  | CO: 0.25; CH4: 19.25 | 24 |
| Sn-Cu/C3N4 | A 300 W Xe lamp with a 420 nm cut-off filter |  | TEA as the sacrificial agent |  | HCHO: 10.80 | 25 |
| Cu purpurin chromophore | Light-emitting diode (λ > 400 nm) |  | DMF as solution; BIH as the sacrificial donor |  | CO: ~0.71 (0.1 mM catalysts) | 26 |

Supplementary References

- S. Xie, C. Deng, Q. Huang, C. Zhang, C. Chen, J. Zhao, H. Sheng, Facilitated photocatalytic CO2 reduction in aerobic environment on a copper-porphyrin metal–organic framework. Angew. Chem. Int. Ed. 62, e202216717 (2013).

- Z. Tai, G. Sun, T. Wang, Z. Li, J. Tai, Netted C-doped TiO2 mesoporous nanostructure decorated by Cu nanoparticles for photocatalytic CO2 reduction. ACS Appl. Nano Mater. 5, 18070–18079 (2022).

- X. Sun, L. Sun, G. Li, Y. Tuo, C. Ye, J. Yang, J. Low, X. Yu, J. H. Bitter, Y. Lei, D. Wang, Y. Li, Phosphorus tailors the d-band center of copper atomic sites for efficient CO2 Photoreduction under visible-light irradiation. Angew. Chem. Int. Ed. 62, e202207677 (2022).

- L. Xiao, C. Yuan, P. Chen, Y. Liu, J. Sheng, S. Zhang, F. Dong, Y. Sun, Cu–S bonds as an atomic-level transfer channel to achieve photocatalytic CO2 reduction to CO on Cu-substituted ZnIn2S4. ACS Sustainable Chem. Eng. 10, 11902–11912 (2022).

- X. Bao, M. Zhang, Z. Wang, D. Dai, P. Wang, H. Cheng, Y. Liu, Z. Zheng, Y. Dai, B. Huang, Molten-salt assisted synthesis of Cu clusters modified TiO2 with oxygen vacancies for efficient photocatalytic reduction of CO2 to CO. Chem. Eng. J. 445, 136718 (2022).

- X. Shi, L. Wang, W. Dai, X. Dong, Y. Bai, L. Ye, CO2 photoreduction catalyzed by Cu-deficient Cu1.95S@CuS: enhanced performance via boosted directional interfacial charge transfer. ACS Catal. 13, 5264–5271 (2023).

- L. Cheng, X. Yue, L. Wang, D. Zhang, P. Zhang, J. Fan, Q. Xiang, Dual-single-atom tailoring with bifunctional integration for high-performance CO2 photoreduction. Adv. Mater. 33, 2105135 (2021).

- X. Jin, Y. Xu, X. Zhou, C. Lv, Q. Huang, G. Chen, H. Xie, T. Ge, J. Cao, J. Zhan, L. Ye, Single-atom Fe triggers superb CO2 photoreduction on a bismuth-rich catalyst. ACS Mater. Lett. 3, 364-371 (2021).

- Q. Wu, H. Ma, Y. Wang, J. Chen, J. Dai, X. Xu, X. Wu, Surface electron localization in Cu-MOF-bonded double-heterojunction Cu2O induces highly efficient photocatalytic CO2 reduction. ACS Appl. Mater. Interfaces 14, 54328–54337 (2022).

- S. Tu, Y. Zhang, A. H. Reshak, S. Auluck, L. Ye, X. Han, T. Ma, H. Huang, Ferroelectric polarization promoted bulk charge separation for highly efficient CO2 photoreduction of SrBi4Ti4O15. Nano Energy 56, 840-850 (2019).

- S. Li, L. Bai, N. Ji, S. Yu, S. Lin, N. Tian, H. Huang, Ferroelectric polarization and thin-layered structure synergistically promoting CO2 photoreduction of Bi2MoO6. J. Mater. Chem. A 8, 9268-9277 (2020).

- G. Shi, L. Yang, Z. Liu, X. Chen, J. Zhou, Y. Yu, Photocatalytic reduction of CO2 to CO over copper decorated g-C3N4 nanosheets with enhanced yield and selectivity. Appl. Surf. Sci. 427, 1165-1173 (2018).

- Y. Zhang, B. Johannessen, P. Zhang, J. Gong, J. Ran, S.-Z. Qiao, Reversed electron transfer in dual single atom catalyst for boosted photoreduction of CO2. Adv. Mater. 35, 2306923 (2023).

- H. Yu, F. Chen, X. Li, H. Huang, Q. Zhang, S. Su, K. Wang, E. Mao, B. Mei, G. Mul, T. Ma, Y. Zhang, Synergy of ferroelectric polarization and oxygen vacancy to promote CO2 photoreduction. Nat. Commun. 12, 4594 (2021).

- Y. Li, B. Li, D. Zhang, L. Cheng, Q. Xiang, Crystalline carbon nitride supported copper single atoms for photocatalytic CO2 reduction with nearly 100% CO selectivity. ACS Nano 14, 10552–10561 (2020).

- N.-Y. Huang, H. He, S. Liu, H.-L. Zhu, Y.-J. Li, J. Xu, J.-R. Huang, X. Wang, P.-Q. Liao, X.-M. Chen, Electrostatic attraction-driven assembly of a metal–organic framework with a photosensitizer boosts photocatalytic CO2 reduction to CO. J. Am. Chem. Soc. 143, 17424–17430 (2021).

- H.-X. Zhang, Q.-L. Hong, J. Li, F. Wang, X. Huang, S. Chen, W. Tu, D. Yu, R. Xu, T. Zhou, J. Zhang, Isolated square-planar copper center in boron imidazolate nanocages for photocatalytic reduction of CO2 to CO. Angew. Chem. Int. Ed. 58, 11752 (2019).

- J. Wang, W. Zhu, F. Meng, G. Bai, Q. Zhang, X. Lan, Integrating dual-metal sites into covalent organic frameworks for enhanced photocatalytic CO2 reduction. ACS Catal. 13, 4316−4329 (2023).

- H. Liu, Y. Chen, H. Li, G. Wan, Y. Feng, W. Wang, C. Xiao, G. Zhang, Y. Xie, Construction of asymmetrical dual Jahn–Teller sites for photocatalytic CO2 reduction. Angew. Chem. Int. Ed. 62, e202304562 (2023).

- G. Wang, Z. Chen, T. Wang, D. Wang, J. Mao, P and Cu dual sites on graphitic carbon nitride for photocatalytic CO2 reduction to hydrocarbon fuels with high C2H6 evolution. Angew. Chem. Int. Ed. 61, e202210789 (2022).

- L. Wang, P. Jin, J. Huang, H. She, Q. Wang, Integration of Copper(II)-porphyrin zirconium metal–organic framework and titanium dioxide to construct Z-scheme system for highly improved photocatalytic CO2 reduction. ACS Sustainable Chem. Eng. 7, 15660–15670 (2019).

- H. Shi, H. Wang, Y. Zhou, J. Li, P. Zhai, X. Li, G. G. Gurzadyan, J. Hou, H. Yang, X. Guo, Atomically dispersed indium-copper dual-metal active sites promoting C-C coupling for CO2 photoreduction to ethanol. Angew. Chem. Int. Ed. 61, e202208904 (2022).

- S.-Q. Wang, X.-Y. Zhang, X.-Y. Dao, X.-M. Cheng, W.-Y. Sun, Cu2O@Cu@UiO-66-NH2 ternary nanocubes for photocatalytic CO2 reduction. ACS Appl. Nano Mater. 3, 10437–10445 (2020).

- L. Zeng, J.-W. Chen, L. Zhong, W. Zhen, Y. Y. Tay, S. Li, Y.-G. Wang, L. Huang, C. Xue, Synergistic effect of Ru-N4 sites and Cu-N3 sites in carbon nitride for highly selective photocatalytic reduction of CO2 to methane. Appl. Catal., B 307, 121154 (2022).

- B. Kim, D. Kwon, J.-O. Baeg, M. Austeria P, G. H. Gu, J.-H. Lee, J. Jeong, W. Kim, W. Choi, Dual-atom-site Sn-Cu/C3N4 photocatalyst selectively produces formaldehyde from CO2 reduction. Adv. Funct. Mater. 33, 2212453 (2023).

- H. Yuan, B. Cheng, J. Lei, L. Jiang, Z. Han, Promoting photocatalytic CO2 reduction with a molecular copper purpurin chromophore. Nat. Commun. 12, 1835 (2021).