Supplementary Information

Modulating Electronic Structure of Metal-Organic Frameworks by Introducing Atomically Dispersed Ru for Efficient Hydrogen Evolution

Sun et al.

Supplementary Figure 1. SEM images of different catalysts. (a) and (d) Ni-BDC, (b) and (e) NiRu0.09-BDC, (c) and f) NiRu0.21-BDC .

Supplementary Figure 2. XRD patterns of Ni-BDC, NiRu0.09-BDC, NiRu0.13-BDC and NiRu0.21-BDC on nickel foam.

Supplementary Figure 3. XRD patterns of NiRu0.13-BDC powder.

Supplementary Figure 4. XPS spectroscopic studies. (a) C 1s and Ru 3d spectra of Ni-BDC and NiRu0.13-BDC. (b) Ru 3p spectra of NiRu0.21-BDC.

Supplementary Table 1. The molar ratio of Ni/Ru in NiRux-BDC.

| Molar ratio(Ni:Ru) | NiRu0.09-BDC | NiRu0.13-BDC | NiRu0.21-BDC |
| --- | --- | --- | --- |
| ICP-MS analysis | 1:0.09 | 1:0.13 | 1:0.21 |

Supplementary Figure 5. X-ray absoption spectra. (a) The magnified Ru K-edge XANES spectra of NiRu0.13-BDC, Ru foil and RuO2, respectively. (b) Ru K-edge EXAFS oscillation functions k3 of NiRu0.13-BDC, Ru foil, and RuO2, respectively.

Supplementary Figure 6. X-ray absoption spectroscopic studies. (a) Ni K-edge Fourier transformed EXAFS spectra of Ni-BDC and NiRu0.13-BDC. (b) Ni K-edge EXAFS oscillation functions k3 of Ni-BDC and NiRu0.13-BDC, respectively.

Supplementary Figure 7. HER performance. (a) The corresponding overpotentials in 1M PBS and (b) in 1 M KOH of Ni-BDC, NiRu0.09-BDC, NiRu0.13-BDC and NiRu0.21-BDC at 10 mA cm-2 and 100 mA cm-2. (c) LSV curves of Ni-BDC, NiRu0.09-BDC, NiRu0.13-BDC and NiRu0.21-BDC toward HER in 1 M HCl. (d) The corresponding overpotentials of different catalysts in 1M HCl.

Supplementary Table 2. Comparisons of HER activity for NiRu0.13 and other reported state of art elelctrocatalysis.

| Catalyst | Media | Overpotential at 10 mA cm-2 (mV) | Substrate | Reference |
| --- | --- | --- | --- | --- |
| NiRu0.13-BDC | 1 M PBS | 36 | Nickel foam | This work |
|  | 1 M KOH | 32 | Nickel foam | This work |
|  | 1 M HCl | 11 | Nickel foam | This work |
| karst NF | 1 M PBS | 60 | Nickel foam | 1 |
| CrOx/Cu–Ni | 1 M PBS | 48 | Cu foam | 2 |
| Ni0.89Co0.11Se2 MNSN/ NF | 1 M PBS | 82 | Nickel foam | 3 |
| N–Co2P/CC | 1 M PBS | 42 | Carbon cloth | 4 |
| NiCo2Px/CF | 1 M PBS | 63 | Carbon fiber | 5 |
| Mn-CoP/Ti | 1 M PBS | 86 | Ti mesh | 6 |
| PtSA‐NT‐NF | 1 M PBS | 24 | Nickel foam | 7 |
| N-Ni | 1 M PBS | 64 | Nickel foam | 8 |
| N,Mn-MoS2/NF | 1 M PBS | 70 | Nickel foam | 9 |
| NiFeRu-LDH | 1 M KOH | 29 | nickel foam | 10 |
| Ni, Zn dual-doped CoO NRs | 1 M KOH | 53 | CFP | 11 |
| R-MoS2/NF | 1 M KOH | 71 | nickel foam | 12 |
| CoSe2 | 1 M KOH | 79 | nickel foam | 13 |
| Ni−N0.19 | 1 M KOH | 42 | CFP | 14 |
| Ni3N/Ni foam | 1 M KOH | 100 | nickel foam | 15 |
| V8C7 | 0.5 M H2SO4 | 38 | nickel foam | 16 |
| CoMoNiS-NF-31 | 0.5 M H2SO4 | 103 | nickel foam | 17 |
| FLNPC@MoP-NC/MoP-C | 0.5 M H2SO4 | 74 | Carbon Fiber | 18 |
| Mo2C-MoOx/CC( | 1 M HClO4 | 74 | Carbon cloth | 19 |
| Fe-doped CoP/Ti | 0.5 M H2SO4 | 78 | Ti mesh | 20 |

Supplementary Figure 8. Turnover frequency (TOF) of different materials at an overpotential of 100 mV.

Supplementary Figure 9. CV plots and double-layer capacitance of different catalysts. CV plots of (a) Ni-BDC, (b) NiRu0.09-BDC, (c) NiRu0.13-BDC and (d) NiRu0.21-BDC at different scan rates. (e) Double-layer capacitance of Ni-BDC, NiRu0.09-BDC, NiRu0.13-BDC and NiRu0.21-BDC.

Supplementary Figure 10. Electrochemical performance of NiRu0.13-BDC. (a) Electrochemical impedance spectra of different catalysts, (b) chronoamperometry curves of NiRu0.13-BDC in 1 M PBS.

Supplementary Table 3. EIS results of Ni-BDC, NiRu0.09-BDC, NiRu0.13-BDC and NiRu0.21-BDC

| Catalyst | Solution series resistances Rs (Ω) | Charge transfer resistance Rct (Ω) |
| --- | --- | --- |
| Ni-BDC | 1.42 | 19.56 |
| NiRu0.09-BDC | 1.45 | 11.41 |
| NiRu0.13-BDC | 1.68 | 0.31 |
| NiRu0.21-BDC | 1.67 | 0.66 |

Supplementary Figure 11. SEM images of NiRu0.13-BDC afters stability test. (a) before HER, (b) (c) after 10h, 30h electrocatalytic stability test at an overpotential of 50 mV in 1 M PBS.

Supplementary Figure 12. XRD patterns of NiRu0.13-BDC before HER, after 10h, 30h electrocatalytic stability test at an overpotential of 50 mV in 1 M PBS.

Supplementary Figure 13. XPS spectra of NiRu0.13-BDC after stability test. (a) Full range XPS patterns, (b) Ru 3p, (c) Ni 2p, (d) O 1s and (e) C 1s and Ru 3d XPS spectra of NiRu0.13-BDC before HER and after 10 h, 30 h electrocatalytic test.

Supplementary Figure 14. Crystal structure models. (a) Ni-BDC, (b) NiRu0.13-BDC.

Supplementary Figure 15. Calculated total DOS of Ni-BDC and NiRu0.13-BDC.

Supplementary Figure 16. Calculated partial density of states (PDOS) of Ni-BDC and NiRu0.13-BDC.

References

1.	Gao, X. et al. Karst landform-featured monolithic electrode for water electrolysis in neutral media. Energy Environ. Sci. 13, 174-182 (2020).

2.	Dinh, C.-T. et al. Multi-site electrocatalysts for hydrogen evolution in neutral media by destabilization of water molecules. Nat. Energy 4, 107-114 (2018).

3.	Liu, B. et al. Nickel-Cobalt Diselenide 3D Mesoporous Nanosheet Networks Supported on Ni Foam: An All-pH Highly Efficient Integrated Electrocatalyst for Hydrogen Evolution. Adv. Mater. 29, 1606521 (2017).

4.	Men, Y. et al. Tailoring the Electronic Structure of Co2P by N Doping for Boosting Hydrogen Evolution Reaction at All pH Values. ACS Catal. 9, 3744-3752 (2019).

5.	Zhang, R. et al. Ternary NiCo2Px Nanowires as pH-Universal Electrocatalysts for Highly Efficient Hydrogen Evolution Reaction. Adv. Mater. 29, 1605502 (2017).

6.	Liu, T. et al. Mn Doping of CoP Nanosheets Array: An Efficient Electrocatalyst for Hydrogen Evolution Reaction with Enhanced Activity at All pH Values. ACS Catal. 7, 98-102 (2016).

7.	Zhang, L., Han, L., Liu, H., Liu, X. & Luo, J. Potential-Cycling Synthesis of Single Platinum Atoms for Efficient Hydrogen Evolution in Neutral Media. Angew. Chem. Int. Ed. 56, 13694-13698 (2017).

8.	You, B. et al. Universal Surface Engineering of Transition Metals for Superior Electrocatalytic Hydrogen Evolution in Neutral Water. J. Am. Chem. Soc. 139, 12283-12290 (2017).

9.	Sun, T. et al. Engineering the Electronic Structure of MoS2 Nanorods by N and Mn Dopants for Ultra-Efficient Hydrogen Production. ACS Catal. 8, 7585-7592 (2018).

10.	Chen, G. et al. Accelerated Hydrogen Evolution Kinetics on NiFe-Layered Double Hydroxide Electrocatalysts by Tailoring Water Dissociation Active Sites. Adv. Mater. 30, 1706279 (2018).

11.	Ling, T. et al. Well-Dispersed Nickel- and Zinc-Tailored Electronic Structure of a Transition Metal Oxide for Highly Active Alkaline Hydrogen Evolution Reaction. Adv. Mater. 31, 1807771 (2019).

12.	Anjum, M. A. R., Jeong, H. Y., Lee, M. H., Shin, H. S. & Lee, J. S. Efficient Hydrogen Evolution Reaction Catalysis in Alkaline Media by All-in-One MoS2 with Multifunctional Active Sites. Adv. Mater. 30, 1707105 (2018).

13.	Zhang, J. Y. et al. Anodic Hydrazine Oxidation Assists Energy-Efficient Hydrogen Evolution over a Bifunctional Cobalt Perselenide Nanosheet Electrode. Angew. Chem. Int. Ed. 57, 7649-7653 (2018).

14.	Li, Y. et al. Processable Surface Modification of Nickel-Heteroatom (N, S) Bridge Sites for Promoted Alkaline Hydrogen Evolution. Angew. Chem. Int. Ed.  58, 461-466 (2019).

15.	Ledendecker, M., Schlott, H., Antonietti, M., Meyer, B. & Shalom, M. Experimental and Theoretical Assessment of Ni-Based Binary Compounds for the Hydrogen Evolution Reaction. Adv. Energy Mater. 7, 1601735 (2017).

16.	Xu, H. et al. A New Platinum-Like Efficient Electrocatalyst for Hydrogen Evolution Reaction at All pH: Single-Crystal Metallic Interweaved V8C7 Networks. Adv. Energy Mater. 8, 1800575 (2018).

17.	Yang, Y. et al. Hierarchical Nanoassembly of MoS2/Co9S8/Ni3S2/Ni as a Highly Efficient Electrocatalyst for Overall Water Splitting in a Wide pH Range. J. Am. Chem. Soc. 141, 10417-10430 (2019).

18.	Liu, B. et al. Few Layered N, P Dual-Doped Carbon-Encapsulated Ultrafine MoP Nanocrystal/MoP Cluster Hybrids on Carbon Cloth: An Ultrahigh Active and Durable 3D Self-Supported Integrated Electrode for Hydrogen Evolution Reaction in a Wide pH Range. Adv. Funct. Mater. 28, 1801527 (2018).

19.	He, L. et al. Molybdenum Carbide-Oxide Heterostructures: In Situ Surface Reconfiguration toward Efficient Electrocatalytic Hydrogen Evolution. Angew. Chem. Int. Ed. 59, 3544-3548 (2020).

20.	Tang, C. et al. Fe-Doped CoP Nanoarray: A Monolithic Multifunctional Catalyst for Highly Efficient Hydrogen Generation. Adv. Mater. 29, 1602441  (2017).