Supporting Information

Poly(benzimidazole)s containing trifluoromethyl substituents and aryl ether linkages for high-temperature proton exchange membrane fuel cell applications

Ping-Yen Chen, Tse-Han Chiu, Tariku Nefo, Hsiao-Wei Hung, Jyh-Chien Chen*

Department of Materials Science and Engineering, National Taiwan University of Science and Technology, 43, Sec. 4, Keelung Rd., Taipei 10607, Taiwan

*Corresponding author. Tel.: +886 2 27376526. E-mail addresses: jcchen@mail.ntust.edu.tw (J.-C. Chen)

Supplement Information:

Fig. S1 13C-1H HSQC spectrum of tetraamine 7

Fig. S2 EI-Mass spectrum of tetraamine 7

Fig. S3 1H NMR spectrum of compound 2

Fig. S4 1H NMR spectrum of compound 3

Fig. S5 1H NMR spectrum of compound 4

Fig. S6 1H NMR spectrum of compound 5

Fig. S7 1H NMR spectrum of compound 6

Table S1 Water uptakes of PBIs membrane

| PBIs | WU (%)a |  |
| --- | --- | --- |
| CF3-PBI-OO | 16 |  |
| OCF3-OPBI [1] | 3 |  |
| OPBI | 4 |  |
| aThe membranes were immersed in water at the room temperature for 24 h. |  |

Table S2 PA uptakes of CF3-PBI-OO and OPBI membranes

| Time (h) | PA uptake (%)a |  |  | Time (h) | PA uptake (%)a | PA uptake (%)a |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | CF3-PBI-OO |  |  |  | OPBI | OCF3-OPBI [1] |  |
|  | 75%b | 65%b | 55%b |  | 85%b | 85%b | 75%b |
| 0.0 | 0 | 0 | 0 | 0.0 | 0 | 0 | 0 |
| 0.3 | 17 | 16 | 15 | 7.0 | 110 | 57 | 85 |
| 0.7 | 44 | 30 | 31 | 15.0 | 160 | 90 | 85 |
| 1.0 | 59 | 41 | 36 | 39.0 | 185 | 101 | 82 |
| 1.3 | 103 | 55 | 42 | 63.0 | 195 | 127 | 93c |
| 1.7 | 166 | 74 | 45 | 87.0 | 199c | 140c | 89 |
| 2.0 | 192 | 85 | 51 | 111.0 | - | 142 | 92 |
| 2.3 | 213 | 108 | 70 |  |  |  |  |
| 2.7 | 271c | 130 | 86 |  |  |  |  |
| 3.0 | 272 | 147c | 93 |  |  |  |  |
| 3.3 | 273 | 149 | 99c |  |  |  |  |
| 3.7 | 273 | 150 | 101 |  |  |  |  |
| aThe membranes were immersed in phosphoric acid solution at the room temperature. bThe concentration of phosphoric acid solution cThe saturated PA uptakes. |  |  |  |  |  |  |  |

Table S3 Proton conductivity of CF3-PBI-OO, OCF3-OPBI, and OPBI membranes

| Polymers | PA uptakea (%) | ADLb (PA/RU) | Proton conductivityc (mS/cm) |  |  |  |  | Ead (kJ/mol) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 80 ℃ | 100 ℃ | 120 ℃ | 140 ℃ | 160 ℃ |  |
| CF3-PBI-OO | 101 | 5.69 | 8.1 | 9.1 | 11.2 | 15.1 | 31.6 | 22.2 |
|  | 150 | 8.45 | 25.0 | 27.5 | 30.9 | 39.0 | 46.2 | 15.9 |
|  | 213 | 12.00 | 28.1 | 50.1 | 56.9 | 91.5 | 115 | 11.8 |
| OCF3-OPBI [1] | 92 | 5.62 | 0.7 | 1.1 | 1.5 | 2.7 | 4.0 | 29.7 |
|  | 101 | 6.17 | 1.0 | 1.6 | 2.5 | 4.1 | 6.2 | 27.2 |
|  | 142 | 8.67 | 2.7 | 3.8 | 5.8 | 8.4 | 11.7 | 21.6 |
| OPBI | 161 | 6.57 | 0.6 | 0.9 | 1.5 | 2.2 | 3.0 | 31.6 |
|  | 199 | 8.13 | 1.2 | 2.0 | 3.1 | 4.3 | 5.3 | 27.7 |
| aPhosphoric acid uptake. bAcid doping level, numbers of PA molecules per repeating unit. cMeasured at anhydrous condition. dCalculated byArrhenius equation: σ=σ0exp(-Ea/RT). |  |  |  |  |  |  |  |  |

Table S4 Cell performance and open circuit voltages of PBI membranes with different PA uptakes

| PBIs | PA uptakec (%) | ADLd (PA/RU) | VOC (V)a,b | Peak power density (mW/cm2)a |
| --- | --- | --- | --- | --- |
| CF3-PBI-OO | 101 | 5.69 | 0.89 | 335 |
|  | 150 | 8.45 | 0.75 | 675 |
|  | 213 | 12.00 | 0.70 | 691 |
| m-PBI | 291 | 15.10 | 0.81 | 573 |
| OPBI | 207 | 8.46 | 0.98 | 453 |
| OCF3-OPBI [1] | 142 | 8.67 | 0.86 | 656 |
| aThe fuel cell was tested at 160 ℃ anhydrous condition. bVOC: open circuit voltages. cPhosphoric acid doping. dAcid doping level, phosphoric acid per repeating unit. |  |  |  |  |  |

Reference

- Chen P-Y, Chiu T-H, Lin F-J, Chen J-C (2022) Polybenzimidazole membranes derived from novel tetraamines containing 2,2′-disubstituted biphenyl structures for high temperature proton exchange membrane fuel cell application. J Membr Sci 654:120569-120578. https://doi.org/10.1016/j.memsci.2022.120569