Supplementary materials

Highly efficient pure-blue organic light-emitting diodes based on rationally designed heterocyclic phenophosphazinine-containing emitters

Longjiang Xing1,†, Jianghui Wang2,†, Wen-Cheng Chen1,3*, Bo Liu1, Guowei Chen1, Xiaofeng Wang1, Season Si Chen,4 Jia-Xiong Chen1,3, Shaomin Ji1,3, Zujin Zhao2,*, Man-Chung Tang4,* and Yanping Huo1,3,5*

1School of Chemical Engineering and Light Industry, Guangdong University of Technology, Guangzhou, 510006, P. R. China

2State Key Laboratory of Luminescent Materials and Devices, Key Laboratory of Luminescence from Molecular Aggregates of Guangdong Province, South China University of Technology, Guangzhou, 510640, P. R. China

3Guangdong Provincial Laboratory of Chemistry and Fine Chemical Engineering Jieyang Center, Jieyang, 515200, P. R. China

4Institute of Materials Research, Tsinghua Shenzhen International Graduate School, Tsinghua University, Shenzhen, 518055, P. R. China

5Analytical & Testing Center, Guangdong University of Technology, Guangzhou, 510006, P. R. China

†These authors contributed equally

*E-mail: wencchen@gdut.edu.cn; mszjzhao@scut.edu.cn; kobetang2021@sz.tsinghua.edu.cn; yphuo@gdut.edu.cn

Quantum chemical calculations

All calculations were performed with Gaussian 16_A03 program package.[1] The ground-state geometries were optimized using the density function theory (DFT) method with B3LYP functional at the basis set level of 6-31G (d), and the ΔEST values were calculated by time-dependent DFT (TD-DFT) method at the B3LYP/6-31G (d) level. The root-mean squared displacement (RMSD) between S0 and S1 molecular geometries was calculated and visualized with the VMD program.[2] NTOs analysis was conducted in Multiwfn 3.7 code.[3] Reorganization energy analysis was carried out using Molecular Materials Property Prediction Package (MOMAP). Based on the optimized S0 molecular geometries, the spin-orbit coupling matrix elements (SOCEMs) between two first singlet and triplet excited states were calculated in B3LYP/G TZVP level using Orca 4.1.2 package.

Analysis of rate constants

The rate constants of radiative decay (kr,S) and nonradiative decay (knr,S) from S1 to S0 states, the rate constants of intersystem crossing (kISC) and reverse intersystem crossing (kRISC) were calculated from the following equations[4]:

kp=1τp ………………………………………………………………………………………(1)

kd=1τd ………………………………………………………………………………………(2)

kr,S = Φpkp + Φpkd ≈ Φpkp ……………………………………………………………………(3)

knr,S = 1 - ΦPLΦPLkr,s ………………………………………………………………………………(4)

kISC = kp - kr,s - knr,s    …………………………………………………………………………(5)

kRISC= (kpkdΦd)/(kISCΦp)  ……………………………………………………………………(6)

Where τp and τd represent the prompt and decay fluorescence lifetime, which determined from transient PL spectra. The kp and kd represent the decay rate constants for prompt and delayed fluorescence, respectively. Φp and Φd indicate prompt and delayed fluorescence components and can be distinguished from the total ΦPL by comparing the integrated intensities of prompt and delayed components in the transient PL spectra.

Synthesis

Commercially available reagents and solvents were used as received unless otherwise noted. BNCz-Br was synthesized according to literature procedures.[5]

Scheme S1. The synthetic routes of BNCz-NPO and BNCz-NPS. (a) Pd2(dba)3, dppf, t-BuONa, toluene, 120 °C, 12 h; (b) DMAP, Boc2O, THF, 80 °C, 12 h; (c) n-BuLi, THF, -78ºC, 1 h; dichloro(phenyl)phosphane, -78ºC, 1 h；30% H2O2 (for 3a) at room temperature, CH2Cl2；or S8 (for 3b) at 110 ºC, 8 h；(d) CF3COOH, CH2Cl2, rt, 12 h; (e) Pd2(dba)3, t-BuONa, t-Bu3PHBF4, toluene, 120 ºC, 12 h.

Synthesis of bis(2-bromophenyl)amine (1). A mixture of 2-bromoaniline (1.72 g, 10 mmol), 1-bromo-2-iodobenzene (4.24 g, 15mmol), Sodium tert-butoxide (2.88 g, 30 mmol), 1,1'-bis(diphenylphosphino)ferrocene (0.554 g, 1 mmol) 40 mL toluene and Pd2(dba)3 (0.45 g, 0.50 mmol) were added and refluxed at 120 °C under nitrogen atmosphere for 12 hours. The mixture was poured into water to quench the reaction and then extracted with dichloromethane. The organic phase was collected and dried over anhydrous Na2SO4. After evaporation of the solvent, the residue was purified via column chromatography using petroleum ether/dichloromethane (10:1, v/v) as an eluent to afford a white solid. (2.59 g, yield: 80%).1H NMR 1H NMR (400 MHz, DMSOd6) δ (ppm): 7.64 (dd, J = 8.0, 1.2 Hz, 2H), 7.36 – 7.24 (m, 2H), 7.07 (dd, J = 8.0, 1.1 Hz, 2H), 7.01 (s, 1H), 6.93 (td, J = 8.0, 1.3 Hz, 2H).

Synthesis of tert-butyl bis(2-bromophenyl)carbamate (2). A mixture of bis(2-bromophenyl)amine (3.24 g, 10 mmol), N,N-dimethyl-4-aminopyridine (0.244 g, 2 mmol) , di-tert-butyl dicarbonate (4.36 g, 20 mmol) and 60 ml THF were added and refluxed at 80°C under nitrogen atmosphere for 12 hours. The mixture was poured into water to quench the reaction and then extracted with dichloromethane. The organic phase was collected and dried over anhydrous Na2SO4. After evaporation of the solvent, the residue was purified via column chromatography using petroleum ether/dichloromethane (3:1, v/v) as eluent to afford white solid. (3.61g, yield: 85%).1H NMR (400 MHz, CDCl3,) δ (ppm): 7.64 (d, J = 6.7 Hz, 2H), 7.43 (d, J = 7.7 Hz, 2H), 7.22 (td, J = 7.8, 1.3 Hz, 2H), 7.10 (td, J = 7.9, 1.5 Hz, 2H), 1.46 (s, 9H).

Synthesis of tert-butyl 10-phenyl-5H-phenophosphazinine-5-carboxylate 10-oxide (3a). Step 1: A mixture of 2 (4.24 g, 10 mmol), and 40 ml THF were added three-neck flash. The flash was evacuated, and refilled with nitrogen for 3 times and the mixture was cooled to -78 °C. n-BuLi (hexane solution, 2.5 M, 30 mmol, 12 mL) was added dropwise under N2, and the resulting mixture was stirred for 1 h at -78 °C. Dichloro(phenyl)phosphane (3.55 g, 20 mmol) was added at -78 ºC and then the reaction mixture was allowed to warm to room temperature overnight. The mixture was poured into water to quench the reaction and then extracted with dichloromethane. The organic phase was collected and dried over anhydrous Na2SO4. After evaporation of the solvent, the mixture was filtered, and the solid was washed with water, ethanol, and dichloromethane, respectively, to afford a white solid. The crude intermediates were directly used to the next step. Step 2: A mixture of the above intermediate (3.75 g, 10 mmol), 30% hydrogen peroxide (H2O2) (20 ml), 30 ml dichloromethane were added and stirred at room temperature under a nitrogen atmosphere for 12 h. The mixture was poured into water to quench the reaction and then extracted with dichloromethane. The organic phase was collected and dried over anhydrous Na2SO4. After evaporation of the solvent, the residue was purified via column chromatography by using petroleum ether/ ethyl acetate (1:1, v/v) as an eluent to afford white solid. (1.76 g, yield: 45%). 1H NMR (400 MHz, CDCl3,) δ (ppm): 8.12 (ddd, J = 12.2, 7.5, 1.0 Hz, 2H), 7.67 (dt, J = 13.2, 6.6 Hz, 2H), 7.59 – 7.37 (m, 7H), 7.32 (td, J = 7.5, 3.0 Hz, 2H), 1.28 (s, 9H). 31P NMR (162 MHz, CDCl3) δ (ppm): 16.92 (s).

Synthesis of tert-butyl 10-phenyl-5H-phenophosphazinine-5-carboxylate 10-sulfide (3b). Step 1: the same as synthetic 3a. Step 2: A mixture of the above intermediate (3.75 g, 10 mmol), 3sulfur (0.97 g, 30 mmol), 30 ml toluene were added and stirred at 110 °C under a nitrogen atmosphere for 12 h. The mixture was poured into water to quench the reaction and then extracted with dichloromethane. The organic phase was collected and dried over anhydrous Na2SO4. After evaporation of the solvent, the residue was purified via column chromatography using petroleum ether/ ethyl acetate (8:1, v/v) as eluent to afford white solid. (1.62g, yield: 40%). 1H NMR (400 MHz, DMSOd6) δ (ppm): 8.16 (ddd, J = 14.8, 7.6, 1.4 Hz, 2H), 7.80 – 7.72 (m, 2H), 7.72 – 7.65 (m, 2H), 7.63 – 7.54 (m, 2H), 7.49 – 7.41 (m, 1H), 7.42 – 7.34 (m, 2H), 7.32 – 7.21 (m, 2H), 1.20 (s, 9H). 31P NMR (162 MHz, DMSOd6) δ (ppm): 20.73 (s).

Synthesis of 10-phenyl-5H-phenophosphazinine 10-oxide (NPO). A mixture of 3a (1.17 g, 3 mmol), trifluoroacetic acid (6.9 ml, 90 mmol), and 20 ml CH2Cl2 were added and refluxed at room temperature under a nitrogen atmosphere for 12 hours. The mixture was poured into water to quench the reaction and then extracted with dichloromethane. The organic phase was collected and dried over anhydrous Na2SO4. After evaporation of the solvent, the residue was purified via column chromatography using petroleum ether/ ethyl acetate (1:1, v/v) as an eluent to afford a white solid. (0.59 g, yield: 68%). 1H NMR (400 MHz, DMSOd6) δ (ppm): 10.40 (s, 1H), 7.69 – 7.36 (m, 9H), 7.26 (dd, J = 8.0, 5.9 Hz, 2H), 7.02 (t, J = 7.3 Hz, 2H). 31P NMR (162 MHz, DMSOd6) δ (ppm): 4.45 (s).

Synthesis of 10-phenyl-5H-phenophosphazinine 10-sulfide (NPS). A mixture of 3b (1.22 g, 3 mmol), trifluoroacetic acid (6.9 ml, 90 mmol), and 20 ml CH2Cl2 were added and refluxed at room temperature under a nitrogen atmosphere for 12 h. The mixture was poured into water to quench the reaction and then extracted with dichloromethane. The organic phase was collected and dried over anhydrous Na2SO4. After evaporation of the solvent, the residue was purified via column chromatography using petroleum ether/ethyl acetate (8:1, v/v) as an eluent to afford a white solid. (0.60 g, yield: 65%).1H NMR (400 MHz, DMSOd6) δ (ppm):10.30 (s, 1H), 7.72 (dd, J = 14.9, 7.7 Hz, 2H), 7.48 (dd, J = 28.4, 21.8 Hz, 7H), 7.31 – 7.15 (m, 2H), 7.08 (t, J = 7.1 Hz, 2H). 31P NMR (162 MHz, DMSOd6) δ (ppm): 16.92 (s).

Synthesis of BNCz-NPO. A mixture of NPO (1.45 g, 5 mmol), (t-Bu)3P•BF4(6.9 ml, 0.25 mmol), Sodium tert-butoxide (0.98 g, 10 mmol), BNCz-Br (2.15 g, 3 mmol), 40 mL toluene and Pd2(dba)3 (0.23 g, 0.50 mmol) were added and refluxed at 120 °C under nitrogen atmosphere for 12 hours. The mixture was poured into water to quench the reaction and then extracted with dichloromethane. The organic phase was collected and dried over anhydrous Na2SO4. After evaporation of the solvent, the residue was purified via column chromatography using petroleum ether/ ethyl acetate (2:1, v/v) as eluent to afford white solid. (1.53 g, yield: 55%).1H NMR (400 MHz, CDCl3,) δ (ppm): 8 9.20 (d, J = 1.7 Hz, 2H), 8.52 (d, J = 1.6 Hz, 2H), 8.31 (s, 2H), 8.26 (d, J = 1.9 Hz, 2H), 8.18 (d, J = 8.8 Hz, 2H), 7.89 (dddd, J = 13.5, 9.1, 6.7, 1.6 Hz,4H), 7.66 – 7.51 (m, 5H), 7.31 (s, 2H), 7.10 (s, 2H), 6.88 (dd, J = 8.7, 6.2 Hz, 2H), 1.70 (s, 18H), 1.48 (s, 18H); 13C NMR (101 MHz, CDCl3) δ (ppm): 146.60, 146.19, 145.51, 145.13, 144.92, 144.87, 141.69, 138.07, 135.88, 134.73, 132.85, 132.27, 132.24, 132.22, 132.14, 131.53, 131.51, 130.00, 128.57, 128.44, 127.25, 124.87, 124.04, 121.61, 121.50, 121.25, 117.43, 117.31, 117.24, 114.47, 114.27, 113.44, 109.37, 35.31, 34.85, 32.22, 31.77; 31P NMR (162 MHz, CDCl3) δ (ppm): 5.13 (s). HRMS (ESI) m/z: [M + H]+ calcd for C64H61BN3OP, 930.4718; found, 930.4717.

Synthesis of BNCz-NPS. A mixture of NPS (1.53 g, 5 mmol), (t-Bu)3P•BF4(6.9 ml, 0.25 mmol), Sodium tert-butoxide (0.98 g, 10 mmol), BNCz-Br (2.15 g, 3 mmol), 40 mL toluene and Pd2(dba)3 (0.23 g, 0.50 mmol) were added and refluxed at 120 °C under nitrogen atmosphere for 12 hours. The mixture was poured into water to quench the reaction and then extracted with dichloromethane. The organic phase was collected and dried over anhydrous Na2SO4. After evaporation of the solvent, the residue was purified via column chromatography using petroleum ether/ ethyl acetate (10:1, v/v) as eluent to afford white solid. (1.41 g, yield: 50%).1H NMR (400 MHz, CDCl3,) δ (ppm): 9.09 (d, J = 1.4 Hz, 2H), 8.88 (d, J = 1.5 Hz, 2H), 8.57 (d, J = 1.9 Hz, 2H), 8.34 (s, 2H), 8.16 (d, J = 8.9 Hz, 2H), 8.04 (ddd, J = 15.7, 7.7, 1.2 Hz, 2H), 7.71 (ddd, J = 14.0, 6.5, 3.0 Hz, 2H), 7.66 – 7.55 (m, 5H), 7.42 (t, J = 7.8 Hz, 2H), 7.26 (t, J = 7.3 Hz, 2H), 6.94 (dd, J = 8.4, 6.4 Hz, 2H), 1.66 (s, 18H), 1.45 (s, 18H); 13C NMR (101 MHz, CDCl3) δ (ppm): 146.52, 146.21, 145.57, 144.95, 144.21, 144.18, 141.74, 138.32, 138.12, 137.44, 132.74, 132.66, 130.93, 130.89, 130.82, 130.09, 128.76, 128.64, 127.36, 124.85, 124.07, 123.12, 122.50, 122.38, 121.74, 121.32, 117.54, 116.94, 116.88, 114.19, 113.94, 113.09, 109.55, 35.37, 34.90, 32.29, 31.85; 31P NMR (162 MHz, CDCl3). δ (ppm): 16.89 (s). RMS (ESI) m/z: [M + H]+ calcd for C64H61BN3PS, 946.4489; found, 946.4487.

Figure S1. Structure and HOMO energy levels of commonly used electron donors and NPO/NPS computed by DFT at the B3LYP/6-31G (d) level.

Figure S2. Cyclic voltammogram of BNCz-NPO and BNCz-NPS.

Figure S3. TGA and DSC (inset) curves of BNCz-NPO and BNCz-NPS at a heating rate of 10 °C min-1

Table S1. Crystal data and structure refinement for BNCz-NPO-α and BNCz-NPO-β

| Parameter | BNCz-NPO-α | BNCz-NPO-β |
| --- | --- | --- |
| CCDC no. | 2253324 | 2282192 |
| Empirical formula | C64H61BN3OP | C64H61BN3OP |
| Formula weight (g mol-1) | 929.93 | 929.93 |
| Temperature (K) | 150.00(10) | 150.00(10) |
| Crystal system | monoclinic | triclinic |
| Space group | P21/n | P-1 |
| a (Å) | 14.4394(2) | 12.6376(4) |
| b (Å) | 13.88700(10) | 15.0173(3) |
| c (Å) | 26.8466(3) | 16.3976(3) |
| α (°) | 90 | 79.740(2) |
| Β (°) | 102.7370(10) | 79.810(2) |
| γ (°) | 90 | 72.857(2) |
| Volume (Å3) | 5250.81(10) | 2900.44(13) |
| Z | 4 | 2 |
| Cal. density (g cm-3) | 1.176 | 1.065 |
| Absorption coefficient (mm-1) | 0.803 | 0.727 |
| F(000) | 1976.0 | 988.0 |
| Crystal size/mm3 | 0.13 × 0.12 × 0.08 | 0.15 × 0.12 × 0.1 |
| Radiation | Cu Kα (λ = 1.54184) | Cu Kα (λ = 1.54184) |
| 2Θ range for data collection (°) | 6.438 to 147.732 | 5.526 to 133.186 |
| Index ranges | -12 ≤ h ≤ 17, -15 ≤ k ≤ 17, -31 ≤ l ≤ 33 | -15 ≤ h ≤ 15, -17 ≤ k ≤ 13, -19 ≤ l ≤ 19 |
| Reflections collected | 20311 | 28045 |
| Independent reflections | 10387 [Rint = 0.0241, Rsigma = 0.0311] | 10132 [Rint = 0.0375, Rsigma = 0.0453] |
| Data/restraints/parameters | 10387/17/654 | 10132/57/688 |
| Goodness-of-fit on F2 | 1.025 | 1.104 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0393, wR2 = 0.0983 | R1 = 0.1092, wR2 = 0.3063 |
| Final R indexes [all data] | R1 = 0.0439, wR2 = 0.1020 | R1 = 0.1254, wR2 = 0.3163 |
| Largest diff. peak/hole (e Å-3) | 0.34/-0.32 | 0.86/-0.45 |

Table S2. Crystal data and structure refinement for BNCz-NPS-α and BNCz-NPS-β

| Parameter | BNCz-NPS-α | BNCz-NPS-β |
| --- | --- | --- |
| CCDC no. | 2285218 | 2247937 |
| Empirical formula | C64H61BN3PS | C64H61BN3PS |
| Formula weight (g mol-1) | 945.99 | 945.99 |
| Temperature (K) | 99.98(13) | 170.00(10) |
| Crystal system | monoclinic | monoclinic |
| Space group | P21/n | Cc |
| a (Å) | 18.88520(10) | 17.4998(9) |
| b (Å) | 25.2745(2) | 21.3090(11) |
| c (Å) | 24.1828(2) | 17.6514(10) |
| α (°) | 90 | 90 |
| Β (°) | 105.4650(10) | 97.258(5) |
| γ (°) | 90 | 90 |
| Volume (Å3) | 11124.86(15) | 6529.5(6) |
| Z | 8 | 4 |
| Cal. density (g cm-3) | 1.130 | 0.962 |
| Absorption coefficient (mm-1) | 1.093 | 0.931 |
| F(000) | 4016.0 | 2008.0 |
| Crystal size/mm3 | 0.16 × 0.13 × 0.11 | 0.15 × 0.13 × 0.11 |
| Radiation | Cu Kα (λ = 1.54184) | Cu Kα (λ = 1.54184) |
| 2Θ range for data collection (°) | 5.158 to 133.198 | 7.884 to 133.188 |
| Index ranges | -22 ≤ h ≤ 20, -30 ≤ k ≤ 18, -28 ≤ l ≤ 28 | -18 ≤ h ≤ 20, -24 ≤ k ≤ 25, -17 ≤ l ≤ 21 |
| Reflections collected | 60705 | 20416 |
| Independent reflections | 19630 [Rint = 0.0329, Rsigma = 0.0380] | 7819 [Rint = 0.0600, Rsigma = 0.0576] |
| Data/restraints/parameters | 19630/1533/1364 | 7819/761/583 |
| Goodness-of-fit on F2 | 1.091 | 1.079 |
| Final R indexes [I>=2σ (I)] | R1 = 0.1004, wR2 = 0.2430 | R1 = 0.1255, wR2 = 0.3416 |
| Final R indexes [all data] | R1 = 0.1053, wR2 = 0.2461 | R1 = 0.1472, wR2 = 0.3529 |
| Largest diff. peak/hole (e Å-3) | 0.63/-0.68 | 1.07/-1.01 |

Figure S4. Molecular geometries and packing modes of BNCz-NPO-α, BNCz-NPO-β, BNCz-NPS-α, and BNCz-NPS-β.

Figure S5. LUMO+1, LUMO, HOMO, HOMO-1 distributions and related energy levels of BNCz-NPO-α, BNCz-NPO-β, BNCz-NPS-α and BNCz-NPS-β.

Figure S6. Absorption and PL spectra of BNCz in toluene (1 × 10-5 M).

Figure S7. Absorption spectra of a) BNCz, b) BNCz-NPO and c) BNCz-NPS in different solvents (1×10-5 M).

Figure S8. PL spectra of a) BNCz, b) BNCz-NPO and c) BNCz-NPS in different solvents (1×10-5 M).

Table S3 Absorption and PL peaks of BNCz, BNCz-NPO and BNCz-NPS measured in different solvents.

|  | BNCz |  |  | BNCz-NPO |  |  | BNCz-NPS |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Solvent | λabsa (nm) | λpla (nm) | FWHMb (nm) | λabsa (nm) | λpla (nm) | FWHMb (nm) | λabsa (nm) | λpla (nm) | FWHMb (nm) |
| n-hexane | 463 | 473 | 19 | 458 | 469 | 18 | 458 | 468 | 18 |
| Butyl ether | 464 | 477 | 21 | 460 | 471 | 20 | 460 | 471 | 19 |
| Isopropyl ether | 464 | 477 | 21 | 459 | 471 | 19 | 459 | 470 | 19 |
| ethyl ether | 464 | 478 | 22 | 459 | 471 | 20 | 459 | 471 | 20 |
| Ethyl acetate | 465 | 481 | 26 | 460 | 477 | 23 | 461 | 477 | 23 |
| Tetrahydrofuran | 466 | 482 | 25 | 461 | 477 | 23 | 461 | 477 | 23 |
| Dichloromethane | 467 | 488 | 29 | 462 | 481 | 25 | 462 | 480 | 25 |
| Acetone | 466 | 487 | 28 | 460 | 480 | 26 | 461 | 479 | 26 |
| Acetonitrile | 466 | 490 | 31 | 461 | 482 | 27 | 461 | 481 | 27 |

a Peak wavelength of absorption and emission in different solvents; b Full-width at half-maximum.

Figure S9. Fluorescence (blue line) and phosphorescence (red line) spectra of a) BNCz-NPO and b) BNCz-NPS in toluene solution (1 × 10−5 M, 77 K).

Figure S10. Temperature-dependent transient PL decays of a) BNCz-NPO and b) BNCz-NPS in oxygen-free toluene solution using a variable pulsed laser (Edinburgh VPL-375).

Table S4. Photophysical data and kinetic parameters of BNCz-NPO and BNCz-NPS in doped films (3 wt% in PhCzBCz).

| Emitter | λema [nm] | FWHMb [nm/eV] | ΔESTc [eV] | PLQYd [%] | τPFe [ns] | τDFf [μs] | krg [107 s−1] | knrg [106 s−1] | kISCg [107 s−1] | kRISCg [105 s−1] |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BNCz-NPO | 478 | 26/0.14 | 0.10 | 95.5 | 2.8 | 28.5 | 7.1 | 3.7 | 28.2 | 1.6 |
| BNCz-NPS | 481 | 26/0.14 | 0.10 | 92.0 | 3.0 | 21.9 | 5.0 | 4.9 | 27.8 | 2.7 |

a)Peak of fluorescence spectrum. b)Full width at half-maximum (FWHM) of fluorescence spectrum. c)S1−T1 energy gap determined from fluorescence and phosphorescence spectra at 77 K. d)Absolute photoluminescence quantum yield. e)Lifetime of prompt fluorescence. f)Lifetime of delayed fluorescence. g)Rate constants of singlet radiative decay (kr), non-radiative decay (knr), intersystem crossing (kISC), and reverse intersystem crossing (kRISC).

Figure S11. PL spectra of a) BNCz-NPO and b) BNCz-NPS doped films (3 wt% in PhCzBCz) at 300 K. Transient PL decay curves of c) BNCz-NPO and d) BNCz-NPS doped films (3 wt% in PhCzBCz) at 300 K using a variable pulsed laser (Edinburgh VPL-375) and a picosecond pulsed diode laser (Edinburgh EPL-375, inset)

Figure S12. The RMSD values of BNCz, BNCz-NPO, and BNCz-NPS between the optimized S0 (red) and S1 (blue) geometries.

Figure S13. Emission spectra simulated by Franck–Condon analysis of S1–S0 transition, the vertical lines are the vibrational transition dipoles with strength > 0.001.

Figure S14. Transition frequencies, S, and reorganization energies of the vibrational modes contribute to the S1-S0 transition of the parent molecule BNCz, BNCz-NPO, and BNCz-NPS in the region of frequency > 1000 cm-1.

Table S5. Summary of Franck-Condon analysis on the S1–S0 transition of BNCz, BNCz-NPO, and BNCz-NPS at the (TD) B3LYP/6-31G(d) level.

| Compd. | Transition (S1→S0) | Frequency (cm-1) | Relative frequency (cm-1) | Line density | Dipole strength (arb. units) |
| --- | --- | --- | --- | --- | --- |
| BNCz | 0→0 | 21649.5367 | 0 | 666.1 | 0.5347 |
|  | 0→21 | 21632.2176 | -17.3191 | 193.6 | 0.1562 |
|  | 0→31 | 21617.3416 | -32.1951 | 114.5 | 0.09271 |
|  | 0→71 | 21609.3069 | -40.2298 | 84.81 | 0.06875 |
|  | 0→91 | 21591.5786 | -57.9581 | 544.0 | 0.4420 |
|  | 0→91,21 | 21574.2594 | -75.2773 | 152.5 | 0.1242 |
|  | 0→91,31 | 21559,3835 | -90.1532 | 93.15 | 0.07614 |
|  | 0→91,71 | 21551.3487 | -98.1880 | 75.69 | 0.06196 |
|  | 0→92 | 21533.6204 | -115.9163 | 224.4 | 0.1841 |
| BNCz-NPO | 0→0 | 21901.2363 | 0 | 717.2 | 0.5498 |
|  | 0→31 | 21889.7477 | -11.4886 | 395.9 | 0.3044 |
|  | 0→32 | 21878.2591 | -22.9772 | 114.2 | 0.08792 |
|  | 0→111 | 21862.5103 | -38.7260 | 112.7 | 0.08697 |
|  | 0→141 | 21844.5658 | -56.6705 | 126.2 | 0.09795 |
|  | 0→151 | 21842.9812 | -58.2551 | 101.9 | 0.07905 |
| BNCz-NPS | 0→0 | 21860.4119 | 0 | 426.5 | 0.3293 |
|  | 0→11 | 21857.0276 | -3.3843 | 408.5 | 0.3159 |
|  | 0→12 | 21853.6433 | -6.7686 | 101.3 | 0.07834 |
|  | 0→31 | 21849.7412 | -10.6707 | 97.82 | 0.07577 |
|  | 0→31,11 | 21846.3569 | -14.0550 | 76.24 | 0.05903 |
|  | 0→141 | 21804.5658 | -55.8461 | 93.18 | 0.07270 |
|  | 0→151 | 21802.4181 | -57.9938 | 76.94 | 0.06013 |
|  | 0→141,11 | 21801.1815 | -59.2304 | 93.55 | 0.07310 |
|  | 0→151,11 | 21799.0338 | -61.3781 | 74.94 | 0.05854 |

Figure S15. Absorption spectra of BNCz-NPO and BNCz-NPS, and PL spectrum of 5TCzBN in toluene solution (1 × 10−5 M, 298 K).

Figure S16. a) Current density-voltage-luminance characteristics, b) EL spectra of HF-I type OLEDs measured at 4 V.

Figure S17. a) Device structure of HF-II type OLEDs and the chemical structure of PPCz-Trz; b) Current density-voltage-luminance characteristics of HF-II type OLEDs; c) EL spectra measured at 4 V.

Table S6. EL performance of the reported high-performance blue MR-TADF emitters. The plotted data for Figure 7 in main text are highlighted with color.

| Dopant type | Emitter | λEL [nm] | FWHM [nm] | EQEmax [%] | EQE100 [%] | EQE1000 [%] | CIE (x, y) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Monoboron | BNCz-NPO | 480 | 26 | 32.1 | 21.7 | 9.7 | (0.11, 0.22) | This work |
|  | BNCz -NPS | 476 | 26 | 29.6 | 23.5 | 13.5 | (0.11, 0.16) | This work |
|  | BNCz-NPO (HF-I) | 476 | 26 | 30.2 | 28.0 | 20.7 | (0.12, 0.22) | This work |
|  | BNCz-NPO (HF-II) | 480 | 26 | 37.6 | 30.2 | 12.0 | (0.11, 0.18) | This work |
|  | BNCz-NPS (HF-I) | 480 | 30 | 31.9 | 31.6 | 26.4 | (0.14, 0.24) | This work |
|  | BNCz-NPs (HF-II ) | 476 | 30 | 32.2 | 29.2 | 17.3 | (0.13, 0.18) | This work |
|  | TBA-BCz-BN (HF) | 470 | 28 | 30.8 | 19.0 | 11.7 | (0.12, 0.15) | 5 |
|  | DCzBNO (HF) | 469 | 45 | 31.7 | - | - | (0.13, 0.15) | 6 |
|  | TCzBNO(HF) | 482 | 52 | 36.5 | - | - | (0.13, 0.25) |  |
|  | γ-Cb-B | 461 | 28 | 19.0 | 16.2 | 7.7 | (0.13, 0.13) | 7 |
|  | Cz-B | 482 | 30 | 22.6 | 16.6 | 6.9 | (0.11, 0.31) |  |
|  | Tip-DtCzB (HF) | 484 | 25 | 29.0 | 23.2 | 11.0 | (0.10, 0.29) | 8 |
|  | tDPA-DtCzB (HF) | 480 | 27 | 30.2 | 27.5 | 18.0 | (0.11, 0.24) |  |
|  | BNO-DPAC (HF) | 448 | 36 | 27.7 | - | 14.5 | (0.151, 0.083) | 9 |
|  | BNO-DMAC (HF) | 449 | 36 | 28.7 | - | 18.2 | (0.149, 0.090) |  |
|  | BNO-tBuDMAC | 447 | 59 | 27.7 | - | 18.8 | (0.155, 0.144) |  |
|  | t-DAB-DPA | 459 | 26 | 27.9 | 21.8 | 8.1 | (0.13, 0.08) | 10 |
|  | t-DABNA | 464 | 26 | 28.4 | 14.8 | 4.4 | (0.13, 0.10) |  |
|  | PAB | 456 | 31 | 14.7 | - | - | (0.145, 0.076) | 11 |
|  | 2tPAB | 456 | 27 | 16.8 | - | - | (0.145, 0.076) |  |
|  | 3tPAB | 460 | 26 | 19.3 | - | - | (0.141, 0.076) |  |
|  | tDPAC-BN (HF) | 460 | 28 | 21.6 | 15.3 | 5.4 | (0.135, 0.094) | 12 |
|  | tDMAC-BN (HF) | 472 | 34 | 22.3 | 19.0 | 10.4 | (0.116, 0.186) |  |
|  | DPACzBN1 | 475 | 34 | 23.6 | 19.3 | 9.6 | (0.14, 0.30) | 13 |
|  | DPACzBN2 | 469 | 28 | 24.0 | 23.5 | 14.3 | (0.13, 0.16) |  |
|  | DPACzBN3 | 472 | 24 | 27.7 | 19.3 | 6.7 | (0.12, 0.18) |  |
|  | B-dpa-Cz | 475 | 27 | 20.1 | 15.3 | 4.7 | (0.11, 0.19) | 14 |
|  | B-dpa-dmAc | 478 | 32 | 24.3 | 23.3 | 14.9 | (0.11, 0.22) |  |
|  | B-dpa-SpiroAc | 478 | 32 | 24.3 | 23.6 | 15.6 | (0.11, 0.22) |  |
|  | B-O-dpa | 443 | 32 | 16.3 | 6.5 | 2.2 | (0.15, 0.05) | 15 |
|  | B-O-Cz | 481 | 63 | 13.4 | 9.5 | 5.9 | (0.13, 0.22) |  |
|  | B-O-dmAc | 475 | 44 | 16.2 | 13.5 | 8.4 | (0.12, 0.21) |  |
|  | B-O-dpAc | 473 | 42 | 17.0 | 14.3 | 9.6 | (0.12, 0.20) |  |
|  | mono-mx-CzDABNA (HF) | 481 | 48 | 21.4 | 14.0 | 7.8 | (0.13, 0.24) | 16 |
|  | tri-mx-CzDABNA (HF) | 472 | 34 | 26.9 | 26.1 | 24.8 | (0.13, 0.19) |  |
|  | DABNA-2 | 467 | 28 | 20.2 | - | - | (0.12, 0.13) | 17 |
|  | DABNA-1 | 459 | 28 | 13.5 | - | - | (0.13, 0.09) |  |
|  | DABNA-NP-TB | 457 | 33 | 19.5 | 17.5 | 12 | (0.14, 0.11) | 18 |
|  | Cz2DABNA-NP-M/TB | 477 | 27 | 21.8 | 20.4 | 14.9 | (0.11, 0.23) |  |
|  | mBP -DABNA-Me | 468 | 28 | 24.3 | 19.5 | 16.0 | (0.12, 0.14) | 19 |
|  | tCBN-DADPO | 472 | 28 | 30.8 | 23.3 | 16.2 | (0.14, 0.22) | 20 |
|  | CzBO | 448 | 30 | 16.3 | 10.7 | 4.7 | (0.15, 0.05) | 21 |
|  | CzBS | 474 | 31 | 29.1 | 27.4 | 20.0 | (0.11, 0.16) |  |
|  | CzBSe | 481 | 33 | 30.1 | 29.7 | 26.1 | (0.10, 0.24) |  |
|  | DCz-BSN | 473 | 29 | 22.0 | 18.6 | 10.0 | (0.11, 0.17) | 22 |
|  | Cz-BSN | 482 | 32 | 18.9 | 13.4 | 6.8 | (0.11, 0.28) |  |
|  | PTZBN3 (HF) | 468 | 46 | 32.0 | 30.3 | 25.0 | (0.15, 0.24) | 23 |
|  | PTZBN2 (HF) | 478 | 48 | 34.8 | 28.8 | 19.5 | (0.15, 0.29 |  |
|  | PTZBN1 (HF) | 489 | 47 | 32.7 | 25.9 | 16.5 | (0.14, 0.41 |  |
|  | TBN-TPA | 474 | 27 | 32.1 | 27.4 | 13.9 | (0.12, 0.19) | 24 |
|  | TCz-BN | 474 | 34 | 18.88 | 15.19 | 10.52 | (0.13, 0.20) | 25 |
|  | ADBNA -Me-Mes | 481 | 32 | 16.2 | 11.1 |  | (0.10, 0.27) | 26 |
|  | ADBNA -Me-Tip | 480 | 33 | 21.4 | 15.4 |  | (0.11, 0.29) |  |
|  | BN-TC | 474 | 37 | 21.2 | 8.7 | 4.2 | (0.13, 0.20) | 27 |
|  | BN-AC | 484 | 27 | 23.4 | 15.9 | 5.5 | (0.10, 0.31) |  |
|  | Tp-DABNA (HF) | 462 | 29 | 27.5 | 18.6 |  | (0.14, 0.13) | 28 |
|  | t-DABNA (HF) | 464 | 34 | 23.3 | 14.7 |  | (0.13, 0.14) |  |
|  | p-TBNCz | 488 | 26 | 27.0 | 11.7 | 5.8 | (0.09, 0.35) | 29 |
|  | OBN | 437 | 44 | 15.7 |  |  | 0.15, 0.09) | 30 |
|  | NBN | 452 | 40 | 23.02 |  |  | (0.14, 0.09) |  |
|  | BIC-pCz (HF) | 466 | 48 | 39.8 |  |  | (0.14, 0.16) | 31 |
|  | BN1 (HF) | 457 | 28 | 31.2 | 18.3 | 9.3 | (0.14, 0.06) | 32 |
|  | BN2 (HF) | 467 | 23 | 33.2 | 25.5 | 15.5 | (0.13, 0.11) |  |
| Polyboron | ODBN | 446 | 54 | 24.15 |  |  | (0.15, 0.10) | 30 |
|  | BIC-mCz (HF) | 432 | 42 | 19.4 |  |  | (0.16, 0.05) | 31 |
|  | mDBIC (HF) | 431 | 42 | 13.5 |  |  | (0.16, 0.05) |  |
|  | BN3 (HF) | 458 | 23 | 37.6 | 34.0 | 26.2 | (0.14, 0.08) | 32 |
|  | V-DABNA -Mes | 480 | 27 | 22.9 | 20.3 | 10.9 | (0.09, 0.21) | 33 |
|  | m[B-N]N1 (HF) | 479 | 27 | 36.0 |  | 32.3 | (0.12, 0.27) | 34 |
|  | m[B-N]N2 (HF) | 485 | 33 | 33.4 |  | 29.7 | (0.14, 0.46) |  |
|  | α-3BNMes (HF) | 443 | 49 | 14.6 | 10.2 |  | (0.15, 0.10) | 35 |
|  | B2 | 460 | 37 | 18.3 | 12.6 |  | (0.13, 0.11) | 36 |
|  | v-DABNA | 469 | 18 | 34.4 | 32.8 | 26.0 | (0.14, 0.11) | 37 |
|  | v-DABNA-OMe | 465 | 23 | 29.5 | 28.8 | 26.9 | (0.13, 0.10) | 38 |
|  | m-ν-DABNA | 471 | 18 | 36.2 |  |  | (0.12, 0.12) | 39 |
|  | 4F-ν-DABNA | 464 | 18 | 35.8 |  |  | (0.13, 0.08) |  |
|  | 4F-mν-DABNA | 461 | 18 | 33.7 |  |  | (0.13, 0.06) |  |
|  | BOBO-Z | 445 | 18 | 16.6 | 12.4 | 5.3 | (0.15, 0.04) | 40 |
|  | BOBS-Z | 455 | 23 | 33.1 | 30.2 | 20.2 | (0.14, 0.06) |  |
|  | BSBS-Z | 463 | 23 | 32.2 | 30.2 | 20.2 | (0.13, 0.08) |  |
|  | m-DiNBO | 466 | 21 | 24.2 | 17.3 |  | (0.13, 0.10) | 41 |
|  | BSBS-N1 | 478 | 21 | 25 |  |  | (0.11, 0.22) | 42 |
|  | NO-DBMR | 469 | 26 | 33.7 |  |  | (0.12,0.12) | 43 |
|  | Cz-DBMR | 491 | 22 | 29.8 |  |  | (0.09,0.34) |  |
|  | BBCz-DB | 469 | 27 | 29.3 |  |  | (0.12, 0.18) | 44 |

Figure S18. 1H NMR spectrum of 1 in CDCl3 (400 MHz, 25 °C).

Figure S19. 1H NMR spectrum of 2 in CDCl3 (400 MHz, 25 °C).

Figure S20. 1H NMR spectrum of 3a in CDCl3 (400 MHz, 25 °C).

Figure S21. 31P NMR spectrum of 3a in CDCl3 (400 MHz, 25 °C).

Figure S22. 1H NMR spectrum of 3b in DMSOd6 (400 MHz, 25 °C).

Figure S23. 31P NMR spectrum of 3b in DMSOd6 (400 MHz, 25 °C).

Figure S24. 1H NMR spectrum of NPO in DMSOd6 (400 MHz, 25 °C).

Figure S25. 31P NMR spectrum of NPO in DMSOd6 (400 MHz, 25 °C).

Figure S26. 1H NMR spectrum of NPS in DMSOd6 (400 MHz, 25 °C).

Figure S27. 31P NMR spectrum of NPS in DMSOd6 (400 MHz, 25 °C).

Figure S28. 1H NMR spectrum of BNCz-NPO in CDCl3 (400 MHz, 25 °C).

Figure S29. 13C NMR spectrum of BNCz-NPO in CDCl3 (400 MHz, 25 °C).

Figure S30. 31P NMR spectrum of BNCz-NPO in CDCl3 at 25 °C.

Figure S31. 1H NMR spectrum of BNCz-NPS in CDCl3 (400 MHz, 25 °C).

Figure S32. 13C NMR spectrum of BNCz-NPS in CDCl3 (400 MHz, 25 °C).

Figure S33. 31P NMR spectrum of BNCz-NPS in CDCl3 at 25 °C.

Figure S34. HRMS spectrum of BNCz-NPO.

Figure S35. HRMS spectrum of BNCz-NPS.

References

[1] Gaussian 16, Revision A.03,  M. J. Frisch, G. W. Trucks, H. B. Schlegel, G. E. Scuseria,  M. A. Robb, J. R. Cheeseman, G. Scalmani, V. Barone, G. A. Petersson, H. Nakatsuji, X. Li, M. Caricato, A. V. Marenich,  J. Bloino, B. G. Janesko, R. Gomperts, B. Mennucci, H. P. Hratchian,  J. V. Ortiz, A. F. Izmaylov, J. L. Sonnenberg, D. Williams-Young,  F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone,  T. Henderson, D. Ranasinghe, V. G. Zakrzewski, J. Gao, N. Rega, G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, T. Vreven, K. Throssell, J. A. Montgomery, Jr., J. E. Peralta, F. Ogliaro, M. J. Bearpark, J. J. Heyd, E. N. Brothers, K. N. Kudin, V. N. Staroverov, T. A. Keith, R. Kobayashi, J. Normand, K. Raghavachari, A. P. Rendell, J. C. Burant, S. S. Iyengar, J. Tomasi, M. Cossi, J. M. Millam, M. Klene, C. Adamo, R. Cammi, J. W. Ochterski, R. L. Martin, K. Morokuma, O. Farkas, J. B. Foresman, and D. J. Fox, Gaussian, Inc., Wallingford CT, 2016.

[2] W. Humphrey, A. Dalke, K. Schulten, J. Mol. Graphics 1996, 14, 33.

[3] T. Lu, F. Chen, J. Comput. Chem. 2012, 33, 580

[4] K. Masui, H. Nakanotani, C. Adachi, Org. Electron. 2013, 14, 2721.

[5] X. Xiao, B. Lei, D. Wu, Z. Bin. Chem. Commun., 2023, 59, 6556.

[6] Y. Xu, J. Han, N. Li, Z. Huang, J. Miao and C. Yang, J. Mater. Chem. C, 2023, DOI: 10.1039/D3TC02574H.

[7] M. Yang, S. Shikita, H. Min, I. S. Park, H. Shibata, N. Amanokura, T. Yasuda, Angew. Chem. Int. Ed. 2021, 60, 23142.

[8] X. Yan, Z. Li, Q. Wang, Y. Qu, Y. Xu, Y. Wang, J. Mater. Chem. C, 2022, 10, 15408

[9] X. Huang, Y. Xu, J. Miao, Y. Jing, S. Wang, Z. Ye, Z. Huang, X. Cao and C. Yang, J. Mater. Chem. C, 2023, 11, 11885.

[10] J. H. Kim, W. J. Chung, J. Kim, J. Y. Lee, Mater. Today Energy 2021, 21, 100792.

[11] Y. Wang, Y. Duan, R. Guo, S. Ye, K. Di, W. Zhang, S. Zhuang, L. Wang, Org. Electron.  2021, 97, 106275.

[12] Y. Wang, K. Di, Y. Duan, R. Guo, L. Lian, W. Zhang, L. Wang, Chem. Eng. J. 2022, 431, 133221.

[13] Y. Qiu, H. Xia, J. Miao, Z. Huang, N. Li, X. Cao, J. Han, C. Zhou, C. Zhong, C. Yang, ACS ACS Appl. Mater. Interfaces 2021, 13, 59035.

[14] J. Park, J. Moon, J. Lim, J. Woo, S. S. Yoon, J. Y. Lee, J. Mater. Chem. C, 2022, 10, 12300.

[15] J. Park, J. Lim, J. H. Lee, B. Jang, J. H. Han, S. S. Yoon, J. Y. Lee, ACS Appl. Mater. Interfaces 2021, 13, 45798.

[16] E. Ravindran, H. E. Baek, H. W. Son, J. H. Park, Y. H. Kim, M. C. Suh, Adv. Funct. Mater. 2023, 33, 2213461.

[17] T. Hatakeyama, K. Shiren, K. Nakajima, S. Nomura, S. Nakatsuka, K. Kinoshita, J. Ni, Y. Ono, T. Ikuta, Adv. Mater. 2016, 28, 2777.

[18] S. Oda, W. Kumano, T. Hama, R. Kawasumi, K. Yoshiura, T. Hatakeyama, Angew. Chem. Int. Ed. 2020, 60, 2882.

[19] H. J. Cheon, Y. S. Shin, N. H. Park, J. H. Lee, Y. H. Kim, Small 2022, 18, 2107574.

[20] J. Bian, S. Chen, L. Qiu, R. Tian, Y. Man, Y. Wang, S. Chen, J. Zhang, C. Duan, C. Han, H. Xu, Adv. Mater. 2022, 34,2110547.

[21] I. S. Park, H. Min, T. Yasuda, Angew. Chem. Int. Ed. 2022, 61, e202205684.

[22] Q. Li, Y. Wu, X. Wang, Q. Yang, J. Hu, R. Zhong, S. Shao, L. Wang, Chem. Eur. J. 2022, 28, e202104214.

[23] T. Hua, J. Miao, H. Xia, Z. Huang, X. Cao, N. Li, C. Yang, Adv. Funct. Mater. 2022, 32, 2201032.

[24] X. Liang, Z. P. Yan, H. B. Han, Z. G. Wu, Y. X. Zheng, H. Meng, J. L. Zuo, W. Huang, Angew. Chem. Int. Ed. 2018, 57, 11316.

[25] Y. Zhang, D. Zhang, J. Wei, Z. Liu, Y. Lu, L. Duan, Angew. Chem. Int. Ed. 2019, 58, 16912.

[26] S. Oda, B. Kawakami, R. Kawasumi, R. Okita, T. Hatakeyama, Organic Letters 2019, 21, 9311.

[27] Y.-H. He, F.-M. Xie, H.-Z. Li, K. Zhang, Y. Shen, F. Ding, C.-Y. Wang, Y.-Q. Li, J.-X. Tang, Mater. Chem. Front.2023, 7, 2454.

[28] H. Mubarok, A. Amin, T. Lee, J. Jung, J. H. Lee, M. H. Lee, Angew. Chem. Int. Ed. 2023, 62, e202306879.

[29] X. Cai, Y. Pu, C. Li, Z. Wang, Y. Wang, Angew. Chem. Int. Ed. 2023, 62, e202304104.

[30] J. Jin, C. Duan, H. Jiang, P. Tao, H. Xu, W. Y. Wong, Angew. Chem. Int. Ed. 2023, 62, e202218947.

[31] X. Wang, Y. Zhang, H. Dai, G. Li, M. Liu, G. Meng, X. Zeng, T. Huang, L. Wang, Q. Peng, D. Yang, D. Ma, D. Zhang, L. Duan, Angew. Chem. Int. Ed. 2022, 61, e202206916.

[32] X. Lv, J. Miao, M. Liu, Q. Peng, C. Zhong, Y. Hu, X. Cao, H. Wu, Y. Yang, C. Zhou, J. Ma, Y. Zou, C. Yang, Angew. Chem. Int. Ed. 2022, 61, e202201588.

[33] S. Oda, B. Kawakami, Y. Yamasaki, R. Matsumoto, M. Yoshioka, D. Fukushima, S. Nakatsuka, T. Hatakeyama, J. Am. Chem. Soc. 2021, 144, 106.

[34] G. Meng, H. Dai, T. Huang, J. Wei, J. Zhou, X. Li, X. Wang, X. Hong, C. Yin, X. Zeng, Y. Zhang, D. Yang, D. Ma, G. Li, D. Zhang, L. Duan, Angew. Chem. Int. Ed. 2022, 61, e202207293.

[35] K. Stavrou, S. Madayanad Suresh, D. Hall, A. Danos, N. A. Kukhta, A. M. Z. Slawin, S. Warriner, D. Beljonne, Y. Olivier, A. Monkman, E. Zysman‐Colman, Adv. Opt. Mater. 2022, 10. 2200688

[36] K. Matsui, S. Oda, K. Yoshiura, K. Nakajima, N. Yasuda, T. Hatakeyama, J. Am. Chem. Soc. 2017, 140, 1195.

[37] Y. Kondo, K. Yoshiura, S. Kitera, H. Nishi, S. Oda, H. Gotoh, Y. Sasada, M. Yanai, T. Hatakeyama, Nat. Photonics 2019, 13, 678.

[38] H. Tanaka, S. Oda, G. Ricci, H. Gotoh, K. Tabata, R. Kawasumi, D. Beljonne, Y. Olivier, T. Hatakeyama, Angew. Chem. Int. Ed. 2021, 60, 17910.

[39]K. Rayappa Naveen, H. Lee, R. Braveenth, K. Joon Yang, S. Jae Hwang, J. Hyuk Kwon, Chem. Eng. J. 2022, 432, 134381.

[40] I. S. Park, M. Yang, H. Shibata, N. Amanokura, T. Yasuda, Adv. Mater. 2022, 34. 2107951

[41] G. Liu, H. Sasabe, K. Kumada, H. Arai, J. Kido, Chem. Eur. J. 2022, 28, e202201605.

[42] M. Nagata, H. Min, E. Watanabe, H. Fukumoto, Y. Mizuhata, N. Tokitoh, T. Agou, T. Yasuda, Angew. Chem. Int. Ed. 2021, 60, 20280.

[43] K. R. Naveen, J. H. Oh, H. S. Lee, J. H. Kwon, Angew. Chem. Int. Ed. 2023, 62. e202306768.

[44] M. Yang, I. S. Park, T. Yasuda, J. Am. Chem. Soc. 2020, 142, 19468.