Supplementary Information

Alloy-Tunable Single-Layer 2D Heterophase Photocatalysts for Efficient Solar Fuel Production

Jiayi Chen†1, Md Nasir Uddin†2, Xiaozhi Liu†3, Rundong Mao1, Kaili Liu2, Hsien-Yi Hsu4, Dong Su*3, Yunguo Li*5, Ido Hadar6, Mark A. Buntine1, Xuyong Yang7, Zongyou Yin*2, and Guohua Jia*1

1 School of Molecular and Life Sciences, Curtin University, Bentley, WA 6102, Australia

2 Research School of Chemistry, Australian National University, Canberra, ACT 2600, Australia

3 Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, China

4 School of Energy and Environment & Department of Materials Science and Engineering, City University of Hong Kong, Kowloon Tong, Hong Kong, China, and Shenzhen Research Institute of City University of Hong Kong, Shenzhen, 518057, China

5 CAS Key Laboratory of Crust−Mantle Materials and Environments, School of Earth and Space Sciences, University of Science and Technology of China, Hefei, Anhui 230026, China

6 Institute of Chemistry, and the Center for Nanoscience and Nanotechnology, The Hebrew University of Jerusalem, Jerusalem 91904, Israel

7 Key Laboratory of Advanced Display and System Applications of Ministry of Education, Shanghai University, Shanghai 200072, P. R. China

† These authors contribute equally to this work.

Corresponding authors E-mail: guohua.jia@curtin.edu.au; zongyou.yin@anu.edu.au; dongsu@iphy.ac.cn; liyunguo@ustc.edu.cn

Supplementary Fig. 1 BF-TEM and STEM-HAADF images of (a-b) MoS2 and (c-d) WS2, respectively. All scale bars are 20 nm.

Supplementary Fig. 2 Thickness histogram of alloyed singly-layer MoxW1-xS2 and MoSySe2-y nanosheets.

Supplementary Fig. 3 TEM images of single-layer MoxW1-xS2 and MoSySe2-y nanosheets. The scale bars are 20 nm.

Supplementary Fig. 4 (a-d) HAADF-STEM images of Mo0.44W0.56S2, Mo0.08W0.92S2, MoS0.91Se1.09 and MoS0.22Se1.78 nanosheets and the corresponding STEM-EDS elemental mappings of Mo, W, S and Se. All scale bars are100 nm.

Supplementary Fig. 5 (a) XRD patterns of synthesised single-layer MoxW1-xS2 nanosheets, the orange lines on the bottom are patterns of 1T phase MoS2 (ICSD: 254956), the grey lines on the bottom and the top are patterns of 2H phase MoS2 (PDF#37-1492) and 2H phase WS2 (PDF#08-0237), respectively. (b) XRD patterns of synthesised single-layer MoSxSe2-x nanosheets, the orange lines on the bottom are patterns of 1T phase MoS2 (ICSD: 254956), the grey lines are patterns of 2H phase MoS2 (PDF#37-1492) and 2H phase MoSe2 (PDF#29-0914), respectively.

Supplementary Table 1

| Calculated molecular formula of MoxW1-xS2 with different molar ratio of added reactant. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Molar ratio of added reactant | Molybdenum | Tungsten | Sulfur | Calculated formula |
| Mo:W = 1:1 | 17.98% | 18.52% | 63.50% | Mo0.44W0.56S2 |
| Mo:W = 1:3 | 8.29% | 26.37% | 65.34% | Mo0.21W0.79S2 |
| Mo:W = 1:5 | 23.93% | 30.54% | 45.53% | Mo0.08W0.92S2 |

Calculation of element ratio in MoxW1-xS2 nanosheets:

2(Mo% + W%) = S%

Mo% + W% + S% = 1,

Therefore,

S% = 66.67%

Mo% = 33.33% - W%.

Supplementary Table 2

| Calculated molecular formula of MoSxSe2-x with different molar ratio of added reactant. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Molar ratio of added reactant | Molybdenum | Tungsten | Sulfur | Calculated formula |
| S:Se = 1:3 | 42.42% | 21.37% | 36.21% | MoS0.91Se1.09 |
| S:Se = 1:4 | 27.61% | 23.71% | 48.68% | MoS0.54Se1.46 |
| S:Se = 1:5 | 31.28% | 9.37% | 59.35% | MoS0.22Se1.78 |

Calculation of element ratio in MoSySe2-y nanosheets:

2Mo% = S% + Se%

Mo% + S% + Se% = 1,

Therefore,

Mo% = 33.33%,

S% = 66.67% - Se%.

Supplementary Fig. 6 The XPS survey spectrum of single-layer MoS2 nanosheets.

Supplementary Fig. 7 The XPS survey spectrum of single-layer WS2 nanosheets.

Supplementary Fig. 8 The XPS survey spectrum of single-layer Mo0.44W0.56S2 nanosheets.

Supplementary Fig. 9 The XPS survey spectrum of single-layer Mo0.21W0.79S2 nanosheets.

Supplementary Fig. 10 The XPS survey spectrum of single-layer Mo0.08W0.92S2 nanosheets.

Supplementary Fig. 11 The XPS survey spectrum of single-layer MoS0.91Se1.09 nanosheets.

Supplementary Fig. 12 The XPS survey spectrum of single-layer MoS1.59Se0.41 nanosheets.

Supplementary Fig. 13 The XPS survey spectrum of single-layer MoS0.22Se1.78 nanosheets.

Supplementary Fig. 14 XPS spectra of Mo 3d of (a) Mo0.44W0.56S2, (b) Mo0.08W0.92S2, (c) MoS0.91Se1.09 and (d) MoS0.22Se1.78 nanosheets, the blue and pink areas indicate 1T’ and 2H phase, respectively.

Supplementary Fig. 15 Raman spectra of (a) MoS0.91Se1.09, (b) MoS0.22Se1.78, (c) Mo0.44W0.56S2 and (d) Mo0.08W0.92S2 nanosheets, respectively.

Supplementary Table 3

| Stability calculation of 1T and 1T’ phase in MoxW1-xS2 or MoSxSe2-x nanosheets with different content of W or Se element. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | XW/Se (%) | 0 | 25 | 5 | 75 | 100 |
| W | E1T (eV) | -20.954 | -21.434 | -21.905 | -22.369 | -22.822 |
|  | E1T’ (eV) | -21.248 | -21.736 | -22.225 | -22.707 | -23.183 |
|  | E1T - E1T’ (eV) | -0.294 | -0.303 | -0.321 | -0.338 | -0.362 |
| Se | E1T (eV) | -20.954 | -20.540 | -20.121 | -19.695 | -19.264 |
|  | E1T’ (eV) | -21.248 | -20.836 | -20.531 | -20.056 | -19.641 |
|  | E1T - E1T’ (eV) | -0.294 | -0.295 | -0.409 | -0.360 | -0.377 |

Supplementary Fig. 16 UV-vis spectra of singly-layer MoS2, WS2, Mo0.21W0.79S2 and Mo0.08S0.91Se1.09 nanosheets.

Supplementary Fig. 17 (a) A STEM image of Mo0.21W0.79S2 nanosheet, (b-d) EELS spectra of Mo-L edges, Mo-M edges, W-M edges and S-L edges. The spectra were acquired in the green area in (a).

Supplementary Fig. 18 Proton-NMR measurement for hydrogen production from methanol. (a) Pure methanol as the control before light illumination, (b) Zoom in section of pure methanol, (c) Reacted pure methanol after light illumination and (d) Zoom in section of the reacted methanol. Experimental conditions: 3 mL pure and reacted methanol diluted with 4 mL CD3OD during the measurement with Bruker 400 MHz instrument.

Supplementary Table 4

| Bandgap calculation of 2H and 1T’ phase in Mo0.21W0.79S2 nanosheets. |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Efermi | Evaccum | EVBM | ECBM | Bandgap |
| 2H - Mo0.21W0.79S2 | -1.127 | 4.526 | -5.653 | -3.806 | 1.847 |
| 1T’ - Mo0.21W0.79S2 | -2.307 | 3.347 | -5.655 | -5.625 | 0.030 |

Supplementary Fig. 19 Free energies ΔG (in eV) for elementary reaction processes of hydrogen evolution from methanol catalyzed on Mo-edge-b, Mo-edge-m, Mo-edge-m+d, S-edge-m+d, and S-edge-m edges, respectively. Numbers inside box are ΔG and the number in bold text indicates the lowest one. We stopped exploring further reactions if the lowest ΔG is bigger than 0.5 eV.