Table AS Hydrogen-bond geometry (Å, º) for2-HDETDHP.

| D—H···A | D—H | H···A | D···A | D—H···A |
| --- | --- | --- | --- | --- |
| O3—H3O···O5i | 0.80 (4) | 1.79 (4) | 2.586 (3) | 178 (3) |
| O4—H4O···O2i | 0.93 (4) | 1.60 (4) | 2.526 (2) | 173 (3) |
| O5—H5O···O1ii | 0.93 (4) | 1.63 (4) | 2.556 (3) | 176 (4) |
| C3—H3B···O1 | 0.98 | 2.48 | 3.439 (3) | 166 |
| C4—H4B···O3iii | 0.98 | 2.54 | 3.504 (3) | 170 |
| C4—H4C···O1iv | 0.98 | 2.49 | 3.457 (3) | 168 |
| C5—H5A···O3iv | 0.98 | 2.46 | 3.430 (3) | 172 |
| C5—H5B···O1iii | 0.98 | 2.42 | 3.382 (3) | 169 |
| C5—H5C···O2 | 0.98 | 2.60 | 3.549 (3) | 164 |

Symmetry codes : (i) -x+2, -y+1, -z ; (ii) -x+1, -y+1, -z ; (iii) -x+1, -y+1, -z+1 ; (iv) x, y-1, z.

Table 1S The crystal data and structure refinement for 2-HDETDHP.

| Crystal data |  |
| --- | --- |
| Chemical formula | C5H14NO+·H2PO4- |
| Mr | 201.16 |
| Crystal system, space group | Triclinic, P1 |
| Temperature (K) | 193 |
| a, b, c (Å) | 6.9232 (3), 8.2807 (4), 9.2333 (3) |
| a, b, g (°) | 84.458 (3), 71.414 (3), 70.758 (3) |
| V (Å3) | 473.68 (4) |
| Z | 2 |
| Radiation type | Cu Ka |
| m (mm-1) | 2.55 |
| Crystal size (mm) | 0.60 × 0.10 × 0.02 |

Figure 1S Molecular structure plot displaying atom labeling. At 50% likelihood, displacement ellipsoids are drawn.

Optimized Geometry

The electronic and geometric properties were calculated DFT at B3LYP and HF methods by 6-311G bases set. The compound has C1 point group symmetry and exists asreal minima on the potential energy surface and the energy of RMS 0.00000766 a.u.

Table 2S Selected structural characteristics of the 2-HDETDHP compound determined both empirically and theoretically through free molecule optimization.

| Parameters | Experimental | DFT/B3LYP/6-311G | HF/6-311G |
| --- | --- | --- | --- |
| P1-O2 P1-O3 P1-O4 P1-O5 O2-H11 O2-H18 O3-H11 O3-H27 O4-H6 O5-H7 O8-C13 O8-H28 N9-C10 N9-C16 N9-C20 N9-C24 C10-H11 C10-H12 C10-C13 C13-H14 C13-H15 C16-H17 C16-H18 C16-H19 C20-H21 C20-H22 C20-H23 C24-H25 C24-H26 C24-H27 | 1.5028 1.5167 1.6724 1.6668 3.1446 1.7328 1.8256 1.8578 0.9812 0.9824 1.4334 0.9782 1.5236 1.5065 1.5165 1.5091 1.1577 1.1096 1.5264 1.1143 1.1030 1.0966 1.1592 1.0964 1.1053 1.1030 1.1043 1.0955 1.0988 1.1451 | 1.4967 1.5080 1.5772 1.5630 3.1675 2.4796 2.9189 2.5973 0.7885 0.9292 1.4271 0.9355 1.5127 1.4993 1.4984 1.4927 0.9900 0.9900 1.5131 0.9899 0.9906 0.9807 0.9799 0.9793 0.9800 0.9794 0.9804 0.9802 0.9800 0.9801 | 1.5596 1.5647 1.6510 1.6700 2.1769 1.9940 3.0521 2.0238 0.9442 0.9439 1.4295 0.9466 1.5237 1.5128 1.4917 1.5120 1.0743 1.0802 1.5255 1.0731 1.0836 1.0776 1.0788 1.0773 1.0765 1.0768 1.0757 1.0766 1.0767 1.0772 |
| O2-P1-O3 O2-P1-O4 O2-P1-O5 O3-P1-O4 O3-P1-O5 O4-P1-O5 P1-O2-H11 P1-O2-H18 H11-O2-H18 P1-O3-H11 P1-O3-H27 H11-O3-H27 P1-O4-H6 P1-O5-H7 C13-O8-H28 C10-N9-C16 C10-N9-C20 C10-N9-C24 C16-N9-C20 C16-N9-C24 C20-N9-C24 N9-C10-H11 N9-C10-H12 N9-C10-C13 H11-C10-H12 H11-C10-C13 H12-C10-C13 O2-H11-O3 O2-H11-C10 O3-H11-C10 O8-C13-C10 O8-C13-H14 O8-C13-H15 C10-C13-H14 C10-C13-H15 H14-C13-H15 N9-C16-H17 N9-C16-H18 N9-C16-H19 H17-C16-H18 H17-C16-H19 H18-C16-H19 O2-H18-C16) N9-C20-H21 N9-C20-H22 N9-C20-H23 H21-C20-H22 H21-C20-H23 H22-C20-H23 N9-C24-H25 N9-C24-H26 N9-C24-H27 H25-C24-H26 H25-C24-H27 H26-C24-H27 O3-H27-C24 | 118.0941 110.1926 110.2356 107.6588 109.5320 99.49300 63.74270 112.1032 53.56100 114.9068 113.0111 76.97170 115.7665 115.7193 111.1013 108.9753 110.4279 110.1260 108.0793 109.7697 109.4304 106.9119 109.7768 115.9435 107.1314 106.4675 110.1568 55.42470 124.5887 142.4157 111.6229 102.6649 110.7388 109.1925 113.6050 108.3895 112.7768 111.8669 112.7130 104.9154 109.3990 104.5807 178.5276 110.9159 111.2376 111.5295 107.7938 107.1500 108.0303 112.8372 112.3725 109.4138 109.3152 106.4662 106.0463 146.7567 | 115.2025 104.8051 110.6392 109.7790 110.2419 105.6110 83.88710 117.5342 47.85040 93.05890 125.2276 51.60660 112.8081 116.6101 114.4546 107.4590 110.5218 110.6509 108.6678 108.7668 110.6793 108.5491 108.5395 114.8995 107.5430 108.5168 108.5591 49.06090 140.0236 147.1515 107.1071 110.3274 110.2834 110.3258 110.2818 108.5179 109.4362 109.4795 109.5027 109.4601 109.4340 109.5147 166.1196 109.4708 109.5114 109.4717 109.4455 109.4325 109.4953 109.4694 109.4779 109.4626 109.4455 109.4584 109.5135 163.7030 | 114.4758 109.3743 112.7916 112.9171 109.0730 96.92980 106.4843 132.1126 63.64720 73.79680 104.6566 57.67080 119.8925 121.2556 114.0569 107.2030 110.7378 111.5392 109.1362 108.9778 109.1874 106.3741 105.9612 115.1457 109.2989 109.6140 110.2359 57.44080 149.4005 108.5808 107.7412 106.0737 110.3288 110.3651 112.5589 109.5586 108.1546 108.2463 108.3156 109.9121 109.9978 112.1043 152.3302 109.3064 109.0363 109.8613 109.5431 109.7702 109.3076 108.6933 107.9333 110.1946 109.5095 109.1620 111.3023 164.1466 |

Figure 2S The optimized molecular structure of 2-HDETDHP.

Table 3S FT-IR vibrational wavenumbers (cm−1) and assignments.

| FT-IR | Assignements |
| --- | --- |
| 3416 3329 3070 2821 2682 2342 2328 1725 1611 1333 1264 1030 997 540 | O–H stretching of water N–H stretching N–H···O, N–H···N stretching P–O–H asymmetric stretching of hydroxide group P–O–H symmetric stretching of hydroxide group O–H···O asymmetric stretching, with water molecules Vibrations of hydrogen bonds formed Quadrant stretching; CNC bending Side-chain asymmetric C–N stretching P=O stretching P–O asymmetric stretching P–O symmetric stretching P–O–H deformation C–N bending vibration |

Table 4S Adjust elements of the full transition hyperpolarizability tensor of [2-HDETDHP].

| XXX | 1.00 | YXX | 2.757 |
| --- | --- | --- | --- |
| XXY | 0.00 | YXY | 0.00 |
| XXZ | 2.55 | YXZ | 5.491 |
| XYX | 0.00 | YYX | 0.00 |
| XYY | 0.386 | YYY | 0.830 |
| XYZ | 0.00 | YYZ | 0.00 |
| XZX | 2.55 | YZX | 5.491 |
| XZY | 0.00 | YZY | 0.00 |
| XZZ | -1.375 | YZZ | -4.644 |

Table 5S Adjust elements of the transition polarizability tensor Alpha of 2-HDETDHP.

| XX | 2.850 | YX | -2.015 | ZX | -0.00 |
| --- | --- | --- | --- | --- | --- |
| XY | -2.015 | YY | 1.480 | ZY | -0.00 |
| XZ | -0.00 | YZ | -0.00 | ZZ | -0.202 |

Milliken population analysis

The Milliken charge distribution of every atom in 2-HDETDHP is displayed in Table 5S. The atoms of the asymmetric unit are listed. The atoms in the molecule have the following numbers: The atomic charge distribution shows that the eight anions have negative charges ranging from -0.72 to -0.50, whereas the H15 and P1 atoms of phosphate have positive charges ranging from 0.152376 to 1.5110.The negative charges of C20, C10, and N9 for the aliphatic group are -0.365832, -0.235895, and -0.516157, in that order. The outcomes of the molecular electrostatic potential study are consistent with this result. Hydrogen atoms have a positive charge that varies from 0.21 to 0.41 according on the atom they are attached to. In conclusion, an approximate value of 0.2 electrons is assigned to the electrical transition from anion to cation.

Table 5S Milliken population analysis in 2-HDETDHP

| Atoms | DFT | HF |
| --- | --- | --- |
| P1 O2 O3 O4 O5 H 6 H7 O8 N 9 C10 H11 H12 C13 H 14 H 15 C16 H 17 H18 H 19 C20 H21 H 22 H 23 C 24 H 25 H 26 H 27 H28 | 1.511969 -0.794571 -0.793442 -0.754216 -0.773005 0.411430 0.400796 -0.573683 -0.516157 -0.235895 0.322516 0.173959 -0.120157 0.265867 0.152376 -0.392850 0.200504 0.336750 0.192870 -0.365832 0.217411 0.220440 0.218950 -0.398528 0.196736 0.198659 0.342520 0.354584 | 2.069530 -0.997768 -0.988038 -0.928522 -0.950915 0.459417 0.453837 -0.704295 -0.655671 -0.174478 0.338229 0.176861 -0.031365 0.277436 0.145771 -0.354377 0.195804 0.365296 0.188029 -0.319400 0.213598 0.216533 0.215107 -0.361083 0.190883 0.195840 0.375641 0.388100 |

FMO Theory

Named as frontier molecular orbital (FMOs), both the highest occupied molecular orbital (HOMO) is an electron donor and the lowest unoccupied molecular orbital (LUMO) is an electron acceptor one. In the present study, the (HOMO – 0.17719 a.u.) and (LUMO -0.01585a.u.) energies were predicted atB3LYPmethod with the 6-311Gbasis set. According to the obtained results, the energy gap between the HOMOs and LUMOs represents the critical parameter in determining the molecular electrical transport properties which help the electron conductivity measurement. The frontier molecular orbitals’ energies (EHOMO, ELUMO) were used to calculate the global chemical reactivity descriptors of the molecule such as the ionization potential electron affinity, the electronegativity, the global hardness, the global softness, the chemical potential and the electrophilicity index. These important descriptors are calculated as follows:

Ionization potential: IP = - EHOMO

Electron affinity: EA = - ELUMO

Electronegativity: χ= - 1/2(ELUMO+ EHOMO)

Chemica lpotential: μ= 1/2(ELUMO + EHOMO)

Global hardness: η= 1/2(ELUMO- EHOMO)

Global softness: S = 1/2η

Electrophilicity index: ω= μ2/2η

Where A is the ionization potential and I is the electron affinity of the molecule. Both parameters can be expressed through HOMO and LUMO orbital energies as I = –EHOMO and EA = –ELUMO. The electro affinity and the Ionization potential of 2-HDETDHP are given in Table 7. The calculated values of the softness, the hardness, the chemical potential, the electronegativity and the electrophilicity index of the molecule are found to be respectively 6.08 eV by B3LYP/6-311G. The soft molecule represents a small HOMO-LUMO gap, while that of the hard molecule is supposed to be large.

Table 6S Difference of energies between the possible combinations, chemical potential,
Electronegativity, Global hardness, Softness and Electrophilicity. All values are in eV
except for S which is given in eV-1.

| DFT/B3LYP/6e311G | Values |
| --- | --- |
| EHOMO (eV) ELUMO (eV) ΔEHOMO-LUMO gap (eV) Chemical Potential μ (eV) Electronegativity χ (eV) Global hardness η (eV) Softness S (eV-1) Electrophilicity (eV) | -4.8188 -0.4313 4.3900 -2.6250 +2.6250 2.1937 0.2279 1.1966 |

Figure 2S Frontier molecular orbitals analysis of 2-HDETDHP