+

Filler (Alumina)

Epoxy Resin

CFW-EP-AL

CFW-EP

EP

Fabricate hybrid composite samples

Recycled carbon fibre prepreg waste

Water absorption testing for 168 hours

| CFW-EP | Solution | Carbon Fibre Waste (wt%) | Epoxy Resin (wt%) | Flexural Strength (MPa) Fit | Composite Desirability |
| --- | --- | --- | --- | --- | --- |
|  | 1 | 2.5 | 97.5 | 91.321 | 1 |

| CFW-EP-AL | Solution | Carbon Fibre Waste (wt%) | Epoxy Resin (wt%) | Alumina (wt%) | Flexural Strength (MPa) Fit | Composite Desirability |
| --- | --- | --- | --- | --- | --- | --- |
|  | 1 | 2.5 | 95 | 2.5 | 130.161 | 1 |

Flexural testing before and after immersion in distilled water

Minitab software optimization for composition of CFW-EP and CFW-EP-AL samples