Supplementary Materials

Recycling of Poly (Methyl Methacrylate) Waste Sheets to Synthesize Catalyst-Free Bi-Functional Cation Exchange Resin for Sequestering of Toxic Pollutants

Ruba Arif1,2, Syed Wasim Ali1, Muhammad Saifullah1, Shabnam Shahida2*, Sajid Iqbal3*

1Chemistry Division, Pakistan Institute of Nuclear Science and Technology (PINSTECH), P.O., Nilore, Islamabad, 45650, Pakistan

2Department of Chemistry, University of Poonch, Rawalakot, Azad Jammu & Kashmir, Pakistan

3Department of Nuclear and Quantum Engineering, KAIST, 291 Daehak-ro, Yuseong-gu,

Daejeon 34141, Republic of Korea

*Corresponding authors:

sajid1@kaist.ac.kr (S. Iqbal),

shabnamshahida01@gmail.com (S. Shahida)

Table S4: Comparison of the base copolymer and resin synthesized at (20 % cross-linked) by recovered monomer from waste polymethylmethacrylate and fresh methylmethacrylate from Alfa Acer.

| Type | Characteristics | Diluent/Porogen |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Cyclohexane |  | Methylisobutyl ketone |  | Toluene |  | Cyclohexanone |  |
|  |  | Rm (E1) | Cm (E2) | Rm (E3) | Cm (E4) | Rm (E5) | Cm (E6) | Rm (E7) | Cm (E8) |
| Copolymer | PSR (µm)* | 300-690 | 180-900 | 90-600 | 120-660 | 150-690 | 120-700 | 60-360 | 90-390 |
|  | Y (%) | 66.48 | 63.60 | 82.61 | 89.60 | 85.80 | 89.62 | 80.70 | 81.66 |
|  | dBP (g/ml) | 0.38 | 0.46 | 0.49 | 0.48 | 0.55 | 0.50 | 0.64 | 0.55 |
|  | PV (ml/g) | 0.68 | 0.49 | 0.41 | 0.43 | 0.31 | 0.39 | 0.19 | 0.28 |
|  | SCa (%) | 28.30 | 23.70 | 28.0 | 24.44 | 80.90 | 69.50 | 52.60 | 48.10 |
|  | SCm (%) | 27.0 | 19.5 | 24.8 | 22.96 | 76.10 | 65.2 | 69.4 | 51.80 |
| Resin | dr (g/ml) | 0.68 | 0.57 | 0.56 | 0.53 | 0.72 | 0.65 | 0.65 | 0.60 |
|  | SCw (%) | 100.12 | 48.16 | 60.03 | 56.75 | 50.84 | 82.19 | 47.85 | 56.27 |
|  | SCH-Na (%) | Nil | 12.93 | Nil | 5.88 | 2.27 | 10.00 | 5.62 | 11.11 |
|  | CPw (meq/ml) | 1.08 | 1.05 | 0.93 | 0.86 | 0.98 | 1.00 | 1.17 | 1.08 |
|  | CPs (meq/ml) | 0.80 | 0.79 | 0.73 | 0.64 | 1.00 | 0.78 | 1.00 | 1.00 |
|  | CPT(meq/ml) | 1.88 | 1.84 | 1.66 | 1.40 | 1.98 | 1.78 | 2.17 | 2.08 |

*Based on microscopic analysis of the beads.

[ Particle size range, PSR.  (µm)*,   Yield, Y (%), Density, dBP (g/ml), Pore volume, PV (ml/g), swelling coefficient in acetone, SCa (%), the swelling coefficient in methanol, SCm (%), Resin: Density, dr (g/ml), swelling coefficient in water SCw (%), swelling coefficient, H to Na, SCH-Na (%), capacity weak acid, CPw, capacity strong acid, CPs, total capacity, CPT] Recovered monomer = Rm, Commercially available monomer = Cm

Table S5: Comparison of the base copolymer and cation exchange resin synthesized by recovered MMA from waste PMMA and fresh MMA from Alfa Acer. [Particle size range, PSR(µm)*,  Yield, Y (%), Density, dBP (g/ml), Pore volume, PV (ml/g), swelling coefficient in acetone, SCa (%), swelling coefficient in methanol, SCm (%), Resin: Density, dr (g/ml), swelling coefficient in water SCw (%), swelling coefficient, H to Na, SCH-Na (%), capacity weak acid, CPw, capacity strong acid, CPs, total capacity, CPt] Recovered monomer = Rm, Commercially available monomer = Cm

(*Based on microscopic analysis of the beads)

|  | Characteristics | X- Linking (%) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 4 |  | 10 |  | 15 |  | 20 |  | 25 |  | 30 |  | 40 |  |
|  |  | Rm (E 9) | Cm (E 10) | Rm (E 11) | Cm (E 12) | Rm (E 13) | Cm (E 14) | Rm (E 3) | Cm (E 4) | Rm (E 15) | Cm (E 16) | Rm (E17) | Cm (E18) | Rm (E19) | Cm (E20) |
| Copolymer | PSR (µm)* | 90- 360 | 120- 570 | 90- 450 | 60- 450 | 120- 600 | 90- 450 | 90- 600 | 120- 660 | 150- 540 | 180- 540 | 150- 540 | 150- 540 | 150- 600 | 120- 720 |
|  | Y (%) | 64.82 | 80.01 | 76.83 | 79.17 | 80.48 | 82.77 | 82.61 | 89.61 | 88.51 | 89.76 | 92.15 | 91.05 | 94.28 | 91.85 |
|  | dBP (g/ml) | 0.68 | 0.61 | 0.67 | 0.65 | 0.55 | 0.53 | 0.49 | 0.48 | 0.47 | 0.48 | 0.46 | 0.43 | 0.45 | 0.44 |
|  | PV (ml/g) | 0.12 | 0.18 | 0.122 | 0.137 | 0.276 | 0.316 | 0.408 | 0.434 | 0.460 | 0.436 | 0.488 | 0.539 | 0.52 | 0.546 |
|  | SCa (%) | 200 | 162.5 | 123 | 100.0 | 49.0 | 48.00 | 28.0 | 24.44 | 26.9 | 25.0 | 29.2 | 24.2 | 10.7 | 22.16 |
|  | SCm (%) | 35.3 | 50.0 | 88.2 | 62.1 | 40.9 | 44.00 | 24.8 | 22.96 | 26.9 | 25.0 | 26,8 | 21.2 | 9.2 | 24.08 |
| Resin | dr (g/ml) | 0.75 | 0.71 | 0.75 | 0.77 | 0.68 | 0.68 | 0.56 | 0.53 | 0.55 | 0.54 | 0.53 | 0.56 | 0.52 | 0.55 |
|  | SCw (%) | 65.24 | 28.57 | 105.12 | 110.20 | 59.73 | 77.27 | 60.03 | 56.75 | 44.08 | 38.18 | 46.43 | 28.30 | 23.32 | 25.92 |
|  | SCH-Na (%) | 12.5 | 39.13 | 10.00 | 5.26 | 4.56 | 23.46 | Nil | 5.88 | Nil | 9.33 | Nil | 5.83 | Nil | 3.33 |
|  | CPW (meq/ml) | 2.38 | 3.25 | 1.79 | 1.76 | 0.79 | 1.46 | 0.93 | 0.86 | 0.49 | 0.43 | 0.36 | 0.31 | 0.39 | 0.42 |
|  | CPS (meq/ml) | 0.24 | 0.23 | 0.36 | 0.48 | 0.55 | 0.54 | 0.73 | 0.64 | 0.78 | 0.82 | 0.84 | 0.95 | 1.01 | 0.95 |
|  | CPT (meq/ml) | 2.62 | 3.48 | 2.15 | 2.24 | 1.34 | 2.00 | 1.66 | 1.40 | 1.27 | 1.25 | 1.20 | 1.26 | 1.40 | 1.37 |