Table 1. BET analyses of synthesized compounds

| Sample | Surface area(m2/g)a | SBET Micro | SBET Mesob | Total pore volumec | Size BJH |
| --- | --- | --- | --- | --- | --- |
| HY | 530 | 510 | 50 | 0.39 | 2.45 |
| HY-N-SO3H | 305 | 140 | 165 | 0.20 | 1.29 |

a Calculated by the BET method, b Calculated by the t-plot method, c Obtained at a relative pressure of 0.99.

Table 2. Synthesis of different coumarins using HY/NaY/MCM-N-SO3H as a catalyst

| aEntry | Catalyst (g) | Substrate | Solvent | Time (min) | Mp(◦C) | Yields (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | HY-N-SO3H (0.02) | Resorcinol | - | 180 | 157-159 | 49 |
| 2 | HY-N-SO3H (0.04) | Resorcinol | - | 110 | 157-159 | 61 |
| 3 | HY-N-SO3H (0.08) | Resorcinol | - | 45 | 157-159 | 99 |
| 4 | HY-N-SO3H (0.1) | Resorcinol | - | 90 | 157-159 | 97 |
| 5 | HY-N-SO3H (0.08) | Phenol | - | 45 | 83-86 | 72 |
| 6 | HY-N-SO3H (0.08) | Resorcinol | DMF | 45 | 156-158 | 70 |
| 7 | HY-N-SO3H (0.08) | Resorcinol | THF | 45 | 156-158 | 60 |
| 8 | HY-N-SO3H (0.08) | Resorcinol | H2O | 45 | 156-158 | 75 |
| 9 | HY-N-SO3H (0.08) | Resorcinol | CH3CN | 45 | 156-158 | 80 |
| 10 | NaY (0.08) | Resorcinol | - | 45 | 156-158 | 25 |
| 11 | HY (0.08) | Resorcinol | - | 45 | 156-158 | 36 |
| 12 | MCM-41 (0.08) | Resorcinol | - | 45 | 156-158 | Trace |
| 13 | NaY-N-SO3H (0.08) | Resorcinol | - | 45 | 156-159 | 52 |
| 14 | NaY-N-SO3H (0.08) | Phenol | - | 45 | 84-85 | 39 |
| 15 | MCM-N-SO3H | Phenol |  | 45 | 84-85 | 13 |
| 16 | MCM-N-SO3H | Resorcinol |  | 45 | 156-158 | 38 |
| 17 | Without catalyst | Phenol, Resorcinol | - | 45 | - | Trace |

a Condition: Catalyst (0.08 g), phenol or resorcinol (1 mmol), ethyl acetoacetate (1 mmol), solvent free, 110 ˚C.

Table 3. Optimization of reaction condition for synthesis of N-Phenyl formamide as the model reaction

| Entry | Catalyst (g) | HCOOH (mmol) | Solvent (1ml) | Time (min) | Yields (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | HY-N-SO3H (0.01) | 1.2 | Solvent free | 120 | 10 |
| 2 | HY-N-SO3H (0.015) | 1.2 | Solvent free | 35 | 60 |
| 3 | HY-N-SO3H (0.02) | 1.2 | Solvent free | 9 | 99 |
| 4 | HY-N-SO3H (0.03) | 1.2 | Solvent free | 20 | 98 |
| 5 | HY-N-SO3H (0.02) | 1.5 | Solvent free | 25 | 60 |
| 6 | HY-N-SO3H (0.02) | 1.2 | THF | 8 | 98 |
| 7 | HY-N-SO3H (0.02) | 1.2 | MeCN | 10 | 97 |
| 8 | HY-N-SO3H (0.02) | 1.2 | Ethylacetate | 3 | 99 |
| 9 | Without catalyst | 2 | Solvent free | 240 | Trace |
| 10 | NaY(0.02) | 2 | Solvent free | 20 | 5 |
| 11 | HY(0.02) | 2 | Solvent free | 20 | 20 |
| 12 | MCM-41(0.02) | 2 | Solvent free | 20 | Trace |
| 13 | NaY-N-SO3H (0.02) | 2 | Solvent free | 20 | 80 |
| 14 | MCM-N-SO3H (0.02) | 2 | Solvent free | 20 | 61 |

Table 4. Formylation of different amines

| Entrya | Substrate | Product | Time (min) | Yields (%)b | Melting point (◦C) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Found | Reported |
| 1 |  |  | 9 | 99 | 47-49 | 46-4842 |
| 2 |  |  | 9 | 99 | 51-53 | 52-5442 |
| 3 |  |  | 60 | 48 | 198-200 | 196-19742 |
| 4 |  |  | 7 | 99 | 142-144 | 141-14342 |
| 5 |  |  | 35 | 86 | 102-104 | 99-10143 |
| 6 |  |  | 40 | 74 | 116-118 | 115-11943 |
| 7 |  |  | 60 | 82 | 76-78 | 78-8043 |
| 8 |  |  | 47 | 69 | * | New |

a Condition: amine (1 mmol), formic acid (1.2 mmol), catalyst (0.02 g), room temperature, solvent free,  b Isolated yields.

* IR (Cm-1): 3134, 2980, 2823, 2696, 1689, 1589, 1454, 1386, 1240, 1006, 864, 748, 615, 543, 422.

1H NMR (DMSOd6, δ= ppm): 6.89 (NH, 2 H), 7.20, 7.21 (Ar-H, 2 H), 7.62, 7.65 (Ar-H, 2 H), 8.22 and 8.34 (CHO, 2 H). 13C NMR (DMSOd6, δ= ppm): 115.4, 122.5, 137.6, 142.0, and 163.6.

Table 5. Comparison catalytic activity of [HY-N-SO3H] with other heterogeneous catalyst for preparation of coumarins

| Catalyst | Catalyst amount | Time (min) | Temperature (◦C) | Yield (%) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Uncatalyzed (solvent) | - | 383 | 78 | 89 | 45 |
| Mesoporous zirconium phosphate (m-ZrP) | 10 wt% | 160 | 150 | 76 | 46 |
| SiO2/Sulfated (20%) (solvent) | 100 mmol | 240 | 200 | 100 | 47 |
| CNC-AMPD-Pd | 0.5 %mol | 120 | 130 | 94 | 48 |
| Zn0.925 Ti0.075 O NPs | 10 %mol | 180 | 110 | 76 | 24 |
| Co/SBA-15 | 0.1 %mol | 180 | 110 | 98 | 49 |
| CMK-5-SO3H | 3 %mol | 20 | 130 | 95 | 50 |
| SnCl4 grafted on silica gel | 5 %mol | 360 | 60 | 63 | 51 |
| ZrO2-TiO2 | 0.050 g | 180 | Room temperature | 97 | 52 |
| [MTMSPIm]Cl@HY-Z (Cu) | 0.18 g | 150 | 130 | 96.5 | 23 |
| Acidic ionic liquid (solvent) | 0.078 g | 120 | 85 | 75 | 53 |
| HY-N-SO3H | 0.08 g | 45 | 110 | 99 | Present |

Table 6. Studying efﬁciency of the present protocol over some reported catalysts to preparation of formamides

| Catalyst | Solvent and reagent | Temperature (◦C) | Time(min) | Yield (%) | Ref. |
| --- | --- | --- | --- | --- | --- |
| α-Fe2O3@HAp-SO3H | Solvent free | Room temperature | 20 | 97 | 54 |
| [N(C4H9)4]3[CrMo6O18(OH)3 C(OCH2)3CH3] | 1,4-dioxane | 80 | 1440 | 91 | 28 |
| Clinoptilolite (Pd@MCP) | Solvent free | 70 | 20 | 97 | 55 |
| POMP-NHC-Ir | MeOH | 120 | 1440 | 80 | 56 |
| HClO4-SiO2 | THF | Room temperature | 15 | 96 | 57 |
| Natrolite zeolite | Solvent free | Room temperature | 20 | 89 | 58 |
| Protic ionic liquid | Solvent free | 70 | 60 | 97 | 59 |
| (NH4)3[FeMo6O18(OH)6] | Additive Na2SO3 | 80 | 120 | 99 | 29 |
| Sulfated titania | MeCN | Room temperature | 30 | 99 | 60 |
| Iodine | Solvent free | 70 | 240 | 96 | 61 |
| HY-N-SO3H | Solvent free | Room temperature | 9 | 99 | present |