Supporting information

Revisiting the absolute green synthesis of MFI zeolite and derived metal-acid bifunctional catalyst

Wenqi Xu, Hongqing Li, Mengxuan Zhu, Rui Wang, Heng Jiang, Changzi Jin*

School of Petrochemical Engineering, Liaoning Petrochemical University, Fushun, 113001, China

E-mail address: jin_chz@163.com (Changzi Jin)

Figure S1 XRD pattern of as-synthesized products prepared from Al-free starting materials. Synthesis condition: Na2O/SiO2=0.072, H2O/SiO2=2.0, 170 oC, 24h.

Table S1 Crystallization of ZSM-5 zeolite under different conditions

| Na2O/SiO2 | SiO2/Al2O3 | SiO2/H2O | t/h | T/℃ | Relative crystallinity |
| --- | --- | --- | --- | --- | --- |
| 0.036 | 40 | 1：2 | 24 | 170 | - |
| 0.072 | 40 | 1：2 | 24 | 170 | 10% |
| 0.108 | 40 | 1：2 | 24 | 170 | 54% |
| 0.144 | 40 | 1：2 | 24 | 170 | 23% |
| 0.072 | 40 | - | 24 | 170 | - |
| 0.072 | 40 | 1：1 | 24 | 170 | 48% |
| 0.072 | 40 | 1：3 | 24 | 170 | 86% |
| 0.072 | 40 | 1：4 | 24 | 170 | 93% |
| 0.072 | 30 | 1：2 | 24 | 170 | 95% |
| 0.072 | 50 | 1：2 | 24 | 170 | 52% |
| 0.072 | 60 | 1：2 | 24 | 170 | 33% |
| 0.072 | 100 | 1：2 | 24 | 170 | 52% |
| 0.072 | - | 1：2 | 24 | 170 | 26% |
| 0.072 | 40 | 1：2 | 24 | 150 | - |
| 0.072 | 40 | 1：2 | 12 | 170 | - |
| 0.072 | 40 | 1：2 | 18 | 170 | 61% |
| 0.072 | 40 | 1：2 | 48 | 170 | 88% |
| 0.072 | - | 1：2 | 24 | 170 | 30% |
| 0.072 | - | 1：2 | 72 | 170 | - |
| 0.072 | 60 | 1：2 | 24 | 170 | 88% |

Figure S2 XRD pattern of as-synthesized products prepared from different Na and Al precursors.

Synthesis condition: SiO2/Al2O3 =40, Na2O/SiO2=0.072, H2O/SiO2=2.0, 170 oC, 24h.

Figure S3 XRD pattern of as-synthesized products prepared by addition of ethanol.

Synthesis condition: SiO2/Al2O3 =40, Na2O/SiO2=0.072, ethanol/SiO2=2.0, 170 oC, 24h.

Figure S4 TEM image of Stӧber SiO2 sphere.

Figure S5 TEM image of PVP-protected Pt nanoparticles.

Figure S6 XRD pattern of as-synthesized products prepared with Stӧber SiO2 sphere by addition of Pt nanoparticles.

Table S2 Detailed products distribution for hydroisomerization of n-heptane over Pt@SiO2 and Pt/SiO2 at 240 oC

| Selectivity (C mol%) |  | Pt@SiO2 | Pt/SiO2 |
| --- | --- | --- | --- |
| Isomers | 2-Methyl Hexane | 33.11 | 12.09 |
|  | 3-Methyl Hexane | 24.85 | 11.39 |
|  | 3-Ethyl Pentane | 0.50 | 0.40 |
|  | 2, 2-Dimethylpentane | 0.03 | 0.01 |
|  | 2, 4-Dimethylpentane | 0.87 | 0.31 |
|  | 3, 3-Dimethylpentane | <0.01 | 0.01 |
| Cracking | Methane | <0.01 | <0.01 |
|  | Ethane | <0.01 | 0.01 |
|  | Propane | 15.21 | 24.71 |
|  | Iso-Butane | 22.99 | 36.70 |
|  | Butane | 0.27 | 1.42 |
|  | Pentane | 0.36 | 1.48 |
|  | 2-Methyl Pentane | 0.13 | 0.32 |
|  | 3-Methyl Pentane | 0.05 | 0.17 |
|  | Hexane | 0.32 | 1.17 |
| Others | Methyl Cyclohexane | 0.46 | 0.75 |
|  | Ethyl Cyclopentane | 0.29 | 0.74 |
|  | Toluene | <0.01 | 0.03 |
|  | Unkown components | 0.54 | 8.28 |