# Supporting Information for

Hydroxy-terminated polybutadiene polyurethane demonstrates exceptional mechanical performance at low temperatures through cross-linking reaction with hyperbranched polysiloxane

Junshan Yuan,† Xiaoying Huang,† Rui Wang, Wei Tian, Weixu Feng and Hongxia Yan*

Key Laboratory of Special Functional and Smart Polymer Materials of Ministry of Industry and Information Technology, Shaanxi Key Laboratory of Macromolecular Science and Technology, School of Chemistry and Chemical Engineering, Northwestern Polytechnical University, Xi'an, Shaanxi, 710129, PR China

Content                                                                                                                  Page

# Fig. S1.  The reaction mechanism of HBPSi-NH2/HTPB composites.S2

# Fig. S2.  FTIR spectra of distillate of HBPSi-NH2 and standard ethanolS2

# Fig. S3.  GPC curve of HBPSi-NH2S2

# Table S1.  GPC data of HBPSi-NH2S2

# Table S2.  Titrimetric results of -OH content in HBPSi-NH2 S3

# Table S3.  Thermal decomposition data of HTPB-0 and HTPB-4 S4

# Fig. S1.  The reaction mechanism of HBPSi-NH2/HTPB composites.

# Fig. S2.  FTIR spectra of distillate of HBPSi-NH2 and standard ethanol.

# Fig. S3.  GPC curve of HBPSi-NH2.

# Table S1  GPC data of HBPSi-NH2.

| Polymer | Mn | Mw | Mz | Mz+1 | PDI (Mw/Mn) |
| --- | --- | --- | --- | --- | --- |
| HBPSi-NH2 | 16300 | 16700 | 17100 | 17500 | 1.02 |

The content of -OH group was determined by titrimetric methods referring to GB/T 7383-2007 (Chinese standard). Firstly, weighed 140 g phthalic anhydride in a beaker, adding 1L pyridine and stirring the mixture until completely dissolved to obtain phthalic anhydride pyridine solution, recorded as acylation reagent. Transferred 25.0 mL acylation reagent into a 250 mL conical flask with a pipette. Then, the sample to be tested was accurately weighed (accurate to 0.001g), mixed with 25.0 mL acylation reagent, and then condensed for reflux for 1 h at 115℃±2℃. Added 4~5 drops phenolphthalein indicator, dropped with sodium hydroxide standard liquid, and recorded the amount of NaOH solution consumed (repeat 3 times). The controlled trial without HBPSi-NH2 was performed 3 times. The I(OH) was calculated by using Eqn (1).

(1)

Where I(OH) is the -OH value of HBPSi-NH2; V0 and V1 are the amount of NaOH solution consumed by controlled trial and HBPSi-NH2 samples, respectively; c is the concentration of NaOH solution; m0 is the mass of the HBPSi-NH2 sample. The result of the titration are listed in Table S2.

# Table S2  Titrimetric results of -OH content in HBPSi-NH2.

| Test number | c (mol·L-1) | V0 (mL) | V1 (mL) | m (g) | I(OH) (mol·g-1) |
| --- | --- | --- | --- | --- | --- |
| Controlled 1 | 0.5 | 83.5 | — | — |  |
| Controlled 2 | 0.5 | 84.2 | — | — |  |
| Controlled 3 | 0.5 | 84.3 | — | — |  |
| Average | 0.5 | 84 | — | — |  |
| 1 | 0.5 | 84 | 67.7 | 0.4059 | 20.08×10-3 |
| 2 | 0.5 | 84 | 70.8 | 0.3003 | 21.98×10-3 |
| 3 | 0.5 | 84 | 70.9 | 0.3053 | 21.45×10-3 |
| Average | — | — | — | — | 21.17×10-3 |

# Table S3  Thermal decomposition data of HTPB-0 and HTPB-4.

|  | 5wt% loss(℃) | 50wt% loss(℃) | DTG(℃) |
| --- | --- | --- | --- |
| HTPB-0 | 321.1 | 444.01 | 472.16 |
| HTPB-4 | 323.98 | 479.04 | 485.71 |