Supplementary Information

Ion migration as a tool to enhance the performance of perovskite CsPbBr3 -ray detectors

Lei Pan1†, Khasim Saheb Bayikadi1†, Indra Raj Pandey1,2, Sujita Karki1, Zhifu Liu3, John A. Peters3,4, Michael De Siena1, Duck Young Chung2, Bruce W. Wessels3, and Mercouri G. Kanatzidis1,2,3*

1Department of Chemistry, Northwestern University, Evanston, IL 60208, USA

2Materials Science Division, Argonne National Laboratory, Lemont, IL 60439, USA

3Department of Materials Science and Engineering, Northwestern University, Evanston, IL 60208, USA

4Department of Chemistry, Physics, & Engineering Studies, Chicago State University, Chicago, IL 60608

†These authors contributed equally to this work

*Correspondence to: m-kanatzidis@northwestern.edu

Supplementary Figure 1.a, reverse current decreasing at different bias voltage. all measurements were performed at room temperature. b, reverse currents normalized to their respective initial values to better observe the decreasing speed. Itis noted that each time after testing at a reverse bias voltage, we applied forward bias to the detector until the small forward current increased to similar large values. Then reverse current decreasing testing at another bias voltage was performed.

Supplementary Figure 2. A CsPbBr3 device with Bi and Au electrode deposited on the same side of the crystal for contact potential difference measurement. The width of the electrodes is ~ 1 mm and the separation of the two electrodes is 2.6 mm.

Supplementary Figure 3. Work function of Kelvin Probe is calibrated to be 5 eV. Without any deliberate biasing, the work function of Bi and Au electrode deposited on CsPbBr3 surface is measured to be 4.8 eV and 5.2 eV, respectively, by the Kelvin Probe. Bandgap and electron affinity of CsPbBr3 is 2.3 eV and 3.3 eV respectively, which is measured in our previous work1. CBM and VBM stand for conduction band minimum and valance band maximum, respectively.

Supplementary Figure 4. As grown CsPbBr3 ingot show quality gradient affected by impurity concentration (adopted from our previous work2). a, PL decay lifetime ave of crystals from different part of the ingot.PL decay time decreases from the bottom part to the top part. The ingot has a color gradient with top part darker than the bottom tip part, which means more impurities in the top part. Shorter PL decay time of the top part of as-grown CsPbBr3 ingot is due to excessive extrinsic impurities. Longer PL decay time means less impurities. b, A typical correlation ofave of crystal from the same ingot but different location in the ingot. c, Statistical correlation of ave and peak of CsPbBr3 crystals from many ingots. Longer PL decay time is usually accompanied by longer PL emission wavelength.

To elucidate the impact of biasing-induced ion migration on CsPbBr3 crystal defect characteristics, a meticulous experimental design was implemented. Two discrete sets of detectors were fashioned from two crystal discs denoted as set-I and set-II, each possessing a uniform thickness of 2 mm. Within each set, four detectors were systematically engineered, with one maintained in an unbiased state and the remaining three subjected to a reverse bias voltage of 300 V for distinct durations. After the crystals were treated with different biasing time, employing a 375 nm pulsed laser diode as the excitation source at ambient temperature, steady-state, and time-resolved photoluminescence (PL) spectra of these crystals were diligently recorded utilizing an Edinburgh Instruments FS5 spectrofluorometer equipped with a 395 nm grating filter. Notably, to obviate any potential confounding effects from surface preparation procedures, PL measurements were exclusively conducted on freshly cleaved crystal surfaces.

Detailed outcomes pertaining to the PL emission characteristics and time-resolved PL decay times have been documented within Table S1 for the set-I and Table S2 for the set-II, respectively. These tables show the nuanced variations in PL emission wavelengths as well as the elongation of the PL decay times after biasing-induced ion migration.

Table S1. PL measurement results of the four CsPbBr3 crystals from the set-I subject to reverse biasing.

| Biasing time | Emission peak peak (nm) | ave (ns) at 529 nm | Fitted decay time components |
| --- | --- | --- | --- |
| None-biased | 529 | 43.1 | τ1: 15.2 ns (B1: 32.53%) τ2: 56.6 ns (B2: 67.47%) |
| 8 hours | 529 | 70.2 | τ1: 19.6 ns (B1: 30.52%) τ2:92.5 ns (B2: 69.48%) |
| 12 hours | 533 | 65.97 | τ1:17.7 ns (B1: 25%) τ2:82.1 ns (B2: 74.95%) |
| 15 hours | 533 | 62.38 | τ1:17.66 ns (B1: 31.42%) τ2:82.84 ns (B2: 68.58%) |

The PL decay was fitted to a multi-exponential decay equation Rt=B1e-t/τ1+B2e-t/τ2+B3e-t/τ3, where Rt is measured PL intensity, B1, B2, B3 are proportionality coefficients. τave is intensity averaged lifetime calculated as τave=Biτi2Biτi.

Table S2. PL measurement results of the four CsPbBr3 crystals from the set-II subject to reverse biasing.

| Biasing time | Emission peak peak (nm) | ave (ns) at 529 nm | Fitted decay time components |
| --- | --- | --- | --- |
| None-biased | 530 | 62.2 | τ1: 22.92 ns (B1: 32.05 %) τ2: 80.75 ns (B2: 67.95%) |
| 5 hours | 532 | 73.77 | τ1: 25 ns (B1: 30.17%) τ2: 95 ns (B2: 69.83%) |
| 10 hours | 535 | 75.38 | τ1: 25.1 ns (B1: 33.79%) τ2: 101.04 ns (B2: 66.21%) |
| 22 hours | 535 | 77.96 | τ1: 22.98 ns (B1: 30.1%) τ2: 101.6 ns (B2: 69.92%) |

Supplementary Figure 5. a, attenuation of 59.5 keV and 122 keV gamma ray by CsPbBr3. 1 mm thick CsPbBr3 can attenuate 91% 59.5 keV and 63% 122 keV gamma ray.b, gamma rays irradiating anode so that holes contribute more to the total induced signal. c, gamma rays irradiating cathode so that electrons contribute more to the total induced signal.

Supplementary Figure 6. Reverse current testing after different forward injection current. Each reverse current shown in b was measured after forward biasing where the forward current increased to certain value as shown in a. The reverse current and forward current were measured alternatively. A larger forward current associated with a longer forward biasing time leads to more charge injection and charge trapping, which results in a larger reverse current peak due to charge de-trapping.

Table S3. PL measurement results of the four CsPbBr3 crystals subject to forward biasing.

| Biasing time | Emission peak peak (nm) | ave (ns) at 532 nm | Fitted decay time components |
| --- | --- | --- | --- |
| None-biased | 532 | 54.0 | τ1: 5.46 ns (B1: 5.29 %) τ2: 28.6 ns (B2: 40.49%) τ3: 77.5 ns (B2: 54.22%) |
| 4 hours | 531 | 58.5 | τ1: 3.9 ns (B1: 3.59%) τ2: 26.8 ns (B2: 37.9%) τ3: 82.2 ns (B2: 58.51%) |
| 8 hours | 533 | 86.7 | τ1: 6.83 ns (B1: 4.75%) τ2: 35.5 ns (B2: 30.86%) τ3: 117.1 ns (B2: 64.4%) |
| 12 hours | 533 | 78.2 | τ1: 5.5 ns (B1: 4.4%) τ2: 31.3 ns (B2: 31.64%) τ3: 106.2 ns (B2: 63.97%) |

A large CsPbBr3 crystal with average PL decay time of ~ 54 ns was broken into four pieces with one served as the non-biased control sample and the remaining three were subjected to forward biasing at 300 V.

Supplementary Figure 7. Schematic structural model of CsPbBr3 showing the presence of an interstitial Br- ion and the positively charged vacancy where the Pb2+ are undercoordinated. In principle, the number of interstitial Br- ions and vacant positively charged sites are equal. On the left, the figure indicates the possible ion migration path under the application of an electric field. The right model represents defect repair through recapturing of the Br- ion by the undercoordinated Pb2+ atom.

Thermal stimulated current (TSC) spectroscopy

For electronic traps using a quasi-equilibrium approach of Bube3, the energy level of the trap ETi is given by the equation (1)

|  | ETi=kTmln⁡(NSvthkTm2βETi) | (1) |
| --- | --- | --- |

where k is the Boltzmann constant, Tm is the TSC peak temperature, N is the effective density of states,S is the capture cross section, vth is the thermal velocity of the carriers, βis the heating rate. The trap energy ETi can be calculated using equation (2) below4, noting that N, the effective density of states, is proportional to T3/2,and vth, the thermal velocity, is proportional to T½

|  | ETi=kTmln⁡(Tm4β) | (2) |
| --- | --- | --- |

The trap concentration NTi can be approximately determined from the collected charge for trap i  (QTi) using equation (3) and (4).

|  | QTi=ITSCidt | (3) |
| --- | --- | --- |
|  | NTi=QTi2μτeAE | (4) |

Here, ITSCiis the collected current for trap i and QTiis the temporal integration of each TSC peak. μ is the carrier mobility, τ the carrier lifetime, e the electron charge, A is the electrode area, and E is the applied electric field. Using equations (2) and (3), the trap depths and capture cross sections for the observed traps were calculated using SIMPA fitting. Potential defects were identified according to reported theoretical calculation results5.

Table S3 shows the SIMPA fitting results for the non-biased and biased CsPbBr3 samples up to 300 K. The total number of traps in the temperature range of 79 K to 300 K is ~ 2×1014 cm-3 and ~5×1012 cm-3 for the non-biased and biased samples, respectively.

Table S3. Individual trap energy and density determined for the CsPbBr3 samples

|  | Tm (K) | ETi (eV) | NTi (1011 cm-3) | Possible defects |
| --- | --- | --- | --- | --- |
| Non-biased CsPbBr3 | 79.68 | 0.14 | 98 | [CsPb]−, [VPb]2− |
|  | 93.01 − 102.10 | 0.16 − 0.19 | 113 | [VCs]− |
|  | 111.32 − 143.51 | 0.21 − 0.28 | 316 | [Pbi]+ |
|  | 154.74 − 181.5 | 0.31 − 0.37 | 250 | [Pbi]2+ |
|  | 190.37 − 243.94 | 0.39 − 0.52 | 385 | [PbBr]2+ |
|  | 253.86 | 0.55 | 230 | [PbBr]3+ |
|  | 270.30 − 286.00 | 0.59 − 0.63 | 218 | [PbBr]3+ |
|  | 288.51 − 299.11 | 0.63 − 0.66 | 485 | [PbBr]3+ |
| CsPbBr3 biased for 36 hours | 82.19 − 83.93 | 0.14 − 0.15 | 1.51 | [CsPb]−, [VPb]2− |
|  | 89.28 − 105.05 | 0.16 − 0.19 | 5.54 | [VCs]− |
|  | 111.69 − 176.25 | 0.21 − 0.36 | 19.10 | [Pbi]+ |
|  | 182.76 − 184.07 | 0.37 | 2.72 | [Pbi]2+ |
|  | 191.09 − 238.21 | 0.39 − 0.51 | 13.90 | [PbBr]2+ |
|  | 248.06 − 262.94 | 0.53 − 0.57 | 4.60 | [PbBr]3+ |
|  | 269.27 − 282.02 | 0.59 − 0.62 | 3.49 | [PbBr]3+ |
|  | 290.83 − 302.46 | 0.64 − 0.67 | 3.35 | [PbBr]3+ |

References

1	He, Y. et al. High spectral resolution of gamma-rays at room temperature by perovskite CsPbBr3 single crystals. Nat Commun9, 1609 (2018).

2	Pan, L. et al. Perovskite CsPbBr3 single-crystal detector operating at 1010 photons/s/mm2 for ultra-high flux X-ray detection.  (2022).

3	Bube, R. H. Photoconductivity of solids.  (RE Krieger Pub. Co., 1978).

4	Fang, Z., Shan, L., Schlesinger, T. & Milnes, A. Study of defects in LEC-grown undoped SI-GaAs by thermally stimulated current spectroscopy. Materials Science and Engineering: B5, 397-408 (1990).

5	Zhang, M. et al. Determination of defect levels in melt-grown all-inorganic perovskite CsPbBr3 crystals by thermally stimulated current spectra. The Journal of Physical Chemistry C122, 10309-10315 (2018).