Supplementary Information

Exciton-Harvesting Enabled Efficient Charged Particle Detection in Zero-Dimensional Halides

Qian Wang1†, Chenger Wang2,3†, Hongliang Shi4†, Jie Chen2,5, Junye Yang2,5, Alena Beitlerova6, Romana Kucerkova6, Zhengyang Zhou1, Yunyun Li1, Martin Nikl6, Xilei Sun2,*, Xiaoping OuYang7,*, and Yuntao Wu1,*

1Shanghai Institute of Ceramics, Chinese Academy of Sciences, Shanghai, 201899, China.

2Institute of High Energy Physics, Chinese Academy of Sciences, Beijing, 100049, China.

3National Engineering Research Center for Rare Earth, Grirem Advanced Materials Co., Ltd. and General Research Institute for Nonferrous Metals; Beijing, 100088, China.

4Department of Physics, Beihang University; Beijing, 100191, China.

5Spallation Neutron Source Science Center, Dongguan 523803, China

6Department of Optical Materials, Institute of Physics of the Czech Academy of Sciences; Prague, 16200, Czech Republic.

7Northwest Institute of Nuclear Technology; Xi’an, 710024, China.

†These authors contributed equally to this work.

*Correspondence author. Email: sunxl@ihep.ac.cn (X. Sun), oyxp2003@aliyun.com (X. OuYang), ytwu@mail.sic.ac.cn (Y. Wu)

Difference between theoretical and measured light yield

The light yields and photoluminescence quantum yields (PLQYs) of low-dimensional copper-based halide scintillators are listed by statistics. The theoretical light yields are estimated according the reported band gap values by Bartram–Lempicki model1:

LR=S*Qβ*Eg#1

where S and Q are the transport/transfer efficiency of the e–h pair energy to the emission centers and the internal quantum efficiency in emission centers, respectively. Here, the values are set as 1. β is 1.5–1.8 for ionic halide compounds and the approximate mean is used as 1.65.

Figure S1. Light yields (a) and PLQYs (b) of low-dimensional copper-based halide scintillators.2, 3, 4, 5, 6, 7, 8, 9, 10, 11, 12, 13, 14

Crystallographic property

The differential scanning calorimetry (DSC) measurement was conducted by using a Netzsch STA449F3 instrument. About 50 mg single crystal was loaded in an Al2O3 crucible, and heated to 450 °C at a rate of 5 °C/min under ultra-high purity argon atmosphere.

Figure S2. DSC profiles of Cs3Cu2I5 and Cs3Cu2I5:Tl in Ar atmosphere.

There is no additional thermal effect induced by Tl doping. The Cs3Cu2I5 shows a pair of exothermic and endothermic peaks at 396 °C and 329 °C corresponding to the melting point (Tm) and crystallization point (Tc). Compared with undoped Cs3Cu2I5, the Tm and Tc decrease slightly in Cs3Cu2I5:Tl. It is worthwhile to note that for both the undoped and Tl-doped Cs3Cu2I5, the thermal supercooling, which causes spontaneous nucleation in the melt into multiple grains, is severe due to a large temperature difference between Tm and Tc, e.g. 67 °C for Cs3Cu2I5 and 70 °C for Cs3Cu2I5:Tl. Moreover, there is an additional exothermic peak at the lower temperature side of the main melting peak. It can be interpreted as the second phase precipitated due to the incongruent melting of Cs3Cu2I5.15 The CsI phase precipitated first (389°C, L0.60CsI+0.40CuI→CsI+L) during the temperature decrease. When the ratio of CsI in the melt is reduced to 0.59, the crystallization process is transformed and the Cs3Cu2I5 main phase is precipitated (329°C, L0.59CsI+0.41CuI→Cs3Cu2I5).

Temperature-dependent in-situ synchrotron powder X-ray diffraction (PXRD) measurements were conducted by using a PANalytical X'Pert diffractometer using Cu Kα radiation. The crystal lattice parameters at different temperatures were calculated by Le bail fitting of PXRD patterns through Jana2006.

Figure S3. a, b, Temperature-dependent in-situ PXRD patterns of Cs3Cu2I5 (a) and Cs3Cu2I5:Tl (b) . c, Crystallographic evolution of thermal expansion coefficients as a function of temperature.

The in-situ PXRD measurements from room temperature to 300 °C were conducted. The XRD patterns as a function of temperature are shown in Fig. S3a and Fig. S3b. The XRD peaks shift to a lower angle due to the thermal expansion effect, for example for (222) crystallographic plane, the angle shifts from 26.283° to 26.008° for Cs3Cu2I5, and 26.317° to 26.028° for Cs3Cu2I5:Tl. The lattice parameters were calculated at different temperatures via the Le bail fitting, and listed in Table S3-4.

The evolution of thermal lattice expansion coefficients along crystallographic axes as a function of temperature is plotted in Fig. S3c. The thermal expansion behavior in Cs3Cu2I5 and Cs3Cu2I5:Tl is similar. The thermal expansion coefficient along b and c axis is of 4.3×10-6 and 4.8×10-6 /°C, respectively, which is about 25% smaller than that along a axis ranging from 6.0×10-6 /°C to 6.5×10-6 /°C. It indicates rather weak thermal expansion anisotropy in both Cs3Cu2I5 and Cs3Cu2I5:Tl, comparing with the LaBr3:Ce that is apt to crack due to a large difference in thermal expansion coefficient along crystallographic axis (28.1×10-6 /°C along a axis and 7.5×10-6 /°C along c axis).16

Table S1. Lattice parameters of Cs3Cu2I5 at different temperatures.

| Temperature (°C) | a (Å) | b (Å) | c (Å) | Pnma α = β= γ= 90° |
| --- | --- | --- | --- | --- |
| 25 | 10.17475 | 11.65392 | 14.36231 |  |
| 80 | 10.20575 | 11.68294 | 14.39435 |  |
| 130 | 10.23617 | 11.71024 | 14.42502 |  |
| 180 | 10.26926 | 11.73768 | 14.45934 |  |
| 230 | 10.30154 | 11.76704 | 14.49425 |  |
| 280 | 10.33668 | 11.79741 | 14.53136 |  |
| 300 | 10.35036 | 11.80856 | 14.54783 |  |

Table S2. Lattice parameters of Cs3Cu2I5:Tl at different temperatures.

| Temperature (°C) | a (Å) | b (Å) | c (Å) | Pnma α = β= γ= 90° |
| --- | --- | --- | --- | --- |
| 80 | 10.19706 | 11.67873 | 14.38901 |  |
| 130 | 10.22742 | 11.7058 | 14.42072 |  |
| 180 | 10.259 | 11.73227 | 14.45337 |  |
| 230 | 10.29278 | 11.76069 | 14.48828 |  |
| 280 | 10.32767 | 11.79028 | 14.52614 |  |
| 300 | 10.34233 | 11.80279 | 14.54313 |  |

Based on the above analysis results, we stress the importance of ampoule design and crystal growth process. The quartz ampoule with a straight capillary was used to prevent the thermal supercooling effect. A large temperature gradient of 30-40 °C and a slow growth rate of 0.3-0.5 mm/h were adopted to avoid the constitutional supercooling effect.

The raw materials were weighed according to the formula, and loaded into a quartz ampoule with 7 mm inner diameter in an Argon-filled glovebox. The loaded raw materials were heated to 120 °C under vacuum of 10-4 Pa to remove any trace moisture prior to sealing with an oxy-hydrogen torch. The crystals were grown from a randomly oriented seed formed in a quartz ampoule with a capillary at the front. Moreover, to avoid the adverse reactions between the crystal and the surface of quartz ampoule, the ampoule was coated with a durable pyrolytic carbon before use.

The crystal growth was conducted in a home-made multi-ampoule vertical Bridgman furnace. The loaded ampoules were first heated to above the melting point of Cs3Cu2I5 for several hours to fully mix and homogenize the melt. After optimization, the translation rate and temperature gradient are found to be 0.4 mm/h and 2025 °C/cm, respectively. After growth completion, the furnace was cooled to room temperature at 5 °C/h.

Evaluation of crystal quality

The optical transmission spectra from 200 to 800 nm were recorded by the PerkinElmer-Lambda 950 ultraviolet-visible spectrophotometer. Refractive index and extinction coefficient spectra were obtained using a sopra GES-SE ellipsometer.

Figure S4. Optical transmission spectra and the theoretical values of crystal slabs.

The theoretical transmittance (Ts) at different wavelengths was calculated by using the following equation17:

Ts=2ncrystalnairncrystal2+nair2#2

where ncrystal and nair are the refractive index of crystal and air as a function of temperature, respectively. The value of nair is 1.0027. The refractive index at the maximum emission wavelength is 1.90 (445 nm) of Cs3Cu2I5 and 1.92 (505 nm) of Cs3Cu2I5:Tl.

Figure S5. a, b, Refractive indexes (a) and extinction coefficients (b) of Cs3Cu2I5 single crystal. c, d, Refractive indexes (c) and extinction coefficients (d) of Cs3Cu2I5:Tl single crystal.

Rietveld refinement by NPD

Table S3. Crystallographic parameters of Cs3Cu2I5:Tl obtained by NPD data at room temperature.

| Sample | Cs3Cu2I5:Tl |
| --- | --- |
| Temperature | 298 K |
| Crystal system | Orthorhombic |
| Space group | Pnma (No. 62) |
| Unit cell parameters | a= 10.1693(3) Å, α=90° b= 11.6495(3) Å, β=90° c= 14.3572(5) Å, γ=90° |
| Rwp | 11.5% |
| Rp | 8.69% |
| χ2 | 1.30 |

Table S4. Atomic positions of Cs3Cu2I5:Tl from NRD Rietveld refinement.

| Atoms | Sites | x | y | z | occ |
| --- | --- | --- | --- | --- | --- |
| Cs1 | 4c | 0.59156 | 0.25000 | 0.55287 | 1.00 |
| Cs2 | 8d | 0.05377 | 0.98806 | 0.67951 | 0.98(1) |
| Tl | 8d | 0.05377 | 0.98806 | 0.67951 | 0.02(1) |
| Cu1 | 4c | 0.24017 | 0.25000 | 0.37443 | 1.00 |
| Cu2 | 4c | 0.21845 | 0.25000 | 0.55227 | 1.00 |
| I1 | 8d | 0.69170 | 0.55827 | 0.55047 | 1.00 |
| I2 | 4c | 0.15729 | 0.25000 | 0.20011 | 1.00 |
| I3 | 4c | 0.97013 | 0.25000 | 0.50940 | 1.00 |
| I4 | 4c | 0.29978 | 0.25000 | 0.71805 | 1.00 |

Photoluminescence

The PL emission and excitation contour mappings were measured with a Horiba Jobin Yvon Fluorolog-3 spectrofluorometer. With the increase of Tl concentration, the relative intensity of Tl-related emission to STE emission increases clearly. For the Cs3Cu2I5:1%Tl sample, it is almost entirely dominated by Tl-related emission. The variations in luminescent center spectral shapes observed during contour mapping are attributed to the overlapping of spectra and coloring deviation.

Figure S6. a, b, c, d, PL and PLE spectra mapping of Cs3Cu2I5 (a), Cs3Cu2I5: 0.01%Tl (b), Cs3Cu2I5: 0.1%Tl (c), and Cs3Cu2I5:1%Tl (d). e, f, Doping concentration dependent PL decay profiles of STE emission (e, λex = 280 nm, λem = 440 nm) and Tl-related emission (f, λex = 330 nm, λem = 530 nm) at room temperature.

Figure S7. Temperature-dependent PL spectra of Cs3Cu2I5:Tl single crystal under 300 nm (a) and 329 nm (b) excitation below 80 K.

Figure S8. PL decay profile of 410 nm (2.99 eV) emission in Cs3Cu2I5:Tl single crystal at 8 K.

Figure S9. Full width at half maximum (FWHM) of STE emission (445 nm) as a function of temperature. The fitted Huang-Rhys factor (S) and phonon frequency (ℏωphonons) are listed in the figure.

Figure S10. a, PL and PLE spectra of Cs3Cu2I5 at 77 and 300 K. b, PL decay time profile of Cs3Cu2I5 at 77 K

Figure S11. PL decay profile of 445 nm (2.79 eV) emission in Cs3Cu2I5:Tl single crystal at 8 K.

Figure S12. PL-PLE mapping of Cs3Cu2I5:Tl single crystal at 77 K.

Figure S13. Two-peak gaussian fitting of Tl-bound exciton emission spectra from 77 to 220 K.

Figure S14. FWHM of Tl-bound exciton emission (510 nm) as a function of temperature. The fitted Huang-Rhys factor and phonon frequency are listed in the figure.

Figure S15. PL decay profile of emission at 510 nm (a) and emission at 550 nm (b) in Cs3Cu2I5:Tl single crystal at 8 K.

Figure S16. PL decay profile of emission from 490 to 570 nm under 330 nm excitation at 77 K. The upper figure shows the feature of single-exponential fitting. The derived results are shown in the right figure.

Thermoluminescence

Thermoluminescence (TL) glove curve measurement was performed with the custom-made thermoluminescence spectrometer. The samples with 4 mm × 4 mm × 3 mm were irradiated under X-ray (Au target, 50 kV, 75 μA) for 15 min at 77 K. Then the samples were heated from 77 K to 480 K with a heating rate of 0.1 K/s.

Figure S17. a, Schematic diagram of the custom-made TL spectrometer. b, TL glow curves of Cs3Cu2I5 and Cs3Cu2I5:Tl single crystals.

Particle detection and discrimination

Figure S18. Pulse height spectra of Cs3Cu2I5 (a) and Cs3Cu2I5:Tl (b) under 241Am excitation acquired using Hamamatsu a R6233-100 PMT.

Figure S19. Emission spectra under X-ray excitation (a), and pulse height spectra under 241Am and 90Sr excitation (b) of composite detector based on ZnS:Ag and plastic scintillator.

Figure S20. Scintillation decay evolution as a function of Tl concentration. (a, b) Time constants and ratios of the fast and slow components under 241Am excitation. (c, d) Time constants and ratios of the fast and slow components under 90Sr excitation. (e) Averaged scintillation decay constants of Cs3Cu2I5:Tl. (f) Scintillation decay profiles of Cs3Cu2I5:1%Tl under 241Am and 90Sr sources excitation.

Figure S21. PSD scatter plots and spectra of Cs3Cu2I5:0.01%Tl and Cs3Cu2I5:0.1%Tl under the excitation of 241Am and 90Sr sources.

220Rn loading and measurement:

A 232Th diffusion source (1.2×103 Bq) was used to produce 220Rn, which was then loaded into a 70 ml gas-wash bottle using a pump. The bottle loaded with 220Rn was placed upside-down on a Cs3Cu2I5:1%Tl crystal and coupled with a PMT (HZC PHOTONICS XP3240) for testing. The PMT was operated at -700V and the signal was recorded directly with a CAEN DT5751 digitizer for 3 hours. To serve as environmental background testing, an air-filled gas-wash bottle was used when measuring radon. This control setup served to establish a comparative context for evaluating the measured radon values.

Figure S22. Schematic diagram of the preliminary 220Rn measurement system.

As compared to widely used scintillation cells (flask coated by scintillator, such as ZnS:Ag, et al.) and liquid scintillation devices (mixture of an organic solvent and flour, such as PPO-loaded DIN, et al.), the device offers a compact structure and lower usage cost.18, 19, 20 The time gate parameters used for the PSD were the same as the tests conducted under the excitation of 241Am and 90Sr sources.

The environmental test result of a gas wash bottle filled with natural air wherein 23 α events were detected during a sampling time of 3 hours, indicating the presence of α emitters in the air, building, or bottle material. The extra α events detected clearly originated from the 220Rn samples loaded into the bottle.

Comparation of α/β discrimination scintillators

Table S5. The physical and scintillation properties of 0D Cs3Cu2I5:Tl single crystal, conventional, and some newly developed solid scintillators for α/β discrimination application.

| Scintillators | Cs3Cu2I5:Tl single crystal | ZnS:Ag composition | CsI:Na single crystal | Plastic scintillator |
| --- | --- | --- | --- | --- |
| Density (g/cm3) | 4.5 | 4.1, ~1 | 4.5 | ~1 |
| Zeff | 52.2 | N/A | 54 | ＜10 |
| Light yield at 662 keV (ph./MeV) | 83 000 | N/A | 41 000 | ~10 000 |
| Energy resolution at 662 keV (%) | 3.3 | N/A | 6.7 | N/A |
| PSD FoM | 2.64 | 1.92 | 3.0 (α/γ) | ~1 |
| Stability | Stable | Sensitive to temperature | Sensitive to humidity | Sensitive to temperature |
| Compact | √ | × | √ | √ |
|  | This work | Ref.2121 | Ref.2222 | Ref.2323 |

Supplementary Reference

1.	Ronda, C.R., Srivastava, A.M. Scintillators. In: Ronda, CR (ed). Luminescence: From Theory to Applications, 2007, pp 105-132.

2.	Zhang, F., et al. Blue–violet emitting K2CuCl3 compound: facile synthesis, photoluminescence and radioluminescence properties. J Mater Sci, 57: 10260-10270 (2022).

3.	Gao, W., et al. One-dimensional all-inorganic K2CuBr3 with violet emission as efficient X-ray scintillators. ACS Applied Electronic Materials, 2: 2242-2249 (2020).

4.	Zhao, X., et al. All-inorganic copper halide as a stable and self-absorption-free X-ray scintillator. J Phys Chem Lett, 11: 1873-1880 (2020).

5.	Cheng, S., et al. Non-hygroscopic, self-Absorption free, and efficient 1D CsCu2I3 perovskite single crystal for radiation detection. ACS Appl Mater Interfaces, 13: 12198-12202 (2021).

6.	Ma, Z., et al. Stable yellow light-emitting devices based on ternary copper halides with broadband emissive self-trapped excitons. ACS Nano, 14: 4475-4486 (2020).

7.	Niu, X., et al. Highly efficient blue emissive copper halide Cs5Cu3Cl6I2 scintillators for X-ray detection and imaging. Ceram Int, 48: 30788-30796 (2022).

8.	Li, J., et al. A highly efficient and stable blue-emitting Cs5Cu3Cl6I2 with a 1D chain structure. Adv Mater, 32: e2002945 (2020).

9.	Lian, L., et al. Highly luminescent zero-dimensional organic copper halides for X-ray scintillation. J Phys Chem Lett, 12: 6919-6926 (2021).

10.	Zhou, Q., et al. Highly efficient copper halide scintillators for high-performance and dynamic X-ray imaging. Nanoscale, 13: 19894-19902 (2021).

11.	Cheng, S., et al. Zero-dimensional Cs3Cu2I5 perovskite single crystal as sensitive X-ray and γ-ray scintillator. Phys Status Solidi Rapid Res Lett, 14: 2000374 (2020).

12.	Cheng, S., et al. Ultrabright and highly efficient all‐inorganic zero‐dimensional perovskite scintillators. Adv Opt Mater, 9: 2100460 (2021).

13.	Han, K., Jin, J., Su, B., Qiao, J., Xia, Z. Promoting single channel photon emission in copper(I) halide clusters for X-Ray detection. Adv Opt Mater, 10: 2200865 (2022).

14.	Xu, T., et al. Lead-free zero-dimensional organic-copper(I) halides as stable and sensitive X-ray scintillators. ACS Appl Mater Interfaces, 14: 14157-14164 (2022).

15.	Wojakowska, A., Górniak, A., Kuznetsov, A.Y., Wojakowski, A., Josiak, J. Phase Diagram of the System Copper(I) Iodide + Cesium Iodide. Journal of Chemical & Engineering Data, 48: 468-471 (2003).

16.	Doty, F.P., et al. Structure and properties of lanthanide halides.  Penetrating Radiation Systems and Applications VIII; 2007.

17.	Mao, R., Zhang, L., Zhu, R.-Y. Optical and scintillation properties of inorganic scintillators in high energy physics. IEEE Trans Nucl Sci, 55: 2425-2431 (2008).

18.	Li, J., et al. Novel liquid scintillator radon detector. Radiation Detection Technology and Methods, 6: 294-301 (2022).

19.	Feng, X.-g., He, Q.-g., Wang, J.-c., Chen, J. A general method for optimizing the parameter of α/β discrimination in liquid scintillation counting. Anal Methods, 6: 115-119 (2014).

20.	Abdalla, A.M., et al. Radon detection using alpha scintillation KACST cell. Nucl Instrum Methods Phys Res A, 922: 84-90 (2019).

21.	Ifergan, Y., et al. Development of a thin, double-sided alpha/beta detector for surface-contamination measurement. IEEE Trans Nucl Sci, 63: 634-638 (2016).

22.	Winyard, R.A., Lutkin, J.E., McBeth, G.W. Pulse shape discrimination in inorganic and organic scintillators. I. Nucl Instrum Methods, 95: 141-153 (1971).

23.	Morishita, Y., Di Fulvio, A., Clarke, S.D., Kearfott, K.J., Pozzi, S.A. Organic scintillator-based alpha/beta detector for radiological decontamination. Nucl Instrum Methods Phys Res A, 935: 207-213 (2019).