Supplementary Materials

Anchoring MoS2 microflowers on oxygen-doped g-C3N4 porous nanosheets

to construct Z-Scheme hybrid composites for efficient photocatalytic hydrogen production

Tiekun Jia1, *, Zhao Deng2, Dongsheng Yu1, Fang Fu1, Qian Zhang3, Yinao Wang3, Ji Hu1, Jili Li1,

Joong Hee Lee4

1. Henan Province International Joint Laboratory of Materials for Solar Energy Conversion and Lithium Sodium based Battery & School of Materials Science and Engineering, Luoyang Institute of Science and Technology, Luoyang, 471023, P. R. China.

2. State Key Lab of Materials Synthesis and Processing, Wuhan University of Technology, Wuhan, 430070, P. R. China.

3. School of Materials Science and Engineering, Guilin University of Technology, Guilin 541004, P. R. China.

4. Department of Nano Convergence Engineering, Jeonbuk National University, Jeonju 54896, Korea; jhl@jbnu.ac.kr

Corresponding author: Tiekun Jia; Email: tiekunjia@126.com

2. Experimental details

2.6 Characterization

The X-ray diffraction (XRD) patterns of the samples were recorded on a Bruker D8 advance diffractionmeter with Cu Kα radiation at room temperature. The scanning electron microscopy (SEM) images were obtained on a Hitachi S-4800 electron microscope. Transmission electron microscopy (TEM) and high-angle annular dark-field scanning transmission electron microscopy (HAADF-STEM) observations were carried out on a FEI Talos F200S transmission electron microscope. X-ray spectroscopy (EDS) elemental maps were employed with an EDX system connected to the TEM instrument. X-ray photoelectron spectroscopy (XPS) was conducted on an ESCALAB 250 Xi spectrometer. UV-visible diffuse reflectance spectra (DRS) were obtained on a TU-1901 UV-Vis spectrometer. Electron paramagnetic resonance (EPR) spectra were recorded on a Bruker MEX-nano spectrometer.

2.7 Photoelectrochemical measurements

The photoelectrochemical performance of the samples was performed on an electrochemical workstation (CHI 660E) in a three-electrode cell with the Na2SO4 aqueous solution (0.5 mol·L-1, pH=6.8) as the electrolyte. The catalyst was deposited on FTO as the working electrode, while Ag/AgCl electrode and Pt foil were employed as the reference electrode and the counter electrode, respectively. Transient photocurrent measurements were accomplished by visible-light on and off alternately every 50s. Electrochemical impedance spectroscopy (EIS) was measured in the frequency range of 105Hz to 0.1Hz with amplitude of 10mV. Mott-Schottky (M-S) plots were measured with frequency of 500, 1000 and 2000Hz in the dark, respectively.

Figure S1 XRD patterns of the as-prepared O-CNS/xMoS2 photocatalysts (x=0.5, 1, 3, 5, 7, 9)

Figure S2 VB XPS analysis of MoS2

Table S1 Comparison of hydrogen evolution of g-C3N4-based photocatalysts

| Samples | Light source | Reactant solution | Hydrogen evolution (μmol h-1 g-1) | Reference |
| --- | --- | --- | --- | --- |
| VPP0.3-CN | 300W Xe Lamp (λ=400 nm) | 100 mL containing 10 vol % TEOA, 3% Pt | 2316.2 | [1] |
| 5-CN/Au/BiVO4 | 300W Xe Lamp (λ> 420 nm) | 90 mL water+ 10 mL TEOA, methanol, 0.5 % Au, | 2986 | [2] |
| Er:WO3/CdS/g-C3N4 QDs | 300W Xe Lamp (λ≥ 400 nm) | 80ml Na2S and Na2SO3 | 1912.12 | [3] |
| g-C3N4/Ag/ZnO | Visible light 30KHz, 80 W | 50 mL water+ Methanol 10 % | 1637.5 | [4] |
| CdS/(Pt/g-C3N4) | 300 W Xe Lamp (λ> 420 nm) | 100 mL water+ 10% TEOA, | 1465.9 | [5] |
| Pt0.5-Au1.5/CN | 300W Xe Lamp (350<λ<580nm) | 90 mL water+ 0.9g Glucose, Certain amounts HAuCl4 and H2PtCl6 | 3180 | [6] |
| 3Pt/SCN | LED solar simulator (400 - 1100 nm) | 90 mL water+ 10 mL TEOA, 3% Pt | 1255.52 | [7] |
| N doped g-C3N5/TiO2 | Natural light 1358.8 W | 50 mL water+ 10% TEOA, 3% Pt | 3515.1 | [8] |
| Cu-Ni(OH)2-C3N4 | 300 W Xe lamp (AM 1.5G) | 90 mL water+ 10ml TEOA, 1% Cu and Ni | 2037.3 | [9] |
| UiO-66-D@g-C3N4/Ni (2.0 %) | 420W Xe Lamp (λ> 420 nm) | 20 mL water+ 10% TEOA and Eosin Y (EY) | 2621 | [10] |
| Pt1-HCN (0.38%) -125 | 300W Xe Lamp (AM 1.5 G) | 50 mL water+ 20% TEOA, 0.38% Pt | 2900 | [11] |
| Oxygen-doped g-C3N4 sheets | 300 W Xenon lamp (λ > 420 nm) | 100 mL aqueous solution containing 10 vol% TEOA, 3% Pt | 2200 | [12] |
| 5%MoS2/O-CNS | 300 W Xenon lamp (λ > 420 nm) | 100 mL aqueous solution containing 10 vol% TEOA, 3% Pt | 4570.7 | This study |

[1] Pan L, Wu G, Wang X, Liu R, Yan B, Zhu X, Mo Z, Sun P, Miao Z, Xu H, (2024) Promotion of intramolecular electron transfer in g-C3N4 tubes by introducing pyridine structure to accelerate photocatalytic hydrogen evolution. Colloids Surf 681: 133261. https://doi.org/10.1016/ j.colsurfa.2024.133261

[2] Muthukumar R, Balaji G, Vadivel S (2023) The charge transfer pathway of g-C3N4 decorated Au/Bi(VO4) composites for highly efficient photocatalytic hydrogen evolution. Int J Hydrog Energy 48: 23856-23865. https://doi.org/10.1016/j.ijhydene. 2023.03.152

[3] Hui Li, Xinyan Li, Lixin Que, Xiaoqing Xu, Jun Cao, Jiaqi Pan, Mei Zhu (2024) S-scheme core-shell nanorods heterojunction of g-CN quantum dots modified Er:WO/CdS towards visible light H evolution via up-conversion fluorescence synergism, Int J of Hydrogen Energ 51:1440-1450. https://doi.org/10.1016/j.ijhydene.2023.11.132

[4] PavanP. Gotipamul, Sondos AbdullahAlqarni , Saravanan Pandiaraj, Maheswaran Rathinam, Siva Chidambaram（2024）Initiation of piezoelectricity expands the photocatalytic H2 production and decomposition of organic dye through g-C3N4/Ag/ZnO tri-components, Mater Sci Energ Techn 7:133-147. https://doi.org/10.1016/j.mset.2023.09.001

[5] Hu W, Zhang J, Tian J, Dang Y, Wang W, Zhan H, Ma B (2022) Greatly enhanced photocatalytic hydrogen production on CdS/(Pt/g-C3N4) via dual functions of Pt on semiconductors interface. Int J Hydrogen Energ 68: 29295-29304. https://doi.org/ 10.1016/j.ijhydene.2022.06.250

[6] Ding F, Yu H, Liu W, Zeng X, Li S, Chen L, Li B, Guo J, Wu C (2024) Au-Pt heterostructure cocatalysts on g-C3N4 for enhanced H2 evolution from photocatalytic glucose reforming. Mater Des 238: 112678. https://doi.org/10.1016/j.matdes.2024. 112678

[7] Nguyen P, Dao Q, Dang T, Hoang T, Chung J, Shin E (2023) Highly dispersed PtO over g-C3N4 by specific metal-support interactions and optimally distributed Pt species to enhance hydrogen evolution rate of Pt/g-C3N4 photocatalysts. Chem Eng J 15:142765. https://doi.org/10.1016/j.cej.2023.142765

[8] Kamalakannan S, Balasubramaniyan N, Bernaurdshaw N,  Vattikondala G (2023)  Impact of nitrogen doping on triazole-based graphitic carbon Nitride-TiO2 (P25) S-scheme heterojunction for improved photocatalytic hydrogen production. Nanoscale Adv 5(21): 5907-5922. https://doi.org/10.1039/d3na00597f

[9] Zhan D, Tian J, Fu Q, Liu P, Zhao Y, Liu W, Li D, Huang Y , Han C (2023) In situ photodeposition of Cu and Ni(OH)2 dual cocatalyst: Synergistic effect on enhancing g-C3N4 photocatalytic H2 evolution. Appl Surf Sci 641:158463. https://doi.org/10.1016/j.apsusc.2023. 158463

[10] Jamma A, Jaksani B, Vennapoosa S, Gonuguntla S, Sk S, Ahmadipour M, Moses Abraham B M, Mondal I, Pal U (2024) Defect-rich UiO-66@g-C3N4/Ni frameworks as efficient water splitting photocatalysts. RSC Mater Adv In press, https://doi.org/10. 1039/d3ma00880k

[11] Mahvelati-Shamsabadi T, Bhamu K, Lee S, Dang T, Khoi V, Hur S, Choi W, Kang S, Shin T,  Chung J (2023) Coordinatively unsaturated atomically dispersed Pt+2-N4 sites on hexagonal nanosheet structure of g-C3N4 for high-performance photocatalytic H2 production. Appl. Catal. B Environ 337: 122959. https://doi.org /10.1016/j.apcatb.2023.122959

[12] Tang H, Xia Z, Chen R, Liu Q, Zhou T (2020) Oxygen doped g-C3N4 with nitrogen vacancy for enhanced photocatalytic hydrogen evolution. Chem-Asian J 15(21): 3456-3461. https://doi.org /10.1002/asia.202000912