Rheological properties of microfibrillated cellulose and hydroxypropyl methylcellulose blends in ethanol/water solvent systems

Egon Petersohn Juniora*, Angelo Cezar Lucizania, Victor Veríssimoa, Cassiano Piresb, Alan Sulato de Andradec, Mailson de Matosd, Gisele Perissuttie, Washington Luiz Esteves Magalhaesa e, Rilton Alves de Freitasb.

Contact information: a: Integrated Program in Engineering & Materials Science, Federal University of Paraná, Polytechnic Center, Curitiba, 81531‑990, Brazil; b: Biopol, Pharmacy Department, Federal University of Paraná, 80210-170, Curitiba, PR, Brazil; c: Department of Forest Engineering and Technology, Federal University of Paraná, Curitiba, PR, 80210-170, Brazil; d: SENAI Institute of Innovation in Electrochemistry, Curitiba, Paraná, Brazil; e: Embrapa Florestas, Estrada da Ribeira, Km 111, Colombo, 83411‑000, Brazil *Corresponding author: egondickens@gmail.com

Supplementary Information (SI)

Fig. SI-1 Oscillatory frequency sweep, performed in a linear viscoelastic range at constant temperature 25 °C. Figures A-C storage modulus G’ (solid symbols), and loss modulus G’’ (open symbols). A – storage modulus and loss modulus for different MFC concentrations in 50 wt% ethanol. B - storage modulus and loss modulus for different HPMC concentrations in 50 wt% ethanol. C - storage modulus and loss modulus for different MFC/HPMC concentrations in 50 % w/w ethanol.

Fig. SI-2 Oscillatory frequency sweep, performed in a linear viscoelastic range at constant temperature 25 °C.Storage modulus (solid), loss modulus (open) and tan δ (half up) for MFC and MFC/HPMC dispersions in 0.0 wt% ethanol.

Fig. SI-3 Flow curves of polymers-ethanol/water mixtures. A – Effect of ethanol on viscosity MFC dispersions. B – Flow curve for dispersions in different MFC concentrations. C - Effect of ethanol on viscosity HPMC dispersions. D – Flow curve for dispersions in different HPMC concentrations. E - Effect of ethanol on viscosity MFC/HPMC dispersions. F - Flow curve for dispersions in different MFC concentrations.

Fig. SI-4 Flow curves of polymers-ethanol/water mixtures with and without urea. A – Effect of urea on viscosity for MFC/HPMC dispersions at ethanol 0.0 %. B – Effect of urea on viscosity for MFC/HPMC dispersions at ethanol 25 %. C - Effect of urea on viscosity for MFC dispersions at ethanol 0.0 %. D – Effect of urea on viscosity for MFC dispersions at ethanol 25 %.

Table SI-1. Flow curves regression parameters using a Hershel-Buckley model for the samples MFC, HPMC and MFC/HPMC.

| Polymer | EtOH (%) | τ0 (Pa) | K (Pa·s) | n | R² |
| --- | --- | --- | --- | --- | --- |
| MFC 1.0 % | 0.0 | 0.000 | 1.779 | 0.403 | 0.998 |
|  | 25 | 0.000 | 2.062 | 0.495 | 0.983 |
|  | 50 | 0.000 | 1.711 | 0.542 | 0.965 |
|  | 70 | 0.000 | 1.814 | 0.543 | 0.992 |
|  | 80 | 3.499 | 0.004 | 1.990 | 0.975 |
| HPMC 0.4 % | 0.0 | -0.007 | 0.047 | 0.915 | 1.000 |
|  | 25 | -0.059 | 0.114 | 0.840 | 0.999 |
|  | 50 | 0.154 | 0.085 | 0.908 | 0.996 |
|  | 70 | 0.015 | 0.058 | 0.903 | 0.999 |
|  | 80 | -0.226 | 0.440 | 0.723 | 1.000 |
| MFC+HPMC 1.0 %/0.4 % | 0.0 | 2.397 | 4.915 | 0.307 | 0.998 |
|  | 25 | 4.355 | 3.672 | 0.420 | 0.999 |
|  | 50 | 2.779 | 5.320 | 0.366 | 1.000 |
|  | 70 | 3.951 | 2.536 | 0.449 | 1.000 |
|  | 80 | 10.125 | 0.103 | 1.039 | 0.987 |

HPMC: hydroxypropylmethylcellulose; MFC: microfibrillated celulose; MFC+HPMC: microfibrillated cellulose + hydroxypropylmethylcellulose; τ0: yield stress; K: flow consistence index; n: flow index.

Table SI-2. Hysteresis loop area obtained for the samples HPMC, MFC and MFC + HPMC.

| Polymer | EtOH (%) | Hysteresis at low ẏ (Pa·s-1) | Hysteresis at medium ẏ (Pa·s-1) | Hysteresis at high ẏ (Pa·s-1) | Hysteresis (Pa·s-1) | Relative Hysteresis (%) |
| --- | --- | --- | --- | --- | --- | --- |
| MFC 1.0 % | 0 |  | - | - | 33,02 | 5,32 |
|  | 25 | 12,43 | -4,40 | 15,81 | 23,84 | 2,39 |
|  | 50 | 4,38 | -15,66 | 10,68 | -0,61 | -0,06 |
|  | 70 | 17,44 | -10,89 | - | 6,54 | 0,62 |
|  | 80 | 21,44 | -183,06 | - | -161,62 | -15,86 |
| HPMC 0.4 % | 0 | - | - | - | 1,64 | 1,45 |
|  | 25 | - | - | - | 1,59 | 0,79 |
|  | 50 | - | - | - | 1,39 | 0,66 |
|  | 70 | - | - | - | 0,66 | 0,50 |
|  | 80 | - | -20,94 | - | -20,94 | -4,31 |
| MFC + HPMC 1.0 %/0.4 % | 0 | - | - | - | 64,30 | 4,69 |
|  | 25 | - | - | - | 25,51 | 1,51 |
|  | 50 | - | - | - | 20,00 | 1,11 |
|  | 70 | - | - | - | 17,34 | 1,29 |
|  | 80 | - | - | - | 15,24 | 1,25 |

ẏ: shear rate;  Hysteresis at low ẏ: 1-<10 1/s; Hysteresis at medium ẏ: <10-23 1/s; Hysteresis at high ẏ: 23-100 1/s.