Table 1 Characteristics of chitosan extracted from shrimp shell

Characteristics Expected value *Found values

Degree of deacetylation (%) 70 -95 83.9 ± 1.2 Molar Mass (kDa) 100 -200 161.5 ± 3.4 Moisture content (% wet basis) until 10.0 9.3 ± 0.2

Table 2 Average values for thickness of CS and CS/CNTs adsorbent films

Films Thickness (mm)

CS 0.147 ± 0.023a CS/CNT0.1% 0.150 ± 0.026a CS/CNT0.3% 0.155 ± 0.021a CS/CNT0.5% 0.158 ± 0.019a

Values are the mean and standard deviation (n=3). The values referenced in the column by the same letters are not significantly different (p>0.05), according to the Tukey test.

Table 3 Color attributes for adsorbent films

Films Color attributes L* a* b * Hab (°)

CS 81.7 ± 0.3a 3.4 ± 0.6a 26.5 ± 0.3a 82.7 ±0.5a CS/CNT0.1% 66.0 ± 0.1b 3.1 ± 0.3b 14.6 ±0.2b 78.0 ± 0.4b CS/CNT0.3% 57.4 ± 0.1c 2.0 ± 0.1c 7.0 ± 0.2c 74.0 ±0.2c CS/CNT0.5% 49.2 ± 0.1d 1.8 ± 020d 5.0 ± 0.2d 70.0 ±0.1d

Values are the mean and standard deviation (n=3). L* (brightness), a* and b* (chromaticities) and Hab angle (°Hue). Values referenced by different letters in the same column are significantly different (p≤0.05).

Table 4 Mechanical properties for adsorbent devices: chitosan films (CS) and films based on chitosan/carbon nanotubes (CS/CNTs)

Films Tensile strength (MPa) Elongation (%)

CS 23.9 ± 0.5a 13.9 ± 0.2b CS/CNT0.1% 4.0 ± 0.9b 31.8 ± 0.2a CS/CNT0.3% 4.6 ± 0.9b 29.9 ± 0.1a CS/CNT0.5% 4.9 ± 0.9b 29.3 ± 0.1a

Calculated the mean and standard deviation (n=3). Values referenced by different letters in the same column are significantly different (p≤0.05).