Novel Hing gum-based adsorbent with optimized synthesis parameters for cationic dye removal

Samiksha Gautam, Vijay Kumar*

Department of Physics, National Institute of Technology Srinagar, Jammu and Kashmir-190006, India

Corresponding author: vj.physics@gmail.com (V. Kumar)

Supplementary Data

Figure S1: Schematic representation of the synthesis process of the HG-based hydrogel.

Figure S2(a):  Plausible mechanism for the initiation of the synthesis of HG-cl-poly(AAm).

Figure S2(b):  Plausible mechanism for the propagation of the synthesis of HG-cl-poly(AAm).

Figure S2(c):  Plausible mechanism for the propagation of the synthesis of HG-cl-poly(AAm).

Figure S3: Possible interactions between MG dye and HG-g-poly(AAm).

Table S1: Experimental design with experimental values of %age swelling.

| Std | Run | Factor 1 | Factor 2 | Factor 3 | Factor 4 | Factor 5 | Response |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | A: Initiator 10-2 Mol/L | B: Monomer 10-1 Mol/L | C: Crosslinker 10-2 Mol/L | D: Solvent mL | E: Time sec | Swelling % |
| 12 | 1 | 3.03 | 8.67 | 3.99 | 8 | 80 | 582 |
| 3 | 2 | 2.35 | 4.32 | 3.99 | 8 | 60 | 491 |
| 15 | 3 | 2.35 | 6.49 | 4.98 | 10 | 70 | 658 |
| 7 | 4 | 1.68 | 4.32 | 3.99 | 12 | 80 | 648 |
| 1 | 5 | 3.03 | 8.67 | 5.98 | 8 | 60 | 614 |
| 6 | 6 | 1.68 | 4.32 | 5.98 | 12 | 60 | 652 |
| 14 | 7 | 2.35 | 6.49 | 4.98 | 10 | 70 | 605 |
| 13 | 8 | 2.35 | 6.49 | 4.98 | 10 | 70 | 655 |
| 5 | 9 | 3.03 | 8.67 | 3.99 | 12 | 80 | 785 |
| 2 | 10 | 1.68 | 8.67 | 3.99 | 8 | 80 | 577 |
| 8 | 11 | 3.03 | 4.32 | 5.98 | 12 | 60 | 557 |
| 4 | 12 | 3.03 | 4.32 | 5.98 | 8 | 80 | 476 |
| 11 | 13 | 1.68 | 4.32 | 5.98 | 8 | 60 | 542 |
| 9 | 14 | 1.68 | 8.67 | 5.98 | 12 | 80 | 780 |
| 10 | 15 | 1.68 | 8.67. | 3.99 | 12 | 60 | 788 |

Table S2: ANOVA table and model statistics for linear model.

| Source | Sum of Squares | Degree of Freedom | Mean Square | F-value | p-value |
| --- | --- | --- | --- | --- | --- |
| Model | 1.322E+05 | 5 | 26439.22 | 67.85 | < 0.0001* |
| A-Initiator | 2795.04 | 1 | 2795.04 | 7.17 | 0.0253* |
| B-Monomer | 48133.33 | 1 | 48133.33 | 123.52 | < 0.0001* |
| D-Solvent | 55200.04 | 1 | 55200.04 | 141.65 | < 0.0001* |
| AB | 5017.04 | 1 | 5017.04 | 12.87 | 0.0059* |
| BD | 7526.04 | 1 | 7526.04 | 19.31 | 0.0017* |
| Lack of Fit | 1734.58 | 7 | 247.80 | 0.2796 | 0.9149# |
| Model Statistics |  |  |  |  |  |
| Standard Deviation | 19.74 | R2 | 0.9752 | Standard Deviation | 19.74 |
| Mean | 627.33 | Adjusted R2 | 0.9598 | Mean | 627.33 |
| C.V% | 3.15 | Predicted R2 | 0.9306 | C.V% | 3.15 |
|  |  | Adeq Precision | 25.1433 |  |  |

*Significant at p-value<0.05

# not significant at p-value<0.05

Table S3: Factorial design with %age swelling as response variable.

| Std | Run | Factor 1 | Factor 2 | Factor 3 | Response |
| --- | --- | --- | --- | --- | --- |
|  |  | Initiator 10-2 Mol/L | Monomer 10-1 Mol/L | Solvent mL | Swelling % |
| 2 | 1 | 3.03 | 6.49 | 10 | 652 |
| 10 | 2 | 3.60 | 8.65 | 13 | 681 |
| 14 | 3 | 2.19 | 8.65 | 18.0454 | 506 |
| 18 | 4 | 2.19 | 8.65 | 13 | 638 |
| 9 | 5 | 0.77 | 8.65 | 13 | 547 |
| 4 | 6 | 3.03 | 10.82 | 10 | 631 |
| 12 | 7 | 2.19 | 12.29 | 13 | 682 |
| 3 | 8 | 1.34 | 10.82 | 10 | 672 |
| 13 | 9 | 2.19 | 8.65 | 7.95462 | 642 |
| 6 | 10 | 3.03 | 6.49 | 16 | 425 |
| 15 | 11 | 2.19 | 8.65 | 13 | 635 |
| 1 | 12 | 1.34 | 6.49 | 10 | 611 |
| 5 | 13 | 1.34 | 6.49 | 16 | 314 |
| 16 | 14 | 2.19 | 8.65 | 13 | 701 |
| 8 | 15 | 3.03 | 10.82 | 16 | 712 |
| 11 | 16 | 2.19 | 5.01 | 13 | 397 |
| 17 | 17 | 2.19 | 0.8 | 13 | 624 |
| 7 | 18 | 1.34 | 10.82 | 16 | 629 |
| 20 | 19 | 2.19 | 8.65 | 13 | 760 |
| 19 | 20 | 2.19 | 8.65 | 13 | 721 |

Table S4: ANOVA analysis table and model statistics for fitted linear model.

| Source | Sum of Squares | Degree of Freedom | Mean Square | F-value | p-value |
| --- | --- | --- | --- | --- | --- |
| Model | 2.355E+05 | 9 | 26161.24 | 14.93 | 0.0001* |
| A-Initiator | 12877.27 | 1 | 12877.27 | 7.35 | 0.0219* |
| B-Monomer | 92066.46 | 1 | 92066.46 | 52.56 | < 0.000* |
| D-Solvent | 37404.67 | 1 | 37404.67 | 21.35 | 0.0009* |
| AB | A-Initiator | 1 | 1512.50 | 0.8634 | 0.3747* |
| BD | 4704.50 | 1 | 4704.50 | 2.69 | 0.1323* |
| BC | 39480.50 | 1 | 39480.50 | 22.54 | 0.0008* |
| A2 | 6095.42 | 1 | 6095.42 | 3.48 | 0.0917* |
| B2 | 31707.01 | 1 | 31707.01 | 18.10 | 0.0017* |
| C2 | 17360.66 | 1 | 17360.66 | 9.91 | 0.0104* |
| Lack of Fit | 3002.19 | 5 | 600.44 | 0.2068 | .9457# |
| Model Statistics |  |  |  |  |  |
| Standard Deviation | 41.85 |  | R2 | 0.9308 | Standard Deviation |
| Mean | 608.70 |  | Adjusted R2 | 0.8684 | Mean |
| C.V% | 6.88 |  | Predicted R2 | 0.8251 | C.V% |
|  |  |  | Adeq Precision | 14.0101 |  |

*Significant at p-value<0.05

# non-significant at p-value>0.1000