Supplementary information for

Scalable two-step annealing method for preparing ultra-high-density single-atom catalyst libraries

Xiao Hai1,10, Shibo Xi2,10, Sharon Mitchell3,10, Karim Harrath4,5,10, Haomin Xu1, Dario Faust Akl3, Debin Kong6, Jing Li1, Zejun Li1, Tao Sun1, Huimin Yang1, Yige Cui1, Chenliang Su7, Xiaoxu Zhao8*, Jun Li4,5*, Javier Pérez-Ramírez3* and Jiong Lu1,9*

1Department of Chemistry, National University of Singapore, 3 Science Drive 3, Singapore 117543, Singapore.

2Institute of Chemical and Engineering Sciences, Agency for Science, Technology and Research, Singapore 627833, Singapore.

3Institute for Chemical and Bioengineering, Department of Chemistry and Applied Biosciences, ETH Zurich, Zurich, Switzerland.

4Department of Chemistry, Southern University of Science and Technology, Shenzhen 518055, China.

5Department of Chemistry and Key Laboratory of Organic Optoelectronics & Molecular Engineering of the Ministry of Education, Tsinghua University, Beijing 100084, China.

6CAS Key Laboratory of Nanosystem and Hierarchical Fabrication, CAS Center for Excellence in Nanoscience, National Center for Nanoscience and Technology, Beijing 100190, China.

7SZU-NUS Collaborative Center and International Collaborative Laboratory of 2D Materials for Optoelectronic Science & Technology of Ministry of Education, Engineering Technology Research Center for 2D Materials Information Functional Devices and Systems of Guangdong Province, Institute of Microscale Optoelectronics, Shenzhen University, Shenzhen 518060, China.

8School of Materials Science and Engineering, Nanyang Technological University, Singapore 639798, Singapore.

9Centre for Advanced 2D Materials and Graphene Research Centre, National University of Singapore, Singapore 117546, Singapore.

10These authors contributed equally: Xiao Hai, Shibo Xi, Sharon Mitchell, Karim Harrath.

*E-mails: xiaoxu.zhao@ntu.edu.sg; junli@tsinghua.edu.cn; jpr@chem.ethz.ch; chmluj@nus.edu.sg

Table of Contents

Supplementary Figures 1-16

Supplementary Tables 1-2

Supplementary Fig. 1 |Catalyst synthesis via one-step annealing. a, b, TEM images (a) and XRD patterns (b) of Ni/NC catalysts with different metal loadings prepared by impregnation of NiCl2 followed by conventional one-step annealing. The formation of large Ni nanoparticles is readily detected at a metal loading of 2 wt.%, and the particle size gradually increases with higher Ni content. Reflections corresponding to the metallic phase are evident in samples containing 5 and 10 wt.% Ni. The absence of reflections in 2 wt.% Ni/NC suggests that the metal loading is below the detection limit.

Supplementary Fig. 2 | Characterization of catalyst carriers. Representative TEM images of as-synthesized NC (a), PCN (e) and CeO2 (i). High-resolution TEM images of NC (b), PCN (f) and CeO2 (j). XRD patterns of NC (c), PCN (g) and CeO2 (k). N2 isotherms of NC (d), PCN (h) and CeO2 (l) derived a total surface area of 1724, 172 and 82 m2 g-1, respectively.

Supplementary Fig. 3 | XANES and EXAFS characterization of Pt1/TiO2 and Pt1/Al2O3 UHD-SACs. The Pt L3-edge a, XANES and b, Fourier transformed EXAFS spectra of Pt1/TiO2 and Pt1/Al2O3 are compared with Pt references (Pt foil and PtO2). The intensities of the white line of Pt1/TiO2 and Pt1/Al2O3 are close to PtO2, suggesting that the Pt atoms are positively charged. Besides, the Fourier transformed EXAFS magnitude of Pt1/TiO2 and Pt1/Al2O3 are characterized by only one significant peak around 1.63Å that is close to the location of the Pt-O peak in the PtO2 reference and thus can be ascribed to Pt-O bonding. The absence of a Pt-Pt peak confirms the Pt species are atomically dispersed on TiO2 and Al2O3. The Pt contents are 8.3 wt.% and 6.8 wt.% for TiO2 and Al2O3, respectively.

Supplementary Fig. 4 | Multimetallic UHD-SACs. a, Periodic table showing the accessible metals for multimetallic UHD-SACs shaded orange. STEM image (b), the corresponding EDX spectra (c) of Ni, Pd and Pt in Ni1Pd1Pt1/NC. Scale bars: 100 nm. d, XRD patterns of Ni1Pd1/NC and Ni1Pd1Pt1/NC only show the broad reflection at 20-30° and 40-50° 2θ belonging to amorphous carbon, no metal-related peaks can be observed. The Ni and Pd loadings are measured to be 4.2 and 8.6 wt.%, respectively, for Ni1Pd1/NC sample. The Ni, Pd and Pt loadings for Ni1Pd1Pt1/NC sample were determined as 2.3, 5.1 and 9.8 wt.%, respectively.

Supplementary Fig. 5 | Elemental mapping of UHD-SACs of various metals on NC. STEM image and corresponding EDS maps of various metals on NC, evidencing the uniform dispersion of metals over the NC support. Scale bars: 100 nm.

Supplementary Fig. 6 | STEM analysis of Pt1/PCN and Pt1/CeO2. Enlarged areas of the ADF-STEM images of Pt1/PCN (a) and Pt1/CeO2 (b) line profiles showing the corresponding size of bright dots of approximately 0.2 nm, which coincides well with the atomic size of Pt. Scale bars: 0.5 nm. c, STEM image and corresponding EDS maps of Pt1/CeO2, evidencing the uniform dispersion of O, Ce and Pt over the support.

Supplementary Fig. 7 | Visualization of UHD-SACs. Atomic-resolution ADF-STEM images of a, various metals on PCN support, b, W, Ir and Pt on CeO2. Scale bars: 1 nm.

Supplementary Fig. 8 | Elemental mapping of UHD-SACs of W, Ir and Pt on CeO2. STEM image and corresponding EDS maps of W, Ir and Pt on CeO2, evidencing the uniform dispersion of W, Ir and Pt over the support. Scale bars: a, b, 100 nm; c, 10 nm.

Supplementary Fig. 9 | Elemental mapping of UHD-SACs of various metals on PCN. STEM image and corresponding EDS maps of various metals on PCN, evidencing the uniform dispersion of metals over the support. Scale bars: 100 nm.

Supplementary Fig. 10 | X-ray diffraction and absroption spectroscopy of UHD-SACs of various metals on different carriers. XRD patterns of UHD-SACs of various metals on a, NC, b, PCN and c, CeO2. The XRD patterns of all single-atom catalysts only exhibit reflections from the supports, no metal-related signatures can be observed. Fourier transformed EXAFS spectra of UHD-SACs of various metals on NC (d), PCN (e) and CeO2 (f). The Fourier transformed EXAFS spectra of all single-atom catalysts show the main peak below 2 Å, which can be ascribed to the metal-N/O bonding. No metal-metal bond is detected in any of the samples, confirming the metals are atomically dispersed on the supports.

Supplementary Fig. 11 | Spectroscopy characterization of Pt UHD-SACs. a, Pt L3-edge XANES spectra of Pt1/NC, Pt1/PCN and Pt1/CeO2. b, Pt 4f XPS spectra of Pt1/NC, Pt1/PCN and Pt1/CeO2.

Supplementary Fig. 12 | Production at kilogram scale. Photos of a, UHD Ni1/PCN catalyst synthesized in kilogram scale and b, the corresponding tubular furnace used for the synthesis (80 × 1400 mm tube size). Ni K-edge c, Fourier transformed EXAFS spectra and d, XANES spectra of UHD Ni1/PCN synthesized at gram and kilogram scales, respectively. The Ni loadings are measured to be 21.3 wt.% and 20.8 wt. % for gram and kilogram scales, respectively.

Supplementary Fig. 13 | Structural characterization of NiCl2/NC, NiCl/NC and Ni1/NC. a, Atomic structural representations of NiCl2/NC, NiCl/NC and Ni1/NC. b, XRD patterns showing the disappearance of reflections arising from NiCl2 after the low-temperature annealing process, indicating that most of the metal precursor reacted with the NC support. c, The Ni K-edge XANES spectra of NiCl2/NC, NiCl/NC and Ni1/NC are compared with NiPc reference. d, e, XPS spectra of Ni 2p (d) and Cl 2p (e) of NiCl2/NC, NiCl/NC and Ni1/NC.

Supplementary Fig. 14 | EXAFS fits of NiCl2/NC, NiCl/NC and Ni1/NC in K plot. EXAFS fits for NiCl2/NC, NiCl/NC and Ni1/NC evidence a close match between measured and calculated spectra. The fitted parameters are reported in Supplementary Table 1.

Supplementary Fig. 15 | Additional electrocatalytic data. Chronoamperometric curve of 1.6 wt.% Ni1/NC (a) and 16.3 wt.% Ni1/NC (b) electrodes under bias from -0.45 V to -1.15 V versus RHE in 0.5 M CO2-saturated KHCO3 aqueous solution.

Supplementary Fig. 16 | DFT calculations. DFT calculated binding energy of intermediates on catalysts for CO2 reduction reaction and HER. A key issue for the electrocatalytic CO2RR to CO is the rate of the competing hydrogen evolution reaction (HER), where H+ does not attach to the CO2 but adsorbs on the catalytic site and then forms an H2 molecule. Thus, the decisive factor in the selective reduction of CO2 is the competition between the free energies of *COOH (G*COOH) and *H (G*H) intermediates on each reaction. Our calculations show that G*COOH (1.57 eV) is lower than G*H (1.67 eV). As a result, CO2RR has lower activation energy than HER, consistent with the high CO2RR performance observed experimentally.

Supplementary Table 1 | Optimization of T1 in the synthesis of Ni1/NC using distinct Ni precursors.

| Ni precursors | T1 (°C)a | T2 (°C) | Ni content (wt. %) |
| --- | --- | --- | --- |
| Ni2(CH3COO)2·4H2O | 100 | 550 | 4.2 |
| NiSO4·7H2O | 300 | 550 | 14.4 |
| NiCl2·6H2O | 100 | 550 | 3.6 |
| NiCl2·6H2O | 200 | 550 | 9.2 |
| NiCl2·6H2O | 300 | 550 | 16.3 |

a T1 is selected to be close to the temperature of decomposition of the Ni precursor. If T1 is selected to be higher than the temperature of decomposition then nanoparticle formation is typically observed. If T1 is much lower than the decomposition temperature then this leads to lower metal contents in the resulting SACs.

Supplementary Table 2 | Results of EXAFS fits of NiCl2/NC, NiCl/NC and Ni1/NC.

| Sample | Shell | N | R (Å) | 2 (10-3Å2) | R factor |
| --- | --- | --- | --- | --- | --- |
| NiCl2/NC | Ni-Cl | 6 | 2.39 | 0.0076 | 0.003 |
|  | Ni-Ni | 6 | 3.49 | 0.0145 |  |
| NiCl/NC | Ni-N | 4.8 | 1.97 | 0.0111 | 0.003 |
|  | Ni-Cl | 0.9 | 2.26 | 0.0032 |  |
| Ni1/NC | Ni-N | 4.6 | 1.89 | 0.0066 | 0.013 |

N, coordination number; R, distance between absorber and backscatter atoms; 2, Debye-Waller factor to account for both thermal and structural disorders; R factor indicates the goodness of the fit. The fitted coordination environment of NiCl2/NC, NiCl/NC and Ni1/NC coincides well with the proposed initial, intermediate and final structures. For the initial NiCl2/NC, Ni is coordinated to 6 Cl. For the intermediate NiCl/NC, Ni is coordinated to 4 N and 1 Cl. For the final Ni1/NC, Ni is coordinated to 4 N.