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Table 1. Physicochemical characteristics of the film.
	Characteristic
	Starch Film
	Starch/AgNPs film

	Thickness, mm
	
	

	Density, g/
	
	

	Moisture Content, %
	
	

	Swelling Power, %
	
	

	Solubility, %
	
	


             1 Values are stated as mean ± standard deviation, n = 3 
             2 Values in the same column with the same superscript letters are not significantly different (p 
          < 0.05)























Table 2. Comparison of various methods for the detection of fenobucarb pesticides.

	Detection methods
	Pesticides 
	Detection limit
	References

	Microcapillary sensor
	Fenobucarb

	5 pg/mL
	[52]

	Electrochemical - Screen-printed carbon electrode modified
	
	0.0089 μM
	[53]

	Nano carbon black modified screen-printed electrode
	
	<8.0 × 10−8 mol L−1
	[54]

	Thermal desorption electrospray ionization tandem mass spectrometry
	
	<50 ppb
	[55]

	Liquid crystal biosensor based on whispering gallery mode
	
	0.1 pg/mL
	[56]

	UPLC–MS/MS
	
	0.07–0.16 μg L−1
	[57]

	Disposable electrochemical sensor using nanocomposite-modified screen-printed electrode
	
	1.30 μM
	[58]

	Colorimetric 
	
	8.86 μM
	Present study
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Table 2. Determination of fenobucarb in fruits using citrate capped AgNPs film.
	Sample
	Spiked conc. ()
	Expected conc. ()
	Found conc. ()
	Recovery (%)
	RSD (%)

	Grape
	0
	0
	23.05
	-
	-

	
	0.05
	23.10
	23.48
	101.68
	0.15

	
	5
	28.05
	28.26
	100.78
	1.30

	
	500
	523.05
	520.88
	99.59
	0.08

	Pumpkin
	0
	0
	32.43
	-
	-

	
	0.05
	32.48
	32.33
	99.56
	0.52

	
	5
	37.43
	36.45
	97.40
	0.25

	
	500
	532.43
	535.02
	100.47
	0.01

	Passion fruit
	0
	0
	26.61
	-
	-

	
	0.05
	26.66
	26.84
	100.70
	1.93

	
	5
	31.61
	32.24
	101.99
	0.21

	
	500
	526.61
	523.61
	99.43
	0.01




