LIST OF TABLES

Table 1. Physicochemical characteristics of the film.

Table 2. Comparison of various methods for the detection of fenobucarb pesticides.

Table 2. Determination of fenobucarb in fruits using citrate capped AgNPs film.

Table 1. Physicochemical characteristics of the film.

| Characteristic | Starch Film | Starch/AgNPs film |
| --- | --- | --- |
| Thickness, mm | 0.0167 ± 0.0066a | 0.0279 ± 0.0053b |
| Density, g/cm3 | 0.0267 ± 0.0036a | 0.0443 ± 0.0041b |
| Moisture Content, % | 0.1153 ± 0.0314a | 0.1068 ± 0.0106a |
| Swelling Power, % | 7.3519 ± 1.3488a | 4.5181 ± 0.8228b |
| Solubility, % | 0.1417 ± 0.0082a | 0.0789 ± 0.0225b |

1 Values are stated as mean ± standard deviation, n = 3

2 Values in the same column with the same superscript letters are not significantly different (p

< 0.05)

Table 2. Comparison of various methods for the detection of fenobucarb pesticides.

| Detection methods | Pesticides | Detection limit | References |
| --- | --- | --- | --- |
| Microcapillary sensor | Fenobucarb | 5 pg/mL | [52] |
| Electrochemical - Screen-printed carbon electrode modified |  | 0.0089 μM | [53] |
| Nano carbon black modified screen-printed electrode |  | <8.0 × 10−8 mol L−1 | [54] |
| Thermal desorption electrospray ionization tandem mass spectrometry |  | <50 ppb | [55] |
| Liquid crystal biosensor based on whispering gallery mode |  | 0.1 pg/mL | [56] |
| UPLC–MS/MS |  | 0.07–0.16 μg L−1 | [57] |
| Disposable electrochemical sensor using nanocomposite-modified screen-printed electrode |  | 1.30 μM | [58] |
| Colorimetric |  | 8.86 μM | Present study |

.

Table 2. Determination of fenobucarb in fruits using citrate capped AgNPs film.

| Sample | Spiked conc. (μM) | Expected conc. (μM) | Found conc. (μM) | Recovery (%) | RSD (%) |
| --- | --- | --- | --- | --- | --- |
| Grape | 0 | 0 | 23.05 | - | - |
|  | 0.05 | 23.10 | 23.48 | 101.68 | 0.15 |
|  | 5 | 28.05 | 28.26 | 100.78 | 1.30 |
|  | 500 | 523.05 | 520.88 | 99.59 | 0.08 |
| Pumpkin | 0 | 0 | 32.43 | - | - |
|  | 0.05 | 32.48 | 32.33 | 99.56 | 0.52 |
|  | 5 | 37.43 | 36.45 | 97.40 | 0.25 |
|  | 500 | 532.43 | 535.02 | 100.47 | 0.01 |
| Passion fruit | 0 | 0 | 26.61 | - | - |
|  | 0.05 | 26.66 | 26.84 | 100.70 | 1.93 |
|  | 5 | 31.61 | 32.24 | 101.99 | 0.21 |
|  | 500 | 526.61 | 523.61 | 99.43 | 0.01 |