(b)

(a)

Table 1: Magnification of outer surface of sample (a) POPU, (b) FPOPU-2 phr, (c) FPOPU-4 phr, and (d) FPOPU-8 phr

| (c) | (d) |
| --- | --- |

Table 2: Area under the graph of the amorphous peaks at 2θ = 20° for FPOPU and POPU

| Formulation | Area under the Graph for the Curves at 2θ = 20° | Crystallinity Index |
| --- | --- | --- |
| POPU | 13316.587 | 64.157 |
| FPOPU-2 phr | 6335.352 | 50.316 |
| FPOPU-4 phr | 5565.107 | 45.656 |
| FPOPU-6 phr | 3188.653 | 48.137 |
| FPOPU-8 phr | 3214.173 | 43.247 |
| FPOPU-10 phr | 2523.709 | 42.217 |
| FPOPU-12 phr | 1165.109 | 37.535 |

Table 3: Gel content of FPOPU

| Formulation | Gc (%) |
| --- | --- |
| POPU | 83.495 ± 0.482 |
| FPOPU-2 phr | 82.679 ± 0.402 |
| FPOPU-4 phr | 82.469 ± 0.261 |
| FPOPU-6 phr | 82.095 ± 0.146 |
| FPOPU-8 phr | 80.601 ± 0.431 |
| FPOPU-10 phr | 79.710 ± 1.101 |
| FPOPU-12 phr | 79.045 ± 0.838 |

Table 4: Pencil Hardness grade for POPU and FPOPU (glass)

| Formulation | Result | Index |
| --- | --- | --- |
| POPU |  | 2H |
| FPOPU-2 phr |  | 6H |
| FPOPU-4 phr |  | 6H |
| FPOPU-6 phr |  | 6H |
| FPOPU-8 phr |  | 3H |
| FPOPU-10 phr |  | 3H |
| FPOPU-12 phr |  | 3H |

Table 5: Pencil Hardness grade for POPU and FPOPU (wood )

| Formulation | Result | Index |
| --- | --- | --- |
| POPU |  | 3H |
| FPOPU-2 phr |  | 3H |
| FPOPU-4 phr |  | 3H |
| FPOPU-6 phr |  | 4H |
| FPOPU-8 phr |  | 4H |
| FPOPU-10 phr |  | 4H |
| FPOPU-12 phr |  | 4H |

Table 6: Pencil Hardness grade for POPU and FPOPU (steel )

| Formulation | Result | Index |
| --- | --- | --- |
| POPU |  | H |
| FPOPU-2 phr |  | 7H |
| FPOPU-4 phr |  | 7H |
| FPOPU-6 phr |  | 8H |
| FPOPU-8 phr |  | 6H |
| FPOPU-10 phr |  | 5H |
| FPOPU-12 phr |  | 6H |

Table 7: Glass surface before and after adhesion test with grade

| Formulation | Before | After | Class |
| --- | --- | --- | --- |
| POPU |  |  | 4B |
| FPOPU-2 phr |  |  | 4B |
| FPOPU-4 phr |  |  | 4B |
| FPOPU-6 phr |  |  | 3B |
| FPOPU-8 phr |  |  | 3B |
| FPOPU-10 phr |  |  | 2B |
| FPOPU-12 phr |  |  | 2B |

Table 8: Wood surface before and after adhesion test with grade

| Formulation | Before | After | Class |
| --- | --- | --- | --- |
| POPU |  |  | 3B |
| FPOPU-2 phr |  |  | 3B |
| FPOPU-4 phr |  |  | 3B |
| FPOPU-6 phr |  |  | 3B |
| FPOPU-8 phr |  |  | 2B |
| FPOPU-10 phr |  |  | 2B |
| FPOPU-12 phr |  |  | 2B |

Table 9: Steel surface before and after adhesion test with grade

| Formulation | Before | After | Class |
| --- | --- | --- | --- |
| POPU |  |  | 5B |
| FPOPU-2 phr |  |  | 5B |
| FPOPU-4 phr |  |  | 4B |
| FPOPU-6 phr |  |  | 5B |
| FPOPU-8 phr |  |  | 5B |
| FPOPU-10 phr |  |  | 5B |
| FPOPU-12 phr |  |  | 3B |

| Formulation | T5% / ℃ | T10% / ℃ | T50% / ℃ | Residual Weight at 700 ℃ (%) |
| --- | --- | --- | --- | --- |
| POPU | 162.717 | 207.475 | 415.296 | 6.245 |
| FPOPU-2 phr | 177.961 | 231.610 | 417.349 | 11.725 |
| FPOPU-4 phr | 178.326 | 232.553 | 418.209 | 15.332 |
| FPOPU-6 phr | 161.225 | 200.815 | 409.278 | 9.493 |
| FPOPU-8 phr | 150.576 | 226.255 | 414.066 | 7.736 |
| FPOPU-10 phr | 148.943 | 249.145 | 415.520 | 6.583 |
| FPOPU-12 phr | 132.793 | 213.361 | 414.133 | 6.064 |

Table 10: Thermal Data for FPOPU

Table 10: Thermal data for POPU and FPOPU

| Sample | Glass Transition Temperature (Tg1) | Glass Transition Temperature (Tg2) | Melting Point (Tm) | Melting Point Area |
| --- | --- | --- | --- | --- |
| POPU | 128.8 | 221.1 | 310.2 | 107.556 |
| FPOPU-2 phr | 129.6 | 227.1 | 309.3 | 121.693 |
| FPOPU-4 phr | 125.2 | 208.6 | 311.5 | 167.528 |
| FPOPU-6 phr | 122.4 | 202.2 | 310.5 | 99.888 |
| FPOPU-8 phr | 121.5 | 205.3 | 308.2 | 102.737 |
| FPOPU-10 phr | 120.3 | 190.8 | 309.4 | 98.562 |
| FPOPU-12 phr | 122.4 | 189.8 | 314.7 | 64.768 |

Table 11: Thermal Data for FPOPU