Supporting Information

Selective and rapid detection of minocycline in milk using a novel fluorescence conjugated polymer probe

Lindan Gong*, Lin Zhang, Hengyuan Wang, Yan Sun, Hongju Zhang, and Lu-an Fan*

College of materials science & chemical engineering, Harbin Engineering University, Harbin, 150001, People’s Republic of China

E-mail: gonglindan@hrbeu.edu.cn, and fanlu_an@hrbeu.edu.cn

Table S1 The spectral data of FOP in different solvents

| Solvent | λabs ( nm ) | λem ( nm ) | Stokes shift ( nm ) | QY |
| --- | --- | --- | --- | --- |
| H2O | 340 | 437 | 102 | 0.15 |
| Ethanol | 339 | 404 | 65 | 0.79 |
| DMF | 335 | 410 | 75 | 0.78 |
| DMSO | 339 | 412 | 73 | 0.74 |
| DMAc | 339 | 409 | 70 | 0.81 |
| ACN | 335 | 405 | 70 | 0.84 |

Figure. S1 Fluorescence emission spectra changes of FOP (20μM in PBS) upon addition of MC. The concentration of FOP was 10 μM in PBS (5 mM, pH = 5, 7, 10) and 0.125 μM ethanol. Inset: The FQE of MC towards FOP. λex = 339 nm

Figure. S2 The anti-interference ability of FOP to the detection of MC (180 µM). The concentration of FOP was 10 μM in PBS (5 mM, pH = 5, 7, 10) and 0.125 μM ethanol. λex = 339 nm

Table S2 The fit data for calculating the LOD value

| Solvent | Linear range ( µM ) | Linear equation ( F0 - F ) / F = K × C MC + b | LOD ( µM ) | R2 |
| --- | --- | --- | --- | --- |
| PBS ( pH = 5 ) | 0 - 12 | 0.0311 ( ± 0.0010 ) C MC + 0.0204 ( ± 0.0074 ) | 0.0228 | 0.9923 |
| PBS ( pH = 7 ) | 0 - 12 | 0.0390 ( ± 0.0011 ) C MC + 0.0221 ( ± 0.0078 ) | 0.0295 | 0.9945 |
| PBS ( pH = 10 ) | 0 - 12 | 0.0371 ( ± 0.0011 ) C MC + 0.0188 ( ± 0.0076 ) | 0.0151 | 0.9943 |
| Ethanol | 0 - 28 | 0.0210 ( ± 0.0006 ) C MC + 0.0148 ( ± 0.0099 ) | 0.0369 | 0.9953 |

Table S3 The LOD obtained from different analytical methods

| Method | Linear range (µM) | LOD (µM) | References number |
| --- | --- | --- | --- |
| Electrochemical method | 1.00 - 2.30 | 0.70 | 27 |
| HPLC | 2.02 x 10-3 - 0.40 | 6.07 x 10-4 | 61 |
| UHPLC - UV | 3.04 - 20.26 | 3.00 | 62 |
| SPE - HPLC | 0.01 - 2.03 | 8.38 × 10−4 | 63 |
| Fluorescence detection | 2.03 - 20.03 | 0.0151 | 34 |
| Fluorescence detection | 2.02 x 10-3 - 1.01 | 6.60 × 10−4 | 64 |
| Fluorescence detection | 0.40 - 10.00 | 0.02 | 65 |
| Present work | 0 - 28 | 0.04 |  |