Electronic supplementary material

Phosphate removal from aqueous solution by Fe-La binary (hydr)oxides: A study of batch experiments and mechanisms

Haijing Duan a,b,c, Lin Zhang a,c, Yulong Wang a,b,c,*, Yanhong Liu d,*, Yangyang Wang a,b,c,*

- College of Environment and Planning, Henan University, Kaifeng, 475004, China

- Key Laboratory of Geospatial Technology for the Middle and Lower Yellow River Regions (Henan University), Ministry of Education, Kaifeng, 475004, China

- Henan Engineering Research Center for Control and Remediation of Heavy Metal Pollution, Henan University, Kaifeng, 475004, China

- College of Software, Henan University, Kaifeng, 475004, China

----------------------------------

*Corresponding authors.

E-mail adresses: 10130133@vip.henu.edu.cn (Y Wang), liuyanhongxmu@163.com (Y Liu), wangyangyangxyz@163.com (Y Wang).

Synthesis of lanthanum hydroxide:

The lanthanum hydroxide adsorbent was synthesized as previously reported (Xu et al., 2017; Wang et al., 2020). La(NO3)3∙6H2O was used to prepare a La(III) solution using DI water, and then the pH of the solution was adjusted to ~10 with a 1 M NaOH solution. The resulting white slurry was allowed to stabilize for 2 hr under vigorous magnetic stirring. Finally, the formed lanthanum hydroxide precipitates were centrifuge-washed with DI water and dried in an oven at 60 °C overnight. After that, the solid product was ground and stored in airtight containers for further use.

Fig. S1 Phosphate speciation as a function of solution pH.

Fig. S2 The release of La(III) in solution after phosphate removal.

Fig. S3 FTIR spectra of Fe/La 3:1, Fe/La 1:1 and Fe/La 1:3 binary (hydr)oxides before and after phosphate adsorption.

References

Xu R, Zhang M, Mortimer RJG, Pan G (2017). Enhanced Phosphorus Locking by Novel Lanthanum/Aluminum-Hydroxide Composite: Implications for Eutrophication Control. Environ Sci Technol 51(6):3418-3425.

Wang YL, Liu YH, Guo TQ, Liu HP, Li JL, Wang SF, Li XH, Wang X, Jia YF (2020) Lanthanum hydroxide: a highly efficient and selective adsorbent for arsenate removal from aqueous solution. Environ Sci Pollut Res 27:42868-42880.