Electronic Supplementary Material

Non-enzymatic detection of uric acid in serum and urine by fluorescent and visual dual-mode sensor based on 3-aminophenylboric acid functionalized carbon dots

Xin Li1,2, Guoqing Chen1,2,*, Anqi Hu1,2, Yi Xiong1,2, Taiqun Yang1,2, Chaoqun Ma1,2, Lei Li1,2, Hui Gao1,2, Chun Zhu1,2, Yamin Wu1,2, Jiao Gu1,2, Hui Wu1,2, Yan Zhou1,2, Weinan Guan1,2, Wei Zhang1,2

1 School of Science, Jiangnan University, Wuxi 214122, China

2 Jiangsu Provincial Research Center of Light Industrial optoelectronic engineering and Technology, Wuxi 214122, China

* Corresponding author

E-mail: jncgq@jiangnan.edu.cn

Tel: +86-139-0617-6695

Contents

Fig. S1 .........................................................................................................................................S-3

Fig. S2 .........................................................................................................................................S-4

Fig. S3 .........................................................................................................................................S-5

Fig. S4 .........................................................................................................................................S-6

Table S1.......................................................................................................................................S-7

References....................................................................................................................................S-8

Fig. S1. A. Stability of fluorescence intensity over time B. The change of fluorescence intensity under different pH C. The change of fluorescence intensity under different UV light (λex = 365 nm) irradiation time D. Stability under different concentrations of salt solution E. Effect of different temperatures on the fluorescence intensity of APBA-CDs

Fig. S2. A. Emission spectra of the system after the addition of different concentrations of UA in serum B. Relationship between fluorescence quenching degree (F0-F)/F0 and UA concentration in serum (Inset: Linear relationship between (F0-F)/F0 and UA concentration in the range of 6-40 μM) C. Emission spectra of the system after the addition of different concentrations of UA in urine D. Relationship between (F0-F)/F0 and UA concentration in urine (Inset: Linear relationship between (F0-F)/F0 and UA concentration in the range of 6-40 μM)

Fig. S3. A. Normalized absorption spectra of the system after the addition of different concentrations of UA in serum B. Relationship between degree of blue shift (λ0-λ)/λ0 and UA concentration in serum (Inset: Linear relationship between (λ0-λ)/λ0 and UA concentration in the range of 6-80 μM) C. Normalized absorption spectra of the system after the addition of different concentrations of UA in urine D. Relationship between (λ0-λ)/λ0 and UA concentration in urine (Inset: Linear relationship between (λ0-λ)/λ0 and UA concentration in the range of 25-50 μM)

Fig. S4. Selectivity (A and B) and anti-interference (C and D) experiments. A and C were photos of samples under daylight, while B and D were photos of samples under UV light (λex=365 nm)

Table S1. Comparison of the performance of different fluorescent probes for detection of UA

| Material | Source | Linear range (μM) | LOD (μM) | Reference |
| --- | --- | --- | --- | --- |
| N-CDs | Citric acid monohydrate + DETA | 0.5-150 | 0.06 | [1] |
| CDs | Dog blood | 5-100 | 0.5 | [2] |
| Fe3+@b-CDs | 1-naphthylamine+ trichloromethane | 67.64-450 | 67.64 | [3] |
| Fe/N-CDs | FeCl3+EDTA+DETA | 0.5-100 | 0.14 | [4] |
| N, P-CDs | Citric acid+ urea+ formamide+ phosphoric acid | 0.5-10 | 0.4 | [5] |
| CDs | Pork | 0.1-100, 100-500 | 0.05 | [6] |
| S, N-CDs | Citric acid+ thiourea | 0.08-10, 10-50 | 0.07 | [7] |
| S, N-CDs | Citric acid+ L-cysteine | 2.5-30 | 0.8 | [8] |
| Si/N-CDs | 3-aminopropyl-triethoxysilane+ citric acid | 0.5-30 | 0.14 | [9] |
| MnO2@CDs | Citric acid+ ethylenediamine | 0.1-200 | 0.045 | [10] |
| Ag NPs/N-CDs | Hydroxyethyl cellulose+ L-citrulline | 2-60 | 0.53 | [11] |
| g-CDs | Passiflora edulis sims shell powder+ m-phenylenediamine | 1-17 | 0.94 | [12] |
| MCDs | Maleic acid+ tris+ benzoic acid | 5-400 | 2.26 | [13] |
| Arg-CDs | L-arginine+ DL-malic acid | 330-630 | 7.14 | [14] |
| APBA-CDs | 3-aminophenylboric acid+ L-glutamine | 7-30 | 0.033 | This work |

References

1.	Li, F., et al., A highly sensitive dual-read assay using nitrogen-doped carbon dots for the quantitation of uric acid in human serum and urine samples. Microchimica Acta, 2021. 188(9).

2.	Yuan, C., et al., Dual-signal uric acid sensing based on carbon quantum dots and o-phenylenediamine. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 2021. 254.

3.	Zhang, D., et al., One-pot synthesis of multicolor carbon quantum dots: One as pH sensor, one with ultra-narrow emission as fluorescent sensor for uric acid. Dyes and Pigments, 2023. 213.

4.	Zhang, W., et al., A universal sensing platform based on iron and nitrogen co-doped carbon dots for detecting hydrogen peroxide and related metabolites in human fluid by ratiometric fluorometry and colorimetry. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 2022. 272.

5.	Hallaj, T., N. Azizi, and M. Amjadi, A dual-mode colorimetric and fluorometric nanosensor for detection of uric acid based on N, P co-doped carbon dots and in-situ formation of Au/Ag core-shell nanoparticles. Microchemical Journal, 2021. 162.

6.	Zhao, C., et al., Green synthesis of carbon dots from pork and application as nanosensors for uric acid detection. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 2018. 190: p. 360-367.

7.	Wang, H., et al., High fluorescence S, N co-doped carbon dots as an ultra-sensitive fluorescent probe for the determination of uric acid. Talanta, 2016. 155: p. 62-69.

8.	Amjadi, M., T. Hallaj, and Z. Kouhi, An enzyme-free fluorescent probe based on carbon dots – MnO2 nanosheets for determination of uric acid. Journal of Photochemistry and Photobiology A: Chemistry, 2018. 356: p. 603-609.

9.	Cao, D., et al., Enzyme-free fluorescence determination of uric acid and trace Hg(II) in serum using Si/N doped carbon dots. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 2021. 263.

10.	Yang, J., et al., A facile fluorescence assay for rapid and sensitive detection of uric acid based on carbon dots and MnO2nanosheets. New Journal of Chemistry, 2018. 42(18): p. 15121-15126.

11.	Zhang, Q., et al., Silver Nanoparticle-Functionalised Nitrogen-Doped Carbon Quantum Dots for the Highly Efficient Determination of Uric Acid. Molecules, 2022. 27(14).

12.	Li, G.-W., et al., Carbon quantum dots with green fluorescence as a probe for detecting uric acid. Chemical Papers, 2022. 76(6): p. 3627-3638.

13.	Qin, J., et al., Bright carbon dots via inner filter effect for the sensitive determination of the purine metabolic disorder in human fluids. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 2018. 203: p. 421-427.

14.	Gan, X., et al., Arginine–malate-based dual-emission carbon dots for uric acid determination in human serum with a miniaturized device. Journal of Materials Science, 2022. 57(1): p. 576-588.