Table 1: Effects of catalysts on the dehydrogenative aromatisation of 4-methylcyclohexanone (1a).a

| Entry | Catalyst | Yield (%) |  |  |
| --- | --- | --- | --- | --- |
|  |  | 2a | 2a′ | 3a |
| 1 | Ni/CeO2-0.3NaNaph | 50 | 3 | 13 |
| 2 | Cu/CeO2-0.3NaNaph | 1 | <1 | <1 |
| 3 | Co/CeO2-0.3NaNaph | <1 | <1 | <1 |
| 4 | Mn/CeO2-0.3NaNaph | <1 | <1 | <1 |
| 5 | Fe/CeO2-0.3NaNaph | <1 | <1 | <1 |
| 6 | Zn/CeO2-0.3NaNaph | <1 | <1 | <1 |
| 7 | Ni/CeO2-NaNaph | 59 | 6 | 11 |
| 8b | Ni/CeO2-NaNaph | 74 | 13 | 3 |
| 9b | Ni/HAP-NaNaph | 1 | <1 | <1 |
| 10b | Ni/ZrO2-NaNaph | <1 | <1 | <1 |
| 11b | Ni/TiO2-NaNaph | <1 | <1 | <1 |
| 12b | Ni/Al2O3-NaNaph | <1 | <1 | <1 |
| 13 | CeO2 | <1 | <1 | <1 |
| 14 | CeO2-NaNaph | <1 | <1 | <1 |
| 15 | Ni(OH)x/CeO2 | <1 | <1 | <1 |
| 16c | Ni/CeO2-NaNaph | <1 | <1 | <1 |
| 17 | Ni/HAP-NaNaph | 2 | <1 | <1 |
| 18d | Ni/HAP-NaNaph | 9 | <1 | <1 |
| 19e | Ni/HAP-NaNaph | 8 | <1 | <1 |
| 20b,f | Ni(cod)2 + IPr | 3 | <1 | <1 |

a Reaction conditions: 1a (0.3 mmol), catalyst (3.3 mol%), DMA (2 mL), Ar (1 atm), 160°C, 24 h. Yields were determined by GC analysis using n-hexadecane as an internal standard. b 180°C. c PhCOOH (0.3 mmol). d CeO2-NaNaph (40 mg). e Na2CO3 (0.3 mmol). f IPr (6.7 mol%). cod = 1,5-cyclooctadiene. IPr = 1,3-bis(2,6-diisopropylphenyl)imidazol-2-ylidene.