# Fates of nutrient elements and heavy metals during thermal conversion of cattle slurry-derived anaerobic digestates

Daniel J. Lane, Olli Sippula, Jorma Jokiniemi, Mikko Heimonen, Niko M. Kinnunen, Perttu Virkajärvi, Narasinha Shurpali

Supplementary Material

Table S1. Experimental matrix

| test ID | sample ID | temperature | reactant gas composition | reaction time | ash/char analyses |  |  |  | product gas analysis |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | (°C) |  | (min) | macronutrient elements | heavy metals | total carbon | powder XRD |  |
| 1 | AD-2018 | 800 | 1.5% O2 / bal. N2 | 25 | X | X | X | X |  |
| 2 | AD-2018 | 1000 | 1.5% O2 / bal. N2 | 60 | X | X | X | X | X |
| 3 | AD-2018 | 1000 | N2 | 20 | X | X | X |  | X |
| 4 | AD-2018 | 1000 | 10% H2 / bal. N2 | 120 | X | X | X |  |  |
| 5 | AD-2018 | 1000 | CO2 | 120 | X | X | X |  |  |
| 6 | AD-2019 | 800 | 1.5% O2 / bal. N2 | 25 | X |  | X |  |  |
| 7 | AD-2019 | 1000 | 1.5% O2 / bal. N2 | 60 | X |  | X |  |  |
| 8 | AD-2019 | 1000 | N2 | 20 | X |  | X |  |  |
| 9 | AD-2019 | 1000 | 10% H2 / bal. N2 | 120 | X |  | X |  |  |
| 10 | AD-2019 | 1000 | CO2 | 120 | X |  | X |  |  |

Table S2. Analysis of inorganic macronutrient elements and heavy metals (Zn, Cu and Mn) in the standard reference material BCR 129 (hay powder).

|  |  | Concentration | Recovery |
| --- | --- | --- | --- |
|  | measured isotope | (mg/kg) | (%) |
| K | 39 | 31122 | 92 |
| Ca | 42 | 5533 | 86 |
| P | 31 | 2407 | 102 |
| Mg | 24 | 1372 | 95 |
| Na | 23 | 3443 | 99 |
| Fe | 57 | 113 | 99 |
| Al | 27 | 101 | 90 |
| Mn | 55 | 79 | 110 |
| Zn | 68 | 37 | 115 |
| Cu | 65 | 9 | 89 |

Table S3. Char/ash yields following thermal conversion of AD-2019 at different operating conditions, and concentrations of macronutrient elements in the char and ash residues.

| temperature | reactant gas composition | yield of ash or char | concentration in char or ash residue (wt. %) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (°C) |  | (%) | P | K | Na | Ca | Mg | C | N |
| 800 | 1.5% O2 / bal. N2 | 16.7 ± 1.7 | 7.0 ± 0.3 | 13.8 ± 0.7 | 2.2 ± 0.1 | 9.6 ± 1.0 | 5.9 ± 0.4 | 0.80 ± 0.01 | <0.1 |
| 1000 | 1.5% O2 / bal. N2 | 16.4 ± 1.6 | 7.0 ± 0.3 | 11.8 ± 0.6 | 1.9 ± 0.1 | 9.6 ± 1.0 | 6.0 ± 0.4 | <0.1 | <0.1 |
| 1000 | N2 | 32.9 ± 3.3 | 3.0 ± 0.1 | 5.3 ± 0.3 | 0.50 ± 0.02 | 4.6 ± 0.5 | 2.8 ± 0.2 | 47.0 ± 4.9 | 0.90 ± 0.04 |
| 1000 | CO2 | 16.4 ± 1.6 | 7.3 ± 0.3 | 13.5 ± 0.6 | 2.4 ± 0.1 | 10.2 ± 1.1 | 6.4 ± 0.4 | 0.25 ± 0.02 | <0.1 |
| 1000 | 10% H2 / bal. N2 | 29.2 ± 2.9 | 1.5 ± 0.1 | 3.3 ± 0.2 | 0.10 ± 0.01 | 5.4 ± 0.6 | 3.2 ± 0.2 | 54.9 ± 5.3 | 0.60 ± 0.03 |

Figure S1. Carbonaceous emissions from pyrolysis (N2) and combustion (1.5% O2 / bal. N2) of AD-2018. Initial sample masses were 0.53 and 0.71 g for pyrolysis and combustion respectively.

Figure S2. Nitrogeneous emissions from pyrolysis (N2) and combustion (1.5% O2 / bal. N2) of AD-2018. Initial sample masses were 0.53 and 0.71 g for pyrolysis and combustion respectively.