Supporting Information

Ammonium vanadate doped by hydrated manganese divalent ions for high-performance zinc-ion batteries

Jidong Hu, Yali Li*, Sijin Shen, Yunxia Dong, Donghao Li, Yongchao Chen, Yujun Fu, Deyan He, and Junshuai Li*

LONGi Institute of Future Technology, and School of Materials & Energy, Lanzhou University, 222 South Tianshui Road, Lanzhou 730000, China

E-mail: liyli@lzu.edu.cn (Y. Li) and jshli@lzu.edu.cn (J. Li).

Figure S1. XPS survey spectra of Mn:NVO and NVO.

Figure S2. SEM image of NVO.

Figure S3. Rate performance of NVO, Mn:NVO, Mn:NVO-1 and Mn:NVO-2.

Figure S4. CV curves of NVO at different scan rates.

Figure S5. Log(i) vs log(v) plots of NVO.

Figure S6. Capacity contributions from the diffusion-controlled and capacitive processes for NVO at various scan rates.

Figure S7. (a) Charge-discharge GITT curves at 0.05 A g−1 and (b) the corresponding Zn2+ diffusion coefficients of NVO.

Figure S8. Comparison of the EIS curves of the AZIBs with Mn:NVO and NVO.

Table S1. Comparison of the energy density and power density between the present work and the recently reported AZIBs.

| Cathode | Energy density (Wh kg−1) | Power density (W kg−1) | Ref. |
| --- | --- | --- | --- |
| KNVO | 324 | 457 | [40] |
| Mg2V2O4 | 140.6 | 147.5 | [48] |
| MnO2 | 270 | 78 | [49] |
| V5O12·H2O | 194 | 2100 | [50] |
| VOPO4 | 122.6 | 328.5 | [51] |
| CUV2O6 | 210 | 317 | [52] |
| DMF-NVO | 436 | 400 | [53] |
| PANI-VOH | 150 | 3900 | [54] |
| Ca0.24V2O5·0.83H2O | 267 | 53.4 | [55] |
| KVOH | 308 | 402 | [56] |
| Mn:NVO | 378 | 362 | This work |

Table S2. Comparison of the electrochemical performance between this work and the recently reported AZIBs.

| Cathode | Electrolyte | Specific capacity | Cycling performance | Ref. |
| --- | --- | --- | --- | --- |
| ZnVO-800 | 2 M ZnSO4 | 314 mAh g−1 at 0.5 A g−1 | 90.8% after 3000 cycles at 5 A g-1 | [57] |
| ox-VOH | 2.0 M Zn(CF3SO3)2 | 268 mAh g−1 at 0.5mA g−1 | 88% after 240 cycles at 0.5 A g−1 | [58] |
| V2O5@PEDOT/CC | 3.0 M Zn(CF3SO3)2 | 360 mAh g−1 at 0.1 A g−1 | 89% after 1000 cycles at 5 A g−1 | [59] |
| NH4V4O10 | 3.0 M Zn(CF3SO3)2 | 296 mAh g−1 at 0.1 A g-1 | 97.5% after 1000 cycles at 10 A g-1 | [60] |
| MnVO | 3.0 M Zn(CF3SO3)2 | 209 mAh g−1 at 0.1 A g-1 | 85.5% after 10000 cycles at 5 A g-1 | [61] |
| H2V3O8 nanowire | 3.0 M Zn(CF3SO3)2 | 423 mAh g−1 At 0.1 A g−1 | 94.3% after 1000 cycles at 5 A g−1 | [62] |
| V3O7/V2O5 | 2.5 M Zn(CF3SO3)2 | 340 mAh g−1 At 0.2 A g−1 | 83% after 6500 cycles at 5 A g−1 | [63] |
| V12O24@C | 3.0 M Zn(CF3SO3)2 | 290.5 mAh g−1 at 0.5 A g−1 | 94.1% after 10000 cycles at 10 A g−1 | [64] |
| PANI/V2O5 | 3.0 M Zn(CF3SO3)2 | 353.6 mAh g−1 at 0.1 A·g−1 | 87.5% after 100 cycles at 0.2 A·g−1 | [65] |
| (NH4)2V6O16⋅1.5H2O | 3.0 M Zn(CF3SO3)2 | 385 mAh g −1 At 0.1 A g −1 | 75% after 10000 cycles at 8 A g−1 | [66] |
| Mn:NVO | 3.0 M Zn(CF3SO3)2 | 474.0 mAh g-1 at 0.5 A g-1 | 85.3% after 3000 cycles at 5.0 A g-1 | This work |