Table 1. Composition and concentration of various components in the MP mixture (polyethylene, PE; polyterephathalate Ethylene, PET; polypropylene, PP; polyvinyl, PVC).
[image: ]

[bookmark: _GoBack]
image1.png
MP Mixture PE PP PvC PET Total (pg.g™t)

Mass Composition 40 40 10 10 -
Metallic Trace Elements (ng.g?') Cu 2.0 3.5 4.7 13.8
Pb 4.9 9.0 786.0 19.5
Zn 9.0 4169.8 432.3 52.6
Cd 6.0 123.2 <LOQ <LOQ

Cr <LOQ 77.9 23.1 359.5





