Highlights:

- Pure CuO were synthesized using a facile hydrothermal method.

- The structure, phase and morphology of the products were observed by hydrothermal method with reduced CuO NPs.

- The specific surface area of the Synthesized NPs was found to be 11.38 m2g-1.

- The capacitance values of CuO were found to be 197, 175, 151, 136 and 123 F g-1 at different scan rates of 10, 25, 50, 75 and 100 mV s−1, respectively