SUPPORTING INFORMATION

Various approaches to the introduction of magnesium ions into post-metallocene (OO)TiCl2-type catalytic systems. Comparison of the catalytic activity of the titanium saligenin complex activated by an Al/Mg co-catalyst (AlknAlCl3-n+Alk2Mg) and Ti/Mg precatalysts obtained in situ in ethylene polymerization

Vladislav A. Tuskaev, Dmitry A. Kurmaev, Svetlana Ch. Gagieva,  Evgenii K. Golubev, Mikhail I. Buzin, Maria D. Evseeva, Viktor N. Khrustalev, Svetlana A. Aksenova, Kasim F. Magomedov, Boris M. Bulychev

Table S1. Crystal data and structure refinement for 3 and 4.

| Identification code | 2 | 4 • 2(C7H16) | 3 • C5H12 |
| --- | --- | --- | --- |
| Empirical formula | C42H58F12MgO6 | C106H162F24Mg5O14 | C51H76F12Mg2O7 |
| Formula weight | 911.19 | 2237.91 | 1077.74 |
| Crystal size, mm |  | 0.13×0.15×0.22 | 0.15×0.18×0.23 |
| Temperature, K | 120 | 100 | 100 |
| Wavelength, Å |  | 1.54184 | 1.54184 |
| Crystal system | Monoclinic | Triclinic | Triclinic |
| Space group | P21/c | P-1 | P-1 |
| a, Å | 14.8157(8) | 16.65075(14) | 10.56804(11) |
| b, Å | 17.5428(10) | 19.78626(14) | 14.71830(16) |
| c, Å | 18.5639(10) | 19.94495(13) | 18.7621(2) |
| , deg. | 90 | 100.2822(6) | 70.8370(10) |
| , deg. | 108.100(3) | 111.1983(7) | 89.7664(8) |
| γ, deg. | 90 | 98.2954(6) | 87.4357(8) |
| V, Å3 | 4586.2(4) | 5869.72(9) | 2753.68(5) |
| Z | 4 | 2 | 2 |
| Density (calc.), Mg/m3 | 1.320 | 1.266 | 1.300 |
| , mm-1 |  | 1.155 | 1.159 |
| F(000) | 1912 | 2372 | 1140 |
| Theta range, deg. |  | 2.33 – 78.16 | 2.49 – 77.95 |
| Index ranges |  | -20 ≤ h ≤ 21, -24 ≤ k ≤ 25, -25 ≤ l ≤ 24 | -13 ≤ h ≤ 13, -18 ≤ k ≤ 18, -22 ≤ l ≤ 23 |
| Reflections collected | 66573 | 150525 | 82994 |
| Independent reflections, Rint | 8927 | 24602, 0.057 | 11631, 0.046 |
| Reflections observed | 7394 | 21721 | 10769 |
| R1 / wR2 (I > 2σ(I)) |  | 0.055 / 0.147 | 0.048 / 0.127 |
| R1 / wR2 (all data) |  | 0.061 / 0.155 | 0.051 / 0.129 |
| Goodness-of-fit on F2 | 1.018 | 1.028 | 1.033 |
| Extinction coefficient |  | ─ | 0.00053(5) |
| Tmin / Tmax |  | 0.133 / 1.000 | 0.928 / 1.000 |
| Δρmax / Δρmin, e.Å-3 | 0.402/ -0.261 | 1.181 / -0.713 | 0.760 / -0.713 |

Table S2. Bond distances (Å) and angles (°) for Mg(II) in 4 and 3.

| Compound 4 |  |  |  |
| --- | --- | --- | --- |
| Mg1─O1 | 1.8937(14) | Mg3─O10 | 1.9548(13) |
| Mg1─O2 | 1.9763(13) | Mg3─F10 | 2.4423(12) |
| Mg1─O3 | 1.9752(13) | Mg3─F15 | 2.4401(12) |
| Mg1─O11 | 2.0244(14) | Mg4─O5 | 2.0215(13) |
| Mg1─F2 | 2.4881(13) | Mg4─O6 | 2.0579(13) |
| Mg1─F7 | 2.5564(12) | Mg4─O7 | 1.9787(13) |
| Mg2─O2 | 1.9931(13) | Mg4─O10 | 1.9669(13) |
| Mg2─O3 | 2.0568(13) | Mg4─O13 | 2.1053(14) |
| Mg2─O4 | 2.0247(13) | Mg5─O6 | 1.9908(13) |
| Mg2─O9 | 1.9652(13) | Mg5─O7 | 1.9791(13) |
| Mg2─O12 | 2.0967(13) | Mg5─O8 | 1.9008(14) |
| Mg3─O4 | 2.0152(13) | Mg5─O14 | 2.0214(13) |
| Mg3─O5 | 2.0055(12) | Mg5─F16 | 2.5285(12) |
| Mg3─O9 | 1.9549(13) | Mg5─F22 | 2.3783(12) |
| O1─Mg1─O2 | 91.08(6) | O2─Mg2─O9 | 122.61(6) |
| O1─Mg1─O3 | 126.96(6) | O2─Mg2─O12 | 98.00(5) |
| O1─Mg1─O11 | 99.74(6) | O3─Mg2─O4 | 83.59(5) |
| O1─Mg1─F2 | 82.09(5) | O3─Mg2─O9 | 154.58(6) |
| O1─Mg1─F7 | 150.80(5) | O3─Mg2─O12 | 90.80(5) |
| O2─Mg1─O3 | 84.60(5) | O4─Mg2─O9 | 79.94(5) |
| O2─Mg1─O11 | 150.16(6) | O4─Mg2─O12 | 144.40(6) |
| O2─Mg1─F2 | 71.97(5) | O9─Mg2─O12 | 91.42(5) |
| O2─Mg1─F7 | 78.16(5) | O4─Mg3─O5 | 148.31(6) |
| O3─Mg1─O11 | 109.72(6) | O4─Mg3─O9 | 80.41(5) |
| O3─Mg1─F2 | 143.51(5) | O4─Mg3─O10 | 118.26(6) |
| O3─Mg1─F7 | 79.46(5) | O4─Mg3─F10 | 68.10(4) |
| O11─Mg1─F2 | 82.02(5) | O4─Mg3─F15 | 86.30(5) |
| O11─Mg1─F7 | 78.99(5) | O5─Mg3─O9 | 116.81(5) |
| F2─Mg1─F7 | 68.79(4) | O5─Mg3─O10 | 80.43(5) |
| O2─Mg2─O3 | 82.07(5) | O5─Mg3─F10 | 87.38(4) |
| O2─Mg2─O4 | 115.83(6) | O5─Mg3─F15 | 68.13(4) |
| O9─Mg3─O10 | 114.36(6) | O6─Mg5─F22 | 144.32(5) |
| O9─Mg3─F10 | 146.56(5) | O7─Mg5─O8 | 90.66(5) |
| O9─Mg3─F15 | 90.63(5) | O7─Mg5─O14 | 152.65(6) |
| O10─Mg3─F10 | 91.11(5) | O7─Mg5─F16 | 76.55(5) |
| O10─Mg3─F15 | 146.56(5) | O7─Mg5─F22 | 73.83(5) |
| F10─Mg3─F15 | 76.79(4) | O8─Mg5─O14 | 100.76(6) |
| O5─Mg4─O6 | 84.17(5) | O8─Mg5─F16 | 150.33(5) |
| O5─Mg4─O7 | 114.49(6) | O8─Mg5─F22 | 82.23(5) |
| O5─Mg4─O10 | 79.74(5) | O14─Mg5─F16 | 81.51(5) |
| O5─Mg4─O13 | 146.78(6) | O14─Mg5─F22 | 83.12(5) |
| O6─Mg4─O7 | 82.66(5) | F16─Mg5─F22 | 68.59(4) |
| O6─Mg4─O10 | 154.21(6) | Mg1─O2─Mg2 | 97.60(6) |
| O6─Mg4─O13 | 90.14(5) | Mg1─O3─Mg2 | 95.57(5) |
| O7─Mg4─O10 | 122.40(6) | Mg2─O4─Mg3 | 97.72(5) |
| O7─Mg4─O13 | 97.07(5) | Mg2─O9─Mg3 | 101.81(6) |
| O10─Mg4─O13 | 92.36(6) | Mg3─O5─Mg4 | 98.04(5) |
| O6─Mg5─O7 | 84.39(5) | Mg3─O10─Mg4 | 101.65(6) |
| O6─Mg5─O8 | 126.72(6) | Mg4─O6─Mg5 | 94.99(5) |
| O6─Mg5─O14 | 107.45(5) | Mg4─O7─Mg5 | 97.92(5) |
| O6─Mg5─F16 | 79.18(4) |  |  |

Compound 3

| Mg1─O1 | 1.8802(12) | Mg2─O2 | 2.1138(12) |
| --- | --- | --- | --- |
| Mg1─O2 | 1.9741(12) | Mg2─O3 | 1.9394(13) |
| Mg1─O4 | 1.9492(11) | Mg2─O4 | 1.9838(12) |
| Mg1─O5 | 1.9931(12) | Mg2─O6 | 2.0363(12) |
| Mg1─F7 | 2.3148(11) | Mg2─O7 | 2.0473(12) |
| O1─Mg1─O2 | 93.74(5) | O4─Mg1─O5 | 119.66(5) |
| O1─Mg1─O4 | 118.87(5) | O4─Mg1─F7 | 71.40(4) |
| O1─Mg1─O5 | 115.05(5) | O5─Mg1─F7 | 81.28(5) |
| O1─Mg1─F7 | 92.68(5) | O2─Mg2─O3 | 162.85(5) |
| O2─Mg1─O4 | 83.62(5) | O2─Mg2─O4 | 79.26(4) |
| O2─Mg1─O5 | 118.05(5) | O2─Mg2─O6 | 91.94(5) |
| O2─Mg1─F7 | 154.17(5) | O2─Mg2─O7 | 98.17(5) |
| O3─Mg2─O4 | 87.54(5) | O4─Mg2─O7 | 108.19(5) |
| O3─Mg2─O6 | 89.38(5) | O6─Mg2─O7 | 117.77(5) |
| O3─Mg2─O7 | 96.33(5) | Mg1─O2─Mg2 | 95.19(5) |
| O4─Mg2─O6 | 133.99(5) | Mg1─O4─Mg2 | 100.32(5) |

Figure S1. DSC curves corresponding to UHMWPE produced on complex 1+Et2AlCl/Bu2Mg (entry 1, table 1).

Figure S2. DSC curves corresponding to UHMWPE produced on precatalyst 1+Me3Al (entry 5, table 1).

Figure S3. DSC curves corresponding to UHMWPE produced on precatalyst 1+Me3Al in nefras (entry 6, table 1).

Figure S4. DSC curves corresponding to UHMWPE produced on precatalyst 1+Et3Al (entry 7, table 1).

Figure S5. DSC curves corresponding to UHMWPE produced on precatalyst 1+Et3Al in nefras (entry 8, table 1).

Figure S6. DSC curves corresponding to UHMWPE produced on precatalyst 1+ iBu3Al (entry 9, table 1).

Figure S7. DSC curves corresponding to UHMWPE produced on precatalyst 1+MAO (entry 10, table 1).

Figure S8. DSC curves corresponding to UHMWPE produced on precatalyst 1+MAO in nefras (entry 11, table 1).

Figure S9. DSC curves corresponding to UHMWPE produced on precatalyst 2+Me3Al in toluene (entry 12, table 1).

Figure S10. DSC curves corresponding to UHMWPE produced on precatalyst 2+Me3Al in nefras (entry 13, table 1).

Figure S11. DSC curves corresponding to UHMWPE produced on precatalyst 1+Et3Al in toluene (entry 14, table 1).

Figure S12. DSC curves corresponding to UHMWPE produced on precatalyst 2+Et3Al in nefras (entry 15, table 1).

Figure S13. DSC curves corresponding to UHMWPE produced on precatalyst 2+iBu3Al in toluene (entry 16, table 1).

Figure S14. DSC curves corresponding to UHMWPE produced on precatalyst 2+iBu3Al in nefras (entry 17, table 1).

Figure S15. DSC curves corresponding to UHMWPE produced on precatalyst 2+MAO in toluene (entry 18, table 1).

Figure S16. DSC curves corresponding to UHMWPE produced on precatalyst 2+MAO in nefras (entry 19, table 1).

Figure S17. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system 1+Et2AlCl/Bu2Mg (entry 1, table 1).

Figure S18. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system {Complex 1 on MgCl2} /Et2AlCl (entry 2, table 1).

Figure S19. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system {Complex 1 on MgCl2} / Et3Al (entry 3, table 1).

Figure S20. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system {Complex 1 on MgCl2} / Et2AlCl/Et3Al (entry 4, table 1).

Figure S21. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 1/Me3Al (entry 5, table 1).

Figure S22. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 1/Me3Al in nefras (entry 6, table 1).

Figure S23. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 1/ Et3Al in toluene (entry 7, table 1).

Figure S24. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 1/ Et3Al in nefras (entry 8, table 1).

Figure S25. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 1/ iBu3Al (entry 9, table 1).

Figure S26. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 1/ MAO in toluene (entry 10, table 1).

Figure S27. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 1/ MAO in nefras (entry 11, table 1).

Figure S28. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 2/ Me3Al in toluene (entry 12, table 1).

Figure S29. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 2/ Me3Al in nefras (entry 13, table 1).

Figure S30. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 2/ Et3Al in toluene (entry 14, table 1).

Figure S31. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 2/Et3Al in nefras (entry 15, table 1).

Figure S32. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 2/iBu3Al in toluene (entry 16, table 1).

Figure S33. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 2/iBu3Al in nefras (entry 17, table 1).

Figure S34. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 2/MAO in toluene (entry 18, table 1).

Figure S35. SEM images of the surface morphology of UHMWPE powders obtained with catalytic system Precatalyst 2/iBu3Al in nefras (entry 19, table 1).