Understanding the degradation process of polyhydroxyalkanoate (PHA)/ poly(butylene adipate-co-terephthalate) (PBAT) biocomposite mulch films and the effects of stabilizers under accelerated aging test

Yuchuan Tiana, Bing Zhoua, and James H. Wanga

a Sinopec Shanghai Research Institute of Petrochemical Technology, Shanghai 201028, PR China

Fig. S1 The XRD information of different ingredients of neat PHA-PBAT films

Table S1 The parameters for PHA-PABT melt blending

| Samples |  | PHA/PBAT | PHA/PBAT-UVA | PHA/PBAT-AO | PHA/PBAT-HRA |
| --- | --- | --- | --- | --- | --- |
| Composition (Mass fraction)a | PBAT | 80 | 80 | 80 | 80 |
|  | PHA | 20 | 20 | 20 | 20 |
|  | ADR | 0.5 | 0.5 | 0.5 | 0.5 |
|  | UVA | 0 | 0.3 | 0 | 0 |
|  | HRA | 0 | 0 | 0 | 0.6 |
|  | AO | 0 | 0 | 0.3 | 0 |
|  | OA* | 10.5 | 10.5 | 10.5 | 10.5 |
| Screw Speed (rpm) |  | 200 | 200 | 200 | 200 |
| Melt Temprature (℃) |  | 175 | 172 | 168 | 177 |
| Melt Pressure (bar) |  | 49 | 30 | 51 | 44 |
| Feeding speed (kg/h) |  | 8.3 | 8.4 | 8.4 | 8.4 |

* OA is the abbreviation for other additives including lubricants, opening agents etc.

a The mass fraction is the relative parts by weight based on 100 parts by weight of polymer.

Table S2 The parameters of different PHA-PABT films

| Additives | Amount (wt%) | Screw speed (rpm) | Drawing Speed (m/s) |  | Blow-up Ratio | Melt Pressure (bar) | Thickness (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| None | - | 30 | 6 | 2.35 |  | - | 13.4 |
| None | - | 30 | 6 | 2.94 |  | - | 19.7 |
| UVA | 0.3 | 30 | 6 | 2.69 |  | 0.3 | 17.5 |
| AO | 0.3 | 30 | 6 | 2.35 |  | 0.3 | 18.8 |
| HRA | 0.6 | 30 | 6 | 2.65 |  | 0.6 | 18.8 |

Table S3 Detailed information of fitted peaks of C 1s of PHA-PBAT  and PHA-PBAT-UV327 before and after aging

| XPS Deconvolution |  |  | sp2 | sp3 | C-O | C=O |
| --- | --- | --- | --- | --- | --- | --- |
| PBAT-PHA | 0 h | Position (eV) | 284.5 | 285 | 286.4 | 288.9 |
|  |  | Area (%) | 26.7 | 53.1 | 13.6 | 6.5 |
|  |  | FWHM (eV) | 1 | 1.2 | 1.2 | 1 |
|  |  | %GL | 80% | 80% | 80% | 80% |
|  | 50 h | Position (eV) | 284.5 | 285 | 286.4 | 288.9 |
|  |  | Area (%) | 36.3 | 41.1 | 12.4 | 10 |
|  |  | FWHM (eV) | 1 | 1.2 | 1.2 | 1 |
|  |  | %GL | 80% | 80% | 80% | 80% |
| PHA-PBAT-UV327 | 0 h | Position (eV) | 284.5 | 285 | 286.3 | 288.9 |
|  |  | Area (%) | 22.4 | 47.4 | 20.1 | 9.4 |
|  |  | FWHM (eV) | 1 | 1.2 | 1.2 | 1 |
|  |  | %GL | 80% | 80% | 80% | 80% |
|  | 50 h | Position (eV) | 284.5 | 285 | 286.3 | 288.9 |
|  |  | Area (%) | 27.1 | 46.7 | 13.7 | 12.5 |
|  |  | FWHM (eV) | 1 | 1.2 | 1.2 | 1 |
|  |  | %GL | 80% | 80% | 80% | 80% |

To whom correspondence should be addressed. JamesWang.sshy@sinopec.com.