Table. 3: Thermodynamic parameters for safranin removal by various adsorption systems under study at 25 ֯C (sorbent dose: 2 g L¯¹; pH 7; initial safranin concentration: 120 mg L¯¹).

Polymer sample T (K) ∆G0 (kJ mol ⁻1) ∆H°( kJ mol ⁻1) ∆S(kJ k⁻1 mol ⁻1)

P(AA-co-MMA) 298 -6.23 -61.15 -0.18

313 -1.13

323 -10.53

CMC/p(AA-co-MMA) 298 -6.53 -48.24 -0.11

313 -4.94

323 -7.70