Supporting Information

Graphene Oxide Boosted: A Multifaceted Examination of CZTS Composite for Enhanced Photocatalysis and Antimicrobial Efficacy

Halit Cavusoglua,b, Marwah Ali Ibrahima,b, Hüseyin Sakalakb,c , Erdogan Günesd, Ahmet Uysal1e, Emre Çıtakf,  Teoman Öztürk1a,g

aDepartment of Physics, Faculty of Science, Selcuk University, 42130, Konya, Türkiye

bAdvanced Nanotechnology Research Laboratory, Faculty of Science, Selcuk University, 42130, Konya, Türkiye

cGraduate School of Natural and Applied Sciences, Nanotechnology and Advanced Materials, Selcuk University, 42130, Konya, Türkiye

dDepartment of Biology, Faculty of Science, Selcuk University, 42130, Konya, Türkiye

eDepartment of Medical Services and Techniques, Vocational School of Health Services, Selcuk University,42130, Konya, Türkiye

fChemical Engineering Department, Faculty of Engineering and Natural Sciences, Konya Technical University, 42250, Konya, Türkiye

gAdvanced Technology Research and Application Center, Selcuk University, 42130, Konya, Türkiye

Fig. S1. SEM-EDX mapping analysis (a) and spectrum (b) of CZTS nanoparticles. The images that indicate the atomic symbols correspond to the EDX.

Table S1. EDX composition analysis of CZTS nanoparticles.

| Elements (Atomic %) | Series | Atomic Percentage (wt. %) |
| --- | --- | --- |
| Oxygen | K-series | 37.43 |
| Sulfur | K-series | 28.42 |
| Copper | K-series | 8.16 |
| Carbon | K-series | 11.97 |
| Zinc | K-series | 8.34 |
| Tin | L-series | 5.68 |

Corresponding authors

E-mail addresses: hcavusoglu@selcuk.edu.tr, (H.C.) ahuysal@selcuk.edu.tr, (A.U) teomanozturk@selcuk.edu.tr  (T.O.)