Supporting Information

Rapid and Positioned Fabrication of Pure Gold Microsphere Arrays with Stable Deep-pressing Anisotropic Conductivity for Next-generation Advanced Packaging

An Cao1,#, Yi Gong1,2,#, Dilong Liu1,#,*, Fan Yang3, Yulong Fan4,*, Xingyou Tian1, and Yue Li 1,3*

1. Key Lab of Materials Physics, Anhui Key Lab of Nanomaterials and Nanotechnology, Institute of Solid State Physics, HFIPS, Chinese Academy of Sciences, Hefei 230031, P. R. China

2. China-Europe Electronic Materials International Innovation Center, Hefei 230000, P. R. China

3. Tiangong University, Tianjin 300387, P. R. China

4. State Key Laboratory of Optical Technologies on Nano-Fabrication and Micro-Engineering, Institute of Optics and Electronics, Chinese Academy of Sciences, Chengdu 610209, P. R. China

# These Authors contributed equally to this work.

*Address correspondence to dlliu@issp.ac.cn, fanyl@ioe.ac.cn, yueli@issp.ac.cn

- Experimental section

1.1 Materials

Chloroauric acid (HAuCl4, 99.9%), ethylene glycol (EG, >99.5%), silver nitrate (AgNO3, >99.8%), 1,4-benzenediol, sodium hydrogen carbonate (NaHCO3), L-ascorbic acid (AA, >99.7%), Chloroplatinic acid hexahydrate (H2PtCl6·6H2O), N,N-Dimethylacetamide (DMAC, >99.0%) and n-butanol were obtained from Sinopharm Chemical Reagent Corporation. Poly (diallyldimethylammonium) chloride (PDDA, Mw=100 000-200 000, 20 wt% in water), polystyrene (PS, average Mw=35 000), Polydimethylsiloxane (PDMS) and trimethylchlorosilane (TMCS) and Potassium hexachloropalladate (K2PdCl6) were purchased from Sigma-Aldrich. Gold-plated conductive microspheres were purchased from Anhui Zhongke Yuanzhen Technology CO.LTD. The deionized water (DI water, 18.2 MΩ cm resistivity at 25 °C) was produced by a Milli-Q integral water purification system. All chemicals and solvents were directly used as received without any further treatment.

1.2 Preparation of gold nanoparticles

The gold nanoparticles with uniform size were synthesized by suing a polyol-reduction method.1 Briefly, HAucl4, PDDA, AgNO3 aqueous solution were added EG in turn, the precursor solution was obtained after shaking evenly. In the precursor solution, the concentrations of HAucl4, PDDA and AgNO3 aqueous were 0.0005 M, 0.0025 M and 0.000025 M respectively. Then the precursor solution was placed in an oil bath at 220 °C for 2 h. When the color of the precursor solution changed from the bright yellow into wine-red, it indicated the successful preparation of gold nanoparticles. The gold nanoparticles colloidal solution was centrifuged at 10,000 rpm for 20 min after cooling to the room temperature. After repeated centrifugation three times, the collected red precipitated products were re-dispersed in an appropriate volume of DI water and used for further assembly. Gold nanoparticles of different sizes could be obtained by adjusting the pH of the precursor solution before the oil bath according to the previous reports.

1.3 Preparation of honeycomb microhole array PS film

The typical process of the preparation of honeycomb microhole array PS film was divided into the two steps.2 Firstly, the silicon (Si) wafers of the microhole array (were prepared using a conventional photolithography strategy) were treated with trimethylchlorosilane vapor for 15 min and then used as molds, PDMS precursor (PDMS elastomer and cross linker at a ratio of 10:1) was cast into the Si wafer and put into the oven at 70 °C for 2 h. The silicon wafer mold was carefully peeled off the PDMS substrate after the PDMS was completely dried, then the PDMS mold with a reverse-pattern array was obtained. Secondly, the PS/DMAC solution (5 wt%) was cast into the PDMS mold and dried at 70 °C for 12 h. Finally, the honeycomb microhole array PS film was successfully prepared after the PDMS mold was removed.

1.4 Preparation of pure gold microspheres

The pure gold microspheres were prepared by using a laser melting method. The typical preparation process as shown in the Scheme 1. Firstly, 20 μL of n-butanol was dropped onto the PS film and left to stand for 5 min, this was to make the interior of the PS film completely infiltrated with n-butanol, then the excess n-butanol was removed by pipette. Secondly, 10 μL of gold nanosphere solution was dropped onto the PS film and left to stand for 5 min, it was to allow the assembly to proceed fully, then the excess gold nanoparticles were rinsed with n-butanol. Finally, this PS film was treated under pulsed laser (532 nm, 22.9 mJ∙cm-2) for 10 second and the gold microspheres were successfully prepared. AuAgPtPd alloy microspheres were prepared by the same steps except for replacing Au nanoparticles with Au@AgPt yolk-shell nanocubes and Au@Pd nanoparticles.

Scheme 1. Schematic illustration of fabrication of gold microspheres array via the well-positioned self-assembly and laser-irradiated ripening strategy.

1.5 Conductivity measurements

The single conductive gold microsphere pressure-resistance tests were performed on a Nanoindentation system (Anton Paar, Step 300-NHT3) with a flat punch tungsten carbide tip. In brief, the samples were diluted with ethanol to a suitable concentration, and added onto the washed tungsten substrate. After the samples were dry, the substrate was fixed horizontally to the test fixture. The maximum load of the nanoindentation system was 50 mN, the load rate was 100 mN/min, the contact time was 1s, the descent speed of the probe was 10 000 nm/min, and the recovery speed was 2 000 nm/min.

1.6 Simulation method

Absorption cross section of different gold colloidosomes consisting of different numbers of hexagonal close-packed (hcp) gold nanosoheres with 60 nm in diameter located on the surface of PS were performed using commercially available full-wave finite-difference time-domain software Ansys Lumerical FDTD. PML conditions were assigned to all six planes of the simulation region. Two sufficiently large Total-Field Scattered-Field (TFSF) sources with orthogonal polarizations were used to illuminate the gold colloidosomes located on the PS film. The refractive index of gold was taken from the experimental result of Johnson Christy, and the refractive index of PS and air were set to 1.6 and 1, respectively. The wavelength was set to 530 nm. The absorption cross section was then obtained from the "asb" analysis group.

The heating process of the colloidosomes is simulated in COMSOL 5.5, Multiphysics with the colloidosomes located inside an air cylinder with radius of 2 µm and height of 4 µm embedded in a PS hemisphere with 500 µm in radius. Another hemisphere is assigned to air with the same radius. Constant temperature condition is assigned to the outer surface of the sphere. The heat capacity, mass density and thermal conductivity of gold are set to 129 J/(kg·K), 19300 kg/m3 and 317 W/(m·K), respectively. The heat capacity, mass density and thermal conductivity of PS are set to 1300 J/(kg·K), 1050 kg/m3 and 0.033 W/(m·K), respectively. The heat capacity of air is set to 1050 kg/m3, and its temperature dependent mass density and thermal conductivity are taken from The Engineering ToolBox. The absorption cross section multiplied by the laser intensity is the total heating power. As the skin depth in gold at 530 nm was about 38 nm3 which was inferior to the size of each nanosphere (60 nm), it was reasonable to believe that only all the outermost nanoparticles work as the heating source in the experiment. As a result, the total heating power was equally distributed to all the outermost nanoparticles in each case in our heating simulations. The sweeping time step was set to 0.1ns, in order not to lose any detail during the heating process. The simulation of colloidosomes on PS immersed in butanol was simulated by simply replacing air by butanol with refractive index of 1.4 used in absorption cross section simulation, and heat capacity 2330 J/(kg·K), mass density 810 kg/m3 and heat conductivity as a function of temperature4 were used in heating simulation. Domain probes were assigned to seven hcp nanoparticles on the top of the gold colloidosomes, all the heating sources (marked as Union in Fig. xxx), all the cluster, all the media (PS + air or Butanol) to monitor their averaged temperature evolution during the heating process. A point probe was purposely set 6 μm far away from the centered gold colloidosomes to monitor the closest neighboring gold colloidosomes heated by the centered one during single-pulse laser illumination, in order to exclude the mutual heating effect. 5

1.7 Characterizations

The morphology of the final products was characterized by a field emission scanning electron microscope (SEM, SU 8020) and a transmission electron microscopy (TEM, FEI Tecnai G2 F20). The optical photographs of the samples were recorded by a digital camera. The non-focused 532 nm Nd:YAG laser had a pulse duration of 10 ns which was repeated at a frequency of 10 Hz.

2. Calculation of theoretical relationship between laser pulse fluence (J(τ)) and diameter of gold microspheres (dp)

On the basis of previous research reports on the heating-melting-fusion mechanism,6 we have made some simplifications to the model to understand the relationship between the laser fluence and the diameter of gold microspheres and give as follow.

A laser energy Qabs that gold nanoparticles can absorb from a single laser pulse is equal to

Eabs=J(τ)σabsλ                            (1)

In this equation, J(τ) is laser fluence dependent on pulse to pulse time τ, σabsλ is the absorption cross section of gold nanoparticles, which is related to laser wavelength λ and refractive index of surrounding medium nm. The laser energy Eabs absorbed by the gold nanoparticles is used to heat the lattice, and when the temperature reaches the melting or boiling point of the lattice (1336 and 3150 K respectively), the gold nanoparticles will melt or evaporate, as follow.6

Eabs=ρpπdp36T0TmCpsTdT+ΔHm+TmTbCplTdT

=ρpπdp36(HTm-HT0)+ΔHm+(HTb-HTm)                   (2)

Here, ρp is density of gold nanoparticles, dp is diameter of gold nanoparticles, T0, Tm, Tb are room temperature, melting temperature and boiling temperature respectively, Cps and Cpl are the gold nanoparticles heat capacities in solid and liquid states, ΔHm is the enthalpy of melting, and HT-HT0 is the relative enthalpy. Considering that the evaporation phenomenon can be ignored in this experiment due to the small fluence (<30 mJ cm-2) and short time (<10 s), Equation (2) can be simplified as follow.

Eabs=ρpπdp36(HTm-HT0)+ΔHm                (3)

Integrated with the equation (1), the general relationship between the size of gold nanoparticles (dp) and laser fluences (J) is given in equation (4).

J(τ)σabsλ=ρpπdp36(HTm-HT0)+ΔHm             (4)

Therefore, given the laser fluence, there is a threshold for the size of the gold microspheres that can be melted by one pulse. At the same time, because the quenching time is much smaller than the interval between the two pulses, the energies of the two lasers cannot be accumulated, so such a threshold cannot be broken even if the number of the pulse output is increased. This result is consistent with our experimental phenomenon.

3. Theoretical diameter decrease from gold colloidosomes into gold microspheres

Since gold colloidosomes are assembled as a hexagonally close-packed model, the distance change of colloidosomes into microspheres is calculated using close packing model. The close-packed structure can be reduced to the ordered arrangement of an infinite number of identical cells, so we only need to study the space utilization of a single cell. As shown in the Figure S7a, the unite cell shape of the close-packed structure is hexagonal prism. The volume of the prism is the volume of the unite cell (equivalent to the volume of the colloidsome).

3.1 The volume of gold microsphere

Assuming that the size of each gold particle is uniform and the radius is r, then the volume of a gold particle is . Each gold particle on the 12 vertices of the unite cell is equally divided by six adjacent unite cells, and each unite cell is divided by 1/6, so the number of particles divided by each vertex of a crystal cell is one. So the total number of particles divided by a cell is . Each gold particle on the upper bottom surface and the lower bottom surface is equally divided by two adjacent unite cells, so the number of gold particles divided by the upper bottom surface and the lower bottom surface of a cell is . The three gold particles in the middle are owned by this cell alone.

Therefore, this unite cell contains a total of six gold particles, and the total volume of gold particles (equivalent to the volume of gold microsphere) is .

3.2 The volume of gold colloidosomes

The shape of the unite cell of gold colloidosome is prismatic, assuming the base area is S and the height is H. So, the volume of the cell is . The top view of the base is shown in Figure S7b, and the area is . As shown in Figure S7c, the three gold particles of the second layer are represented by blue circles. The central gold particle of the bottom surface and the first gold particle of the second layer are observed. The center distance of the two gold particles is obviously 2r, but the height differenceis unknown. The horizontal distance is (according to the Pythagorean theorem). As shown in Figure S7d, the between the bottom gold particle and the middle gold particle can be calculated according to the Pythagorean theorem, that is

The diameter conversion rate () of gold colloidosomes to gold microspheres. It is assuming that the volume conversion rate of colloidosome into microsphere isunder the close pecking model.

In order to facilitate experimental statistics, the volume conversion rate was converted to direct conversion rate, therefore,

Therefore, in the ideal close-packed case, .

Figure S1. (a) The absorption spectrum of gold nanosphere. (b) TEM image of raw gold nanoparticles. (c) SAED pattern of raw gold nanosphere. (d) The histogram of size statistics of the raw gold nanoparticles.

Figure S2. (a) Digital photograph of honeycomb microhole PS array film. (b) The diffraction pattern of the 2D honeycomb microhole-array film irradiated by a 633 nm laser pen (c) SEM image of honeycomb microhole array PS film. (d) SEM image of honeycomb microhole array PS film at a cross-sectional view, and the inset showing the high-magnification SEM image of microhole.

Figure S3. Low-magnification SEM image of gold colloidosomes, and inset showing the high-magnification SEM image of gold colloidosome.

Figure S4. SEM images of gold colloidosomes treated with different laser pulses.

Figure S5. Low-magnification SEM image of gold microspheres prepared based on layer-by-layer melting mechanism.

Figure S6. The diameter of gold microspheres exhibits a coefficient of variation (CV) of 4.03%.

Figure S7. (a) Schematic diagram of unite cell of the close packing model. (b) Top view of six bottom gold particles in a close packing model. (c) Top view of six bottom gold particles and three interlayer gold particles. (d) Side view of bottom intermediate gold particle and upper gold particle.

Figure S8. (a) SEM image of gold colloidosomes after irradiated when laser fluence is 30.0 mJ·cm-2. (b) SEM image of gold colloidosomes after irradiated when laser fluence over 50.0 mJ·cm-2.

Figure S9. (a) TEM image of gold octahedrons. (b) The histogram of size statistics of gold octahedrons. (c) TEM image of gold bipyramids. (d) The histogram of size statistics of gold bipyramids. (e) TEM image of nonuniform gold nanoparticles. (f) The histogram of size statistics of nonuniform gold nanoparticles.

Figure S10. (a) Low-magnification SEM image of the gold colloidosomes with gold octahedrons, and inset showing the high-magnification SEM image of the gold colloidosomes. (b) Low-magnification SEM image of the gold microspheres and inset showing the high-magnification SEM image of the gold microsphere.

Figure S11. (a) Low-magnification SEM image of the gold colloidosomes with gold bipyramids, and inset showing the high-magnification SEM image of the gold colloidosomes. (b) Low-magnification SEM image of the gold microspheres and inset showing the high-magnification SEM image of the gold microsphere.

Figure S12. (a) Low-magnification SEM image of the gold colloidosomes with nonuniform gold nanoparticles, and inset showing the high-magnification SEM image of the gold colloidosomes. (b) Low-magnification SEM image of the gold microspheres and inset showing the high-magnification SEM image of the gold microsphere.

Figure S13. (a-c) The simulated 2D electromagnetic filed distribution of gold microspheres. (e-g) The calculated cross sections of absorption, scattering and extinction of gold microspheres. (the diameter of gold microsphere is 300, 375 and 500 nm)

Figure S14. The calculated cross sections of absorption, scattering and extinction of gold colloidosomes when environmental medium is 1-butanol (the diameter of gold colloidosomes is 450 nm).

Figure S15. The calculated temperature of substrate, colloidosomes and gold NP union as a function of time when irradiated by laser (the diameter of gold colloidosomes is 450 nm, environmental medium is 1-butanol).

Reference

1.	Zhang T, Li X, Li C, Cai W, Li Y. One-Pot Synthesis of Ultrasmooth, Precisely Shaped Gold Nanospheres via Surface Self-Polishing Etching and Regrowth. Chem Mater 33, 2593-2603 (2021).

2.	Liu D, Aleisa R, Cai Z, Li Y, Yin Y. Self-assembly of superstructures at all scales. Matter 4, 927-941 (2021).

3.	Olmon RL, et al. Optical dielectric function of gold. Phys Rev B 86, 235147 (2012).

4.	Fan J, Liu S, Song F, Wang X. Measurements of the thermal conductivity of three pure alcohols and their binary mixtures with methyl myristate component of biodiesel. Thermodynamics 142, 106009 (2020).

5.	Xu Y, Fan Y, Qing YM, Cui TJ, Lei D. A generalized method for calculating plasmoelectric potential in non-Mie-resonant plasmonic systems. Nanophotonics 11, 2453-2464 (2022).

6.	Pyatenko A, Wang H, Koshizaki N, Tsuji T. Mechanism of pulse laser interaction with colloidal nanoparticles. Laser & Photonics Reviews 7, 596-604 (2013).