Supplementary Information

Miniaturized on-chip spectrometer enabled by electrochromic modulation

Menghan Tian,1,2 Baolei Liu,1,2* Zelin Lu,1 Yao Wang,1 Ze Zheng,1 Jiaqi Song,1 Xiaolan Zhong,1* and Fan Wang1*

1 School of Physics, Beihang University, Beijing, 100191, China

2 These authors contributed equally to this work.

*Correspondence: liubaolei@buaa.edu.cn; zhongxl@buaa.edu.cn; fanwang@buaa.edu.cn

Table of contents:

S1. The principles of electrochromic materials.

S2. The electrochromic performance of ECD.

S3. Transmission spectra in CIE color space diagrams.

S4. Example reconstructions under different detection modes.

S5. Schematic of the optical setup.

S6. Photo of the miniaturized on-chip spectrometer.

- The principles of electrochromic materials

Tungsten oxide (WO3) is a cathodic electrochromic material with high optical transmission contrast and excellent electrochromic stability. As a cathodic electrochromic material, the WO3 film changes from transparent bleached state to blue colored state under the action of dual insertion of cations and electrons. It reversibly returns to the transparent state when applying reverse voltage and the ions and electrons are extracted. The basic chemical reaction equation of the electrochromic process can be expressed as [1]:

WO3|bleached+xM++xe-   MxWO3|colored,            (1)

where M+ represents the electrolyte ion, e- represents the electron, and x represents the number of moles of the embedded ion. The coloring mechanism of WO3 has long been highly controversial, and the most accepted theory is that WO3 and the embedded ions can generate MxWO3 with a tungsten-bronze structure through reversible reaction. In contrast, the spectral absorption during the electrochromic process arises from the charge transfer or polariton transition between W ions of different valence states.

Nickel oxide is an anode electrochromic material, the ion and electrons embedding process is the bleaching process, showing a colorless transparent state; and the ion extracting process is the coloring process, which usually shows a brown or brown-black state. Nickel oxide films may involve multiple crystalline phases in the electrochromic process. Standard nickel monoxide (NiO) has a salt-rock lattice, with a lattice constant of 0.4178 nm and a single-crystal NiO density of 6.67 g-cm-3. However, it is more difficult to obtain pure NiO, and the oxygen content is usually high. This oxygen leads to vacancies in Ni2+, which is why nickel oxide materials generally exhibit p-type semiconductor characteristics. Nickel oxide films can also have good electrochromic effects in non-aqueous electrolytes, such as LiClO4-PC solution, and the following reactions are generally accepted at present [2-4]:

Liα0Ni1-x1Ocolored+α1Li++α1e-↔Li(α0+α1)Ni1-x2O(bleached),	(2)

Li(α0+α1)Ni1-x2O(bleached)↔ Liα2Ni1-x3Ocolored+α3Li++α3e-,	(3)

where α0+α1=α2+α3, the transition between Ni2+/Ni3+ alters the absorption of visible light, which is macroscopically manifested as a change of color or transmittance.

- The electrochromic performance of ECD.

Figure S1. The CV curves of ECD at 10, 30, 50, 80, and 100 mV/s scanning speeds, respectively.

Figure S2. The relationship between area energy density and sweep velocity.

Figure S3. The transmittance evolution curve of ECD, by applying a square wave voltage range in -1.5V and 1.8V.

- Transmission spectra in CIE color space diagrams.

Figure S4. Transmittance spectra of ECD (bleached state) at different polarization angles in corresponding CIE color space diagrams.

- Example reconstructions under different detection modes

Figure S5. Reconstructions of the spectrum with two mixed peaks under different detection modes.

- Schematic of the optical setup

Figure S6. Schematic of the optical setup for calibration and measurement of the ECOS.

- Photo of the miniaturized on-chip spectrometer

Figure S7. Photo of the electrochromic computational on-chip spectrometer (ECOS).

Reference:

- Granqvist C G. Electrochromic tungsten oxide films: Review of progress 1993–1998. Solar Energy Materials and Solar Cells, 2000, 60(3): 201-262.

- Passerini S. The Intercalation of Lithium in Nickel Oxide and Its Electrochromic Properties. Journal of The Electrochemical Society, 1990, 137(10): 3297.

- Campet G, Morel B, Bourrel M, et al., Electrochemistry of nickel oxide films in aqueous and Li+ containing non-aqueous solutions: an application for a new lithium-based nickel oxide electrode exhibiting electrochromism by a reversible Li+ ion insertion mechanism[J]. Materials Science and Engineering: B, 1991, 8(4): 303–308.

- Lin Y-S, Chen P-W, Lin D-J, et al., Electrochromic performance of reactive plasma-sputtered NiOx thin films on flexible PET/ITO substrates for flexible electrochromic devices[J]. Surface and Coatings Technology, 2010, 205: S216–S221.