Supplementary Information

Aluminum-doped carbon dots for the simultaneous selective detection of five tetracycline antibiotics

Chaojie Yu, Qinxing Sun, Zongzhen Wang, Mengxue Sun, Xiang Xu,* Weina Li*

College of Chemistry and Pharmaceutical Sciences, Qingdao Agricultural University, Qingdao, 266109, China.

* Correspondence to: Qingdao Agricultural University, 700 Changcheng Road, Qingdao 266109, China.

*Corresponding author

E-mail: wnli@qau.edu.cn (W. N. Li), rainerxu@163.com (X. Xu)

Table of Contents

Fig. S1. The relationship between the fluorescence intensity of Al-CDs and (a) MC, (b) TC, (c) OTC, (d) DOC and (e) CTC at a concentration of 0-500 μM.........................…………………………………………..………...…...…S-3

Fig. S2. Detection of (a) MC, (b) TC and (c) DOC seawater samples by Al-CDs....………………………………………………………….………...………S-3

Table S1. Fluorescence lifetime of Al-CDs and Al-CDs+TC……….………..…… S-3

Table S2. Determination of MC, TC, DOC in seawater samples using Al-CDs through fluorescence intensity.…………………………………………....……….. S-3

Fig. S1. The relationship between the fluorescence intensity of Al-CDs and (a) MC, (b) TC, (c) OTC, (d) DOC and (e) CTC at a concentration of 0-500 μM.

Fig. S2. Detection of (a) MC, (b) TC and (c) DOC seawater samples by Al-CDs.

Table S1. Fluorescence lifetime of Al-CDs and Al-CDs+TC.

| Sample | τ1 (ns) | A1% | τ2 (ns) | A2% | τave (ns) |
| --- | --- | --- | --- | --- | --- |
| Al-CDs | 2.004 | 46.2 | 8.112 | 53.8 | 5.29 |
| Al-CDs+TC | 1.567 | 39.7 | 7.310 | 60.3 | 5.03 |

Table S2. Determination of MC, TC, DOC in seawater samples using Al-CDs through fluorescence intensity.

| Unit | Added (μM) | Fluorescence spectra |  |  |
| --- | --- | --- | --- | --- |
|  |  | Detected (μM) | Recovery (%) | RSD (%) |
| MC | 20 | 22.51 | 112.55 | 2.43 |
|  | 60 | 56.66 | 94.43 | 2.65 |
|  | 100 | 92.83 | 92.83 | 2.12 |
|  | 120 | 113.89 | 94.95 | 2.87 |
| TC | 20 | 24.41 | 122.05 | 3.02 |
|  | 60 | 69.11 | 115.18 | 3.46 |
|  | 100 | 97.41 | 97.41 | 2.98 |
|  | 120 | 123.49 | 102.91 | 2.31 |
| DOC | 20 | 18.93 | 94.65 | 2.87 |
|  | 60 | 59.89 | 99.82 | 1.98 |
|  | 100 | 92.74 | 92.74 | 2.45 |
|  | 120 | 112.63 | 93.86 | 3.36 |