Electronic Supplementary Information (ESI)

Construction of artificial metalloenzymes

by protein refolding

Guangnan Ou a, b,*, Biyan Hec

a Department of Biological Engineering, Jimei University, Xiamen 361021, Fujian, China.

b Fujian Provincial Key Laboratory of Food Microbiology and Enzyme Engineering, Xiamen  361021, Fujian, China.

c Department of Environmental Engineering, Jimei University, Xiamen 361021, Fujian, China.

Ⅰ. General	2

Ⅱ. UV-vis absorption spectroscopy measurements	2

Ⅲ. Circular dichroism spectroscopy measurements	2

Ⅳ. Peroxidase activity assay	3

Fig. S1  DichroWeb fitting for BSA with a NRMSD value of 0.018.	3

Fig. S2  DichroWeb fitting for Hem+BSA with a NRMSD value of 0.018.	4

Fig. S3  DichroWeb fitting for rnBSA with a NRMSD value of 0.021.	4

Fig. S4  DichroWeb fitting for Hem-BSA with a NRMSD value of 0.018.	5

Fig. S5  The initial rate of oxidation of guaiacol catalyzed by Hem+BSA.	6

Fig. S6  The initial rate of oxidation of guaiacol catalyzed by Hem-BSA.	6

Fig. S7 Lineweaver–Burk plots of the double reciprocal of the Michaelis-Menten equation of Hemin	6

References	7

Ⅰ. General

Horseradish peroxidase, hemin, and guaiacol were purchased from Sigma-Aldrich. BSA was purchased from China National Pharmaceutical Group Co., Ltd. (Sinopharm). All other chemicals and reagents were of analytical grade.

Ⅱ. UV-vis absorption spectroscopy measurements

The UV-vis absorption spectra were obtained using an UNICO 2800 UV-vis spectrophotometer equipped with a thermostated cell holder.

Ⅲ. Circular dichroism spectroscopy measurements

Circular Dichroism (CD) measurements were carried out on an Applied Photophysics (UK) (Model: CIRASCAN) spectropolarimeter equipped with a Peltier temperature controller. All the CD measurements were performed at 25℃ with an accuracy of ± 0.1℃. Spectra were collected with a scan speed of 200 nm min-1 and with a spectral bandwidth of 1 nm. Each spectrum was the average of two scans. Secondary structure (Far-UV CD) was measured over the wavelength range of 190-250 nm using a 0.1 cm path length cuvette. Phosphate buﬀer solutions were subtracted from all the measurements. The results were expressed as mean residue ellipticity (MRE) in    deg cm2 dmol-1 which is deﬁned as

MRE=θobsmdegMnlC

where θobs is the CD in millidegrees, M is molecular weight of the protein in g/dmol, n is the number of amino acid residues (583 in the case of BSA), l is the path length (0.1 cm) of the cuvette, and C is the concentration of the protein in g/L.

The quantitative determination of helix, sheet, and other secondary structure contents of proteins based on their CD spectra was calculated on analysis website, DichroWeb (located at: http://dichroweb.cryst.bbk.ac.uk) using CONTINLL as the algorithm with ridge regression methods and dataset 7.[1]

The “goodness-of-fit” parameter is the Normalised Root Mean Squared Deviation (NRMSD), which provides a means of evaluating the difference between the experimental and calculated spectra. It is defined as:

NRSD=λ(θexp-θcalc)2λ(θcalc)2

where θexp and θcalc are the experimental and back-calculated ellipticities, respectively, at each data point in the spectrum, with lower values indicating a closer match between experimental and reference data. NRMSD values for analyses using CONTINLL would be a very good fit if the NRMSD values are less than 0.03.[2]

Ⅳ. Peroxidase activity assay

Peroxidase activity was measured by following the H2O2-dependent oxidation of guaiacol at 470 nm. Guaiacol stock solutions (1.0 mmol/L) were prepared by dissolving guaiacol in 0.1 mol/L buffer. H2O2 stock solutions (150 mmol/L) were prepared daily by appropriate dilution of 30% H2O2 in distilled water. The assay was performed by mixing 500 μL guaiacol stock solutions with 15 μL of catalyst solution (final concentration 1.0 μmol/L). In the case of temperature dependence experiments, the mixture was then incubated at the designated temperature for 10 min. The reaction was started by adding 15 μL of 150 mmol/L H2O2. The initial velocity (v0) of the oxidation of guaiacol was determined from linear plotting of the absorbance versus time, using an extinction coefficient of 2.66×104 (mol/L)-1/cm for guaiacol-derived oxidation product.

All assays were carried out at room temperature except the temperature dependence experiments using a UV-Vis spectrophotometer (Unico, UV2800) which cell was connected to a thermostat.

Fig. S1  DichroWeb fitting for BSA with a NRMSD value of 0.018.

Fig. S2  DichroWeb fitting for Hem+BSA with a NRMSD value of 0.018.

Fig. S3  DichroWeb fitting for rnBSA with a NRMSD value of 0.021.

Fig. S4  DichroWeb fitting for Hem-BSA with a NRMSD value of 0.018.

Fig. S5  The initial rate of oxidation of guaiacol catalyzed by Hem+BSA.

Fig. S6  The initial rate of oxidation of guaiacol catalyzed by Hem-BSA.

Fig. S7 Lineweaver–Burk plots of the double reciprocal of the Michaelis-Menten equation of Hemin

References

- N. Sreerama, R.W. Woody, Anal. Biochem., 2000, 287, 252-260.

- A. J. Miles, S. G. Ramalli, B. A. Wallace, Protein Sci., 2022, 31, 37-46.