Supporting Information

Targeted glomerular mesangium transfection by antifibrotic gene nanocarriers inhibits kidney fibrosis and promotes regeneration

Yifan Tai, Zhen Liu, Yanrong Wang, Xinyan Zhang, Ruifang Li, Jiangyue Yu, Yao Chen, Lili Zhao, Jia Li, Xueyuan Bai, Deling Kong*, Adam C. Midgley*

Supplementary Experimental Section/Methods

Animal Study Design: Randomized allocation of mice was determined by the researcher first randomly assigning numbers to mice, and then applying the Excel ‘Rand()’ function followed by descending sorting. Mice were then sequentially allocated into each treatment group. Treatment orders were randomized using the same method at the time of surgery and at the time of systemic administration. To ensure blinding, different researchers conducted animal experiments, histology, gene/protein analysis, and data analysis. G*Power (software version 3.1.9.6) was used to determine total animal sample sizes for the hypothesized substantial antifibrotic effect of interventions in renal fibrosis models, according to Cohen’s d standardized mean difference.

Fourier Transform Infrared Spectroscopy (FTIR): Attenuated total reflectance (ATR)-FTIR (TENSOR II; Bruker, Billerica, MA, US) was used to analyze the composition and properties of M-HA, triserine, and HS. The scan range was set to 4000–400 cm−1 with 4 cm−1 resolution. The indicated characteristic peaks were determined in the different analyzed material components to identify the successful conjugation between M-HA and triserine to yield HS.

Plasmid DNA cloning: Amplifications of cloned pDNA-BMP7 and pDNA-EGFP were performed by transforming one-shot competent Escherichia coli before growth on ampicillin containing agar plates. Single colonies were selected and amplified according to AxyPrep Plasmid Maxiprep Kit instructions (Axygen, Corning, Union City, California, US). Cloned plasmids were digested with the appropriate endonucleases and sized by 1% agarose gel flat-bed electrophoresis before band digestion, purification, and DNA sequencing to confirm the inclusion of the inserted open reading frames.

DNA encapsulation efficiency: The remaining pDNA concentration was determined after each pDNA absorption step in the LbL assembly procedure, by measuring the OD of 2 µL supernatant after centrifugation and removal of the NP (15,000 × g, 30 min, 4°C). The encapsulated pDNA concentration was measured using a BioDrop µLITE+ (BioDrop, Cambridge, UK) and expressed as a percentage of the initial 250 µg pDNA solution.

DNA protection and release assays: A suspension of 1 µg mL-1 NP sample was incubated with 10 U DNase I (Thermo Fisher Scientific), 1 U chitosanase (Merk-Millipore), 10 µg mL-1 hyaluronidase (Sigma-Aldrich), or both chitosanase and hyaluronidase, at 37°C for 90 min. DNase I was inactivated by heating to 65°C for 10 min. The solutions were mixed with DNA loading buffer and DNA release/degradation were assessed by 1% agarose gel flat-bed electrophoresis. Gels were visualized and photographed using a Tanon 2500 Gel Imaging System (Tanon, Shanghai, China). If the pDNA remained encapsulated within NPs, the pDNA could be visualized entrapped within the loaded wells, as NPs were unable to migrate through the gel and intact NPs protected against pDNA release. Similarly, 1 µg mL-1 NP freshly synthesized NP or those stored for 1-month were mixed with DNA loading buffer and DNA release/degradation were assessed as above.

Cytotoxicity and proliferation assays: Cells were seeded into 12-well culture plates at a density of 2.5 × 104 and when cultures had reached 90% confluency (cytotoxicity assays) or 50% confluency (proliferation assays), the culture medium was replaced with fresh serum-free F12K or serum-free DMEM/F12 for 48 h (growth arrest). Cells were incubated with the indicated treatments for 0, 24, 48, and 72 h. CCK-8 (Cell Counting Kit-8; Beyotime, Haimen, China) assays were performed as follows: 10% of CCK-8 reagent was added to the target wells (90% F-12K or 90% DMEM). CCK-8 utilizes water-soluble tetrazolium salt-SST-8 (WST-8), which is reduced by dehydrogenases of cells, to give soluble orange colored formazan. The amount of the formazan dye generated by dehydrogenase is directly proportional to the number of living cells. At each time point, cells were incubated with CCK-8 reagent for 4 h before the medium was aliquoted into wells of a 96-well plate and absorbance was measured at 450 nm wavelength, using a Bio-Rad optical plate reader (Hercules, California, US). The wells were replenished with fresh medium containing the indicated treatments for the subsequent analyses.

Assessment of cellular route of nanoparticle uptake: Mesangial cells and PTECs were grown on 24-well cell slides and incubated with serum-free medium containing Cy5@PCH-NP or Cy5@PCHS-NP. After 24 h, cells were fixed and immunostained for EEA-1 or LAMP1 to visualize Cy5 co-localization with endosomes and lysosomes, respectively. Phalloidin staining was used to better visualize and differentiate the mesangial cells. A laser confocal scanning microscope was used for visualization and image capture. Details of the antibodies used are provided in Table S2.

The switch in NP uptake route into PTECs was further investigated by pre-treatment of 80% confluent growth-arrested PTECs with Hank’s Balanced Salt Solution (HBSS, pH 7.4) for 1 h, followed by HBSS containing 370 nм genistein, 1mм lysozyme, 100 µм amiloride, 100 µм chlorpromazine, 100 µg mL-1 free M-HA, or 100 µg mL-1 free HS for 4 h and in the presence of 10 µg mL-1 Cy5@PCH-NP or Cy5@PCHS-NP. The culture solution was removed, and cells were gently washed with HBSS three times. Subsequently, cells were lysed in 300 µL of lysis buffer (100 mм Tris/HCl, 2 mм EDTA, 0.05% Triton X-100, pH 7.8). The amount of Cy5 that had been internalized was measured using a Tecan Spark multimode microplate reader (Tecan, Männedorf, Switzerland) at an excitation wavelength ~683 nm and emission wavelength ~703 nm.

Biodistribution and safety evaluation: The major organs were harvested at the experimental endpoints, halved or quarters, and fixed in 10% formalin overnight. Following gradient dehydration, organ samples were embedded in paraffin, cut to 6-μm thick sections, and mounted on glass microscopy slides. Sections were stained with H&E to observe potential changes to tissue architecture or stained by Von Kossa to observe potential presence of calcification.

Supplementary Figures

Figure S1. Synthesis of conjugated HA-triserine. (A) Pathway for the synthesis of M-HA backbone modification with (cys)-Triserine peptide motifs. Maleimide (MAL) groups react with sulfhydryl (SH) groups in water at pH 7 via Michael addition, forming a stable thioether bond. HA-MAL was linked with the sulfhydryl group of the cysteine (cys) attached to the Triserine peptide to yield HA-triserine (HS). (B) Confirmation of successful modification by FTIR, which showed double peaks of HS between 1600 and 1700 cm-1 (red plot), indicative of the loss of the (cys)-Triserine free thiol group (black plot) and conjugation to MAL-HA (blue plot).

Figure S2. Additional NP characterization. (A) TEM images of homogenously dispersed P-NP and PCHS-NP. (B) Zeta potentials measured before and after each subsequent layering step of the LbL assembly of PCHS-NPS-NP (s.d., n = 5). (C) Encapsulation efficiency of 250 µg pDNA per 10.7 mg NP mass. (D,E) DNA protection assays. (F) TEM images and (G) DLS analysis of hydrodynamic diameter of PCHS-NP before and after storage for 30 days (1 month) at 4 °C in PBS. (H) Agarose gel electrophoresis to determine DNA leakage after storage at 4 °C for 20 or 30 days (1 month). (I) Zeta potentials of freshly synthesized PCHS-NP and PCHS-NP after 30 days (1 month) of storage (s.d., n = 3). All data are representative of at least three independent experiments.

Figure S3. Cytocompatibility testing. The effects of PCHS-NP treatments at the indicated concentrations on (A) mesangial cell cytotoxicity and proliferation, and (B) PTEC cytotoxicity and proliferation over 3 days. All data are presented as the mean ± s.e.m. of at least three independent experiments. Statistical significance is indicated by *P≤0.05, **P≤0.01, ***P≤0.001, and ns=no significance, as indicated by Two-way ANOVA and Tukey’s post-hoc testing.

Figure S4. Verification of overexpressed rhBMP7 activity. The relative mRNA expression of BMP7 in (A) mesangial cells and (B) PTECs after treatment with PCHS-NP or Lipofectamine LTX (s.e.m., n = 3). Western blot analysis of BMP7, phospho-SMAD1/5, total SMAD1, and total SMAD5 protein production and relative densitometric quantification in (C) mesangial cells and (D) PTECs (s.e.m., n = 3). Immunoblots are representative of at least three independent experiments. Statistical significance is indicated by *P≤0.05, **P≤0.01, ***P≤0.001, and ns=no significance, as indicated by two-tailed Student’s t-test between independent data groups.

Figure S5. Cy5 encapsulation and assessment of cellular uptake of NP. (A) DLS and TEM of Cy5@P-NP. (B) Zeta potential of P-NP and Cy5@P-NP (s.d., n = 5). (C) Detection of fluorescence emission from Cy5@P-NP and Cy5@PCHS-NP. (D) Endosomal (EEA1) and lysosomal (LAMP1) localization of Cy5@PCH-NP and Cy5@PCHS-NP in mesangial cells and PTECs. (E) PTECs pre-incubated with various internalization inhibitors or competitors for 4 h before addition of Cy5@PCH-NP (s.e.m., n = 5) (F) PTECs pre-incubated with the indicated various internalization inhibitors or competitors for 4 h before addition of Cy5@PCHS-NP (s.e.m., n = 5). All images are representative of at least 5 independent experiments. Statistical significance is indicated by *P≤0.05, **P≤0.01, ***P≤0.001, and ns=no significance, as analyzed by One-way ANOVA and Tukey’s post-hoc testing.

Figure S6. In vitro assessment of fibrosis-related gene expression. Relative mRNA expression of profibrotic gene markers, ACTA2, COL1A1, COL3A1, FN1, and FN1 splice variant EDA-fibronectin in (A) mesangial cells and (B) PTECs treated with TGF-β1 or TGF-β1+PCHS-NP co-treatment (s.e.m., n = 5). Statistics are indicated as *P≤0.05, **P≤0.01, ***P≤0.001, and ns = no significance, as measured by One-way ANOVA with Tukey’s multiple comparison post-hoc test.

Figure S7. NP biodistribution safety evaluation. Representative (A) H&E and (B) Von Kossa staining of heart, liver, spleen, lung, and health kidney tissues evaluated at the experimental end points of each treatment. All tissues maintained an apparently healthy tissue structure without obvious signs of damage or calcification. Images are representative of n = 3 individual animals. Scale bars, 200 µm.

Figure S8. Evaluation of collagen types in whole kidney tissues. Western blot and quantifications for whole kidney tissue protein expression of collagens I, III, and IV (s.d., n = 3). Statistics are indicated as *P≤0.05, **P≤0.01, ***P≤0.001, and ns = no significance, as measured by One-way ANOVA with Tukey’s multiple comparison post-hoc test.

Figure S9. Anti-inflammatory effects of PCHS-NP treatments in vivo. (A) Immunocytochemistry staining for CD68 and iNOS to label macrophages and pro-inflammatory M1-like macrophages, respectively (representative of n = 5). Quantification of (B) CD68+ macrophages, and (C) iNOS+ M1-like macrophages (s.d., n = 5). (D) RT-qPCR analysis of the relative mRNA expression of pro-inflammatory markers, Tnfa, Tgfb1, and Il6 (s.d., n = 5). Statistics are indicated as *P≤0.05, **P≤0.01, ***P≤0.001, and ns = no significance, as measured by One-way ANOVA with Tukey’s multiple comparison post-hoc test.

Figure S10. Overexpression of BMP7 following PCHS-NP treatment leads to its production in the kidney for at least one week. (A) Western blot analysis of BMP7 in whole kidney tissue in sham groups (healthy control) and at 4 or 7 days after a single i.v. tail vein injection of PCHS-NP. Immunoblots for β-actin served as loading controls. (B) Immunofluorescence staining of BMP7 protein in the kidney cortex in sham groups (healthy control) and at 4 or 7 days after a single i.v. tail vein injection of PCHS-NP. Scale bar = 100 µm. All images are representative of three independent experiments. The results indicated that BMP7 was strongly expressed after 4 days, and this expression level dropped at 7 days but remained above control levels. Therefore, a rationale for weekly delivery of PCHS-NP was established.

Figure S11. Renoprotective effects of PCHS-NP treatments against FA-induced injury and fibrosis. (A) Representative whole kidney section and zoomed kidney section staining for α-SMA with quantification shown alongside (graphed data shown as ± s.d. of 8 kidney sections obtained from n = 4 mice). Scale bars = 2 mm, whole sections; 100 µm, zoomed sections. Statistics are indicated as ***P≤0.001, as measured by One-way ANOVA with Dunnett’s multiple comparison post-hoc test. (B) Western blot analysis of α-SMA, fibronectin, collagen IV, and SOX9 protein expression in whole kidney tissue obtained for indicated groups. Immunoblots for β-actin served as loading controls. Densitometric analysis is shown alongside (± s.d., n = 3). Relative mRNA expression of (C) profibrotic gene markers, Acta2, Fn1, Fn1 splice variant EDA-fibronectin, Col4a1, and Mmp9; (D) kidney injury markers, Havcr1 and Lcn2; (E) kidney health markers, Cdh1, Nphs1, and Nphs2; and (F) inflammatory markers, Tgfb1, Il6, Tnfa, and Nos2 in whole kidney tissue (± s.d., n = 4 separate tissue samples). Statistics are indicated as *P≤0.05, **P≤0.01, ***P≤0.001, and ns = no significance, as measured by One-way ANOVA with Tukey’s multiple comparison post-hoc test.

Figure S12. NP biodistribution safety evaluation after repeated intervention.  (A) Western blot analysis of BMP7 protein expression in tissues of major organs after each indicated treatment. Immunoblots for β-actin served as loading controls. The associated densitometric analysis is shown below each immunoblot (± s.d., n = 3). Statistics are indicated as *P≤0.05, **P≤0.01, ***P≤0.001, and ns = no significance, as measured by One-way ANOVA with Tukey’s multiple comparison post-hoc test. Representative images for (B) H&E staining of liver and (C) Von Kossa staining of liver and kidney tissues evaluated at the experimental end points of each treatment. Marginally but statistically significantly elevated liver expression of BMP7 in the RI group had no obvious effects on apparently healthy liver tissue structure, and both liver and kidney exhibited no signs of calcification. Images are representative of n = 3 individual animals. Scale bars, 200 µm.

Table S1. Custom primers for RT-qPCR.

| Target | Forward (5’3’) | Reverse (5’3’) |
| --- | --- | --- |
| mmu-Acta2 | CTGACAGAGGCACCACTGAA | ACAATACCAGTTGTACGTCCAGAG |
| mmu-Cdh1 | AACCCAAGCACGTATCAGGG | GAGTGTTGGGGGCATCATCA |
| mmu-Col4a1 | GGCCCTTCATTAGCAGGTGT | GTGAGGACCAACCGTTAGGG |
| mmu-EDA-Fn1 | GAATCCAGTCCACAGCCATT | TGAACACTGGGTGCTATCCA |
| mmu-Fn1 | ACGGTTTCCCATTACGCCAT | GGCACCATTTAGATGAATCGCA |
| mmu-Gapdh | AAGAGGGATGCTGCCCTTAC | TACGGCCAAATCCGTTCACA |
| mmu-Hmox1 | CAGAAGAGGCTAAGACCGCC | GCAGTATCTTGCACCAGGCTA |
| mmu-Il6 | TCTCTGGGAAATCGTGGAAATGA | GGTACTCCAGAAGACCAGAGGA |
| mmu-Kim1 | ACCCACTACATTTTGTCCCCA | GTGCCATTCCAGTCTGTAGGA |
| mmu-Mmp9 | GACTTTTGTGGTCTTCCCCA | AGCGGTACAAGTATGCCTCTG |
| mmu-Nfe2l2 | GCAACTCCAGAAGGAACAGG | AGGCATCTTGTTTGGCAATG |
| mmu-Ngal | GGAACGTTTCACCCGCTTTG | CATTGGTCGGTGGGGACAGA |
| mmu-Nos2 | CATGCTACTGGAGGTGGGTG | CATTGATCTCCGTGACAGCC |
| mmu-Nphs1 | TATCGCCAAGCCTTCACAGG | CAGCGAAGGTCATAGGGTC |
| mmu-Nphs2 | GTAGTGGACGTGGACGAGGTTC | CTTGATGCCTTCCTCTGGTCG |
| mmu-Tgfb1 | CCTGTCCAAACTAAGGC | GGTTTTCTCATAGATGGCG |
| mmu-Tnfa | ATAGCTCCCAGAAAAGCAAGC | CACCCCGAAGTTCAGTAGACA |
| hsa-ACTA2 | CCGGGACTAAGACGGGAATC | TTGTCACACACCAAGGCAGT |
| hsa-BAXF | CCCGAGAGGTCTTTTTCCGAG | CCAGCCCATGATGGTTCTGAT |
| hsa-BCL2 | GGTGGGGTCATGTGTGTGG | CGGTTCAGGTACTCAGTCATCC |
| hsa-BMP7* | GCTTCGTCAACCT[CA]GTGGAA | AACCGGAACTC[TC]CGATGGTG |
| hsa-CASP8 | TTTCTGCCTACAGGGTCATGC | TGTCCAACTTTCCTTCTCCCA |
| hsa-COL1A1 | GCCAAGACGAAGACATCCCA | GTTTCCACACGTCTCGGTCA |
| hsa-COL3A1 | GAGGATGGTTGCACGAAACA | TAGTCTCACAGCCTTGCGTG |
| hsa-EDA-FN1 | ACAGTCAGTGTGGTTGCCTT | TTCAGGTCAGTTGGTGCAGG |
| hsa-FN1 | AACAAACACTAATGTTAATTGCCCA | TCGGGAATCTTCTCTGTCAGC |
| hsa-GAPDH | TCGGAGTCAACGGATTTGGT | TGAAGGGGTCATTGATGGCA |
| hsa-HMOX1 | AAGACTGCGTTCCTGCTCAAC | AAAGCCCTACAGCAACTGTCG |
| hsa-KEAP1 | CTGGAGGATCATACCAAGCAGG | GGATACCCTCAATGGACACCAC |
| hsa-NFE2L2 | TCCAGTCAGAAACCAGTGGAT | GAATGTCTGCGCCAAAAGCTG |
| hsa-NQO1 | GAAGAGCACTGATCGTACTGGC | GGATACTGAAAGTTCGCAGGG |

*[NN] indicates species mismatch; N, human; N, mouse; primers also allow for amplification of mouse Bmp7.

Table S2. Antibodies and dilutions.

| Method | Target | Dilution | Source | Product Code |
| --- | --- | --- | --- | --- |
| Immuno-cytochemistry | α-SMA | 1:200 | Abcam | ab7817 |
|  | Fibronectin | 1:200 | Abcam | ab2413 |
|  | Collagen III | 1:100 | Abcam | ab184993 |
|  | F-actin (Phalloidin) | 1:200 | Solarbio | CA1620 |
|  | EEA1 | 1:200 | Abcam | Ab2900 |
|  | LAMP1 | 1:100 | Abcam | ab25630 |
|  | Goat anti-Rabbit（Alexa Fluor 488） | 1:200 | Invitrogen | A-11008 |
|  | Goat anti-Rabbit（Alexa Fluor 594） | 1:200 | Invitrogen | A-11037 |
| Western blot | α-SMA | 1:2,000 | Abcam | ab5694 |
|  | BMP7 | 1:1,000 | Proteintech | 12221-1-AP |
|  | β-actin | 1:5,000 | Bioss Antibodies | bs-0061R |
|  | Fibronectin | 1:1,000 | Abcam | ab2413 |
|  | Collagen I | 1:1,000 | Abcam | ab260043 |
|  | Collagen III | 1:2,000 | Abcam | ab184993 |
|  | Collagen IV | 1:2,000 | Abcam | ab6586 |
|  | SMAD1 | 1:1,000 | Proteintech | 10429-1-AP |
|  | SMAD5 | 1:2,000 | Proteintech | 12167-1-AP |
|  | SMAD1/5 (phospho) | 1:1,000 | Cell Signaling Technology | 9516T |
|  | SOX9 | 1:1,000 | Abcam | ab185230 |
|  | Goat Anti-Rabbit (HRP) | 1:2,000 | Cohesion Biosciences | CSA2115 |
|  | Goat Anti-Mouse (HRP) | 1:2,000 | Cohesion Biosciences | CSA2108 |
| Tissue immuno-fluorescence | BMP7 | 1:200 | Proteintech | 12221-1-AP |
|  | PDGFRα | 1:500 | Abcam | ab203491 |
|  | LRP2 | 1:200 | Abcam | ab236244 |
|  | F-actin (Phalloidin) | 1:200 | Solarbio | CA1620 |
|  | Ki67 | 1:200 | Abcam | Ab15580 |
|  | α-SMA | 1:1,000 | Abcam | ab7817 |
|  | SOX9 | 1:200 | Abcam | ab185230 |
|  | CD68 | 1:50 | Abcam | ab283654 |
|  | iNOS | 1:100 | Abcam | ab178945 |
|  | Goat anti-Rabbit（Alexa Fluor 488） | 1:200 | Invitrogen | A-11008 |
|  | Goat anti-Rabbit（Alexa Fluor 594） | 1:200 | Invitrogen | A-11037 |
| Immuno-histochemistry | α-SMA | 1:200 | Abcam | ab5694 |
|  | Fibronectin | 1:1,000 | Abcam | ab2413 |
|  | Collagen IV | 1:500 | Abcam | ab6586 |
|  | Goat Anti-Rabbit (HRP) | 1:200 | Cohesion Biosciences | CSA2115 |