# Supporting Information

Preparation and Characterization of Biodegradable Polyester/Natural Protein Electrospun Nanofiber with Wound Healing Activity

Chin-San Wu1,*, Shan-Shue Wang1 , Dung-Yi Wu2

1Department of Applied Cosmetology, Taiwan Steel University of Science and Technology, Kaohsiung City, Taiwan 82101, Republic of China

2Department of Materials Science and Engineering, Johns Hopkins University, Baltimore, MD 21218, USA

* Corresponding author. Tel: +886-7-6077685; Fax: +886-7-6077788;

E-mail address: cws1222@tsust.edu.tw,t50008@ tsust.edu.tw (C.-S. Wu)

Water absorption percentage

The water absorption percentage (W1%) was then calculated using the following formula, which provided the weight gain as a percent:

W1%= (Wb-Wa)Wa×100%                               (1)

Wa: The weight of the dry samples was measured and recorded.

Wb: After withdrawing a sample from the water, surface moisture was removed using clean paper, and the film mass was measured and recorded.

Table S1. Formulation composites support designations and compositions

| Sample code | Component |  |  |
| --- | --- | --- | --- |
|  | PCL (wt%) | PCL-g-MA (phr) | LP (wt%) |  |
| PCL | 100 | － | － |  |
| PCL/LP 5wt% | 95 | － | 5 |  |
| PCL/ LP 10wt% | 90 | － | 10 |  |
| PCL/ LP 15wt% | 85 | － | 15 |  |
| PCL/ LP 20wt% | 80 | － | 20 |  |
| MPCL | 100 | 10 | － |  |
| MPCL/ LP 5wt% | 95 | 10 | 5 |  |
| MPCL/ LP 10wt% | 90 | 10 | 10 |  |
| MPCL/ LP 15wt% | 85 | 10 | 15 |  |
| MPCL/ LP 20wt% | 80 | 10 | 20 |  |

PCL: polycaprolactone; MPBSL: modified PCL [(added compatibility maleic anhydride (MA) grafted PCL (PCL-g-MA)]; LP : larvae protein powder.

Table S2. Effects of larvae protein powder (LP) content on the tensile properties of polycaprolactone (PCL)/LP and modified PCL (MPCL)/LP nanofibers.

| LP | PCL/LP |  |  | MPCL/LP |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| (wt%) | E(MPa) | δ (MPa) | ε(%) | E (MPa) | δ (MPa) | ε(%) |
| 0 | 37.6±5.1 | 3.35±0.13 | 183.6±5.6 | 36.8±5.2 | 3.26±0.16 | 182.8±5.7 |
| 5 | 32.3±5.8 | 2.81±0.15 | 150.5±5.8 | 40.3±5.7 | 3.56±0.20 | 151.3±5.9 |
| 10 | 27.7±6.0 | 2.39±0.17 | 120.8±6.0 | 48.8±5.8 | 3.86±0.23 | 131.2±6.2 |
| 15 | 23.6±6.1 | 2.13±0.17 | 111.3±6.2 | 45.3±5.9 | 3.78±0.25 | 128.5±6.3 |
| 20 | 20.3±6.2 | 1.61±0.18 | 109.5±6.5 | 43.1±6.0 | 3.72±0.28 | 126.3±6.5 |

δ: tensile strength, ε: elongation at failure, E: Young's modulus.

Scheme S1 Chemical reaction of MPCL and preparation of the MPCL/LP nanofibers,

Figure S1. Fourier transform-infrared spectra of LP.