Table 1. The IR absorption bands of the salophen ligand and its complexes.

| Sample | ν(C=N) | ν(C-N) | ν(Phenolic C-O) | ν(M-O) | ν(M-N) |
| --- | --- | --- | --- | --- | --- |
| Salophen | 1611 | 1479 | 1275 | - | - |
| Ni (II) complex | 1604 | 1457 | 1339 | 458 | 543 |
| Zn (II) complex | 1615 | 1461 | 1324 | 437 | 532 |

Table 2. The absorption bands, the emission bands, Stock shift and flourescence  quantum yield of the salophen ligand and its complexes.

| Sample | λabs (nm) | λem (nm) | Δλs (nm) | ∅f |
| --- | --- | --- | --- | --- |
| Salophen | 211 268 336 | 555 | 341 | 0.1097 |
| Ni (II) complex | 265 292 377 473 | 425 | 171 | 0.0134 |
| Zn (II) complex | 246 302 404 | 529 | 225 | 0.1217 |

Table 3. The AC conductivity (σac) at 50 kHz, DC conductivity and hopping values of the pure PMMA film and PMMA LSCs.

| Sample | AC conductivity (σac) at 50 kHz (S m−1) | DC conductivity (Ω-1 cm-1) | Hopping Value |
| --- | --- | --- | --- |
| Pure PMMA | 1.82× 10−9 | 7.94 × 10-7 | 0.9 |
| Ni (II) complex/PMMA LSC | 1.15 × 10-8 | 1.42×10-6 | 0.82 |
| Zn (II) complex/PMMA LSC | 2.11 × 10-9 | 2.56×10-6 | 0.5 |

Table 4. The optical parameters, and the first order rate constant of the pure PMMA film and PMMA LSCs before and after exposure to direct sunlight for 8 hrs.

| Sample | λabs (nm) | λem (nm) | Δλs (nm) | ∅f | Refractive index | Transmittance at 650nm | K ×10-2 (min-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pure PMMA | 220 | 540 | 320 | 0.00485 | 2.007 | 91.2% | - |
| Ni (II) complex/PMMA LSC (before) Ni (II) complex/PMMA LSC (after) | 260 264 | 475 438 | 215 219 | 0.01733 0.0102 | 2.15 2.14 | 89.8% 89.8% | - 0.011 |
| Zn (II) complex/PMMA LSC (before) Zn (II) complex/PMMA LSC (after) | 256 260 | 470 360 481 | 214 221 | 0.0833 0.0405 | 2.12 2.12 | 90.4% 90.4% | - 0.009 |

Table 5. The Urbach energy, direct and indirect optical bandgaps of the pure PMMA and PMMA LSCs before and after exposure to direct sunlight for 8 hrs.

|  | Direct bandgab |  |  |  |  | Indirect bandgab |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample | Eg1 | Eg2 | Eg3 | Eg4 | Eg5 | Eg1 | Eg2 | Eg3 | Eg4 | Eu |
| Pure PMMA | 4.9 | - | - | - | - | 4.8 | - | - | - | 0.448 |
| Ni (II) complex/PMMA LSC (before) Ni (II) complex/PMMA LSC (after) | 3 2.9 | 3.4 3.4 | 4.02 4 | 4.22 - | - - | 2.8 2.7 | 3 3.55 | 3.64 - | 3.7 - | 4.1996 3.406 |
| Zn (II) complex/PMMA LSC (before) Zn (II) complex/PMMA LSC (after) | 3.56 3.59 | 3.7 3.65 | 4.18 4.16 | 4.22 4.22 | 4.38 4.3 | 3.4 3.3 | 3.88 3.75 | 3.92 3.9 | 4.06 4 | 1.254 1.1626 |

Table 6. Photocurrent density–voltage parameters of the Silicon solar cell befor and after coupling with PMMA LSCs.

| Sample | Isc (A/cm-2) | Voc (V) | Pout (w) | FF | ɳ(%) | ɳ(relative)% |
| --- | --- | --- | --- | --- | --- | --- |
| Without the collectors | 0.06072 | 0.549 | 0.03333 | 0.52 | 8.6686 | - |
| With Ni (II) complex/PMMA LSC | 0.156 | 0.552 | 0.086112 | 0.303 | 13.0459 | 50.496% |
| With Zn (II) complex/PMMA LSC | 0.166 | 0.545 | 0.09047 | 0.291 | 13.16339 | 51.581% |