Supplementary Information

Table S1  List of single metal catalysts used to screen the active components.

| Catalyst | X6-HCM/% | SCPL/% | YCPL/% |
| --- | --- | --- | --- |
| TiO2 | 73.7% | 5% | 3.7% |
| Ru/TiO2 | 93.6% | 13.4% | 12.5% |
| Rh/TiO2 | 70.5% | 2.7% | 1.9% |
| Pd/TiO2 | 72.3% | 9.3% | 6.7% |
| Pt/TiO2 | 72.7% | 10.0% | 7.3% |
| Cu/TiO2 | 77.0% | 1.8% | 1.4% |
| Co/TiO2 | 77.7% | 3.2% | 2.5% |

Reaction conditions: 6-HCM (1.5 mmol), catalyst (0.05 g), H₂O (10 mL), NH₃·H₂O (5 mL), 250 °C, 5 h, 1 MPa N2.

Figure S1

Analysis of LC-MS.

Mass spectrometry analysis of the reaction solution showed that C6H12NO2 (6-hydroxycaproamide,6-HCM) corresponded to m/z = 132.1023[M+H]+ in the mass spectrum, closely aligning with the theoretical value of m/z = 132.1025. C6H11NO (caprolactam, CPL) exhibited a m/z = 114.0908[M+H]+ in the mass spectrum, which agreed well with the theoretical value of m/z = 114.0919. C6H9NO2 (adipimide) displayed a m/z = 128.0701[M+H]+, which was consistent with the theoretical value of m/z = 128.0712. C6H14N2O (6-aminocaproamide) demonstrated a m/z = 131.1176 [M+H]+, close to the theoretical value of m/z = 131.1184.

GC-MS of Valeramide and CPL.

Valeramide

m/z:101.1(98.4%)

Caprolactam，CPL

m/z:113.1(99.4%)

Figure S2  HRTEM images of the Ru5Co6/TiO2.