Table 1 Screening of reaction parameters for the synthesis of

| Entry | Catalyst (mg) | Solvent | Time (min) | Yield (%) |
| --- | --- | --- | --- | --- |
| 1 | Catalyst Free | Ethanol | 480 | 15 |
| 2 | CuCr2O4 (10) | Water | 100 | 60 |
| 3 | [Sipim]HSO4 (100) | Water (Reflux) | 75 | 75 |
| 4 | [Sipim]HSO4 (100) | Ethanol: Water (1:1) (Reflux) | 60 | 86 |
| 5 | NiFe2O3@SiO2-Pr-DBU nanocatalyst (5) | Ethanol | 50 | 80 |
| 6 | NiFe2O3@SiO2-Pr-DBU nanocatalyst (10) | Ethanol | 35 | 85 |
| 7 | NiFe2O3@SiO2-Pr-DBU nanocatalyst (10) | Water | 25 | 92 |
| 8 | NiFe2O3@SiO2-Pr-DBU nanocatalyst (15) | Water | 15 | 96 |

Table 2 Synthesis of dihydropyrano[3,2-c] chromenes using NiFe2O3@SiO2-Pr-DBU nanocatalyst. a, b