Abdallaoui, Doua; Meftah, Afak; Sengouga, Nouredine; Abdallaoui, Maroua; Labed, Madani (2024), “Enhancement of MAPb0.75Sn0.25I3 solar cell efficiency by doping HTL and ETL layers”, Mendeley Data, V1, doi: 10.17632/cprrvskd9h.1

Enhancement of MAPb0.75Sn0.25I3 solar cell efficiency by doping HTL and ETL layers

Doua Abdallaoui1, Afak Meftah1, Nouredine Sengouga1,*, Maroua Abdallaoui1, and Madani Labed2,3 *

1Laboratory of Semiconducting and Metallic Materials (LMSM), University of Mohamed Khider, BP 145 RP, 07000, Biskra, Algeria

2Department of Semiconductor Systems Engineering and Institute of Semiconductor and System IC, Sejong University Seoul 05006, Republic of Korea

3Institute of Semiconductor and System IC, Sejong University Seoul 05006, Republic of Korea

*Corresponding author: n.sengouga@univ-biskra.dz (Nouredine Sengouga) and madani@sejong.ac.kr (Madani Labed)

Table S1: Material parameters for different HTL layers.

| Parameter | CUSCN [1] |  | Cu2O [2] |
| --- | --- | --- | --- |
| Eg (eV) | 3.8 | 2 |  |
| χ (eV) | 1.7 | 3.2 |  |
| µn (cm2V-1s-1) | 0.0002 | 200 |  |
| µp (cm2V-1s-1) | 0.2 | 80 |  |
| εr | 10 | 7.11 |  |
| NA (cm-3) | - | 8×1013 |  |
| ND (cm-3) | 1×1018 | - |  |
| NC (cm-3) | 1.7×1019 | 2×1017 |  |
| NV (cm-3) | 2.5×1021 | 1.1×1019 |  |

Table S2 : The band gap values of the Cu2O and Cu2O1-xMx [3].

| Cu2O1-xMx | Eg |
| --- | --- |
| Cu2O | 2 |
| Cu2O0.88S0.12 | 2.098 |
| Cu2O0.88Se0.12 | 2.021 |
| Cu2O0.88Te0.12 | 1.875 |

Table S3: Material parameters for different ETL layers.

| Parameter | TiO2 [4] | ZnO [5] |
| --- | --- | --- |
| Eg(eV) | 3.2 | 3.373 |
| χ(eV) | 4.1 | 4.2 |
| μn(cm2V-1s-1) | 20 | 100 |
| μp(cm2V-1s-1) | 10 | 25 |
| εr | 13 | 9 |
| NA(cm-3) | 1×1018 | 1×1018 |
| ND(cm-3) | - | - |
| Nc | 2.2×1018 | 2.2×1018 |
| Nv | 1.8×1019 | 1.8×1019 |

Table S4: The band gap values and affinity of the ZnO and Zn1-xCuxO [6,7].

| Parameter | Eg (eV) | χ(eV) |
| --- | --- | --- |
| ZnO | 3.373 | 4.2 |
| Cu0.0278Zn0.9722O | 1.122 | 4 |
| Cu0.0417Zn0.9583O | 1.031 | 3.9 |

References

[1]	M.J. Patel, S.K. Gupta, P.N. Gajjar, Electronic structure and optical properties of β-CuSCN: A DFT study, Mater Today Proc 28 (2020) 164–167. https://doi.org/10.1016/j.matpr.2020.01.469.

[2]	A.A. Hssi, L. Atourki, N. Labchir, K. Abouabassi, M. Ouafi, H. Mouhib, A. Ihlal, A. Elfanaoui, S. Benmokhtar, K. Bouabid, Structural and optical properties of electrodeposited Cu2O thin films, Mater Today Proc 22 (2020) 89–92. https://doi.org/10.1016/j.matpr.2019.08.100.

[3]	B. Zhou, L. Luo, Y. Zhang, Y. Hu, Z. Xie, Z. Duan, X. Yang, First-principles study of the crystal structure, electronic and optical properties of Cu 2 O 1-x M x (M = S, Se, Te), Mater Res Express 9 (2022) 035902. https://doi.org/10.1088/2053-1591/ac5a32.

[4]	Yu.M. Evtushenko, S.V. Romashkin, N.S. Trofimov, T.K. Chekhlova, Optical Properties of TiO2 Thin Films, Phys Procedia 73 (2015) 100–107. https://doi.org/10.1016/j.phpro.2015.09.128.

[5]	A.K. Singh, S.K. Singh, Optical properties of ZnO, in: Nanostructured Zinc Oxide, Elsevier, 2021: pp. 189–208. https://doi.org/10.1016/B978-0-12-818900-9.00014-0.

[6]	Z. Ma, F. Ren, X. Ming, Y. Long, A.A. Volinsky, Cu-Doped ZnO Electronic Structure and Optical Properties Studied by First-Principles Calculations and Experiments, Materials 12 (2019) 196. https://doi.org/10.3390/ma12010196.

[7]	B. Hussain, A. Aslam, Bandgap and Electron Affinity Optimization of Zinc Oxide for n-ZnO/p-Si Single Heterojunction Solar Cell, in: 2017 IEEE 44th Photovoltaic Specialist Conference (PVSC), IEEE, 2017: pp. 2355–2357. https://doi.org/10.1109/PVSC.2017.8366196.