Supporting

Figure S1. SEM images and corresponding EDS element mapping for (a) Alg and (b) AlgNB  hydrogels, all the hydrogels show a visible internal porous structure; (c) Statistical results of the content of different elements, the atomic ratio of Mo to S is about 1 to 2, corresponding to MoS2.

Figure S2. The strategy of chemically bonding MoS2 to the AlgNB pre-gel preserves its uniform dispersion and stability, the MoS2 nanosheets begins to settle in the Alg pre-gel after the first day, and maintains a uniform dispersion in the AlgNB pre-gel over over seven days.

Figure S3. 5-Fu releasing behaviors. (a) UV-vis-NIR spectra of 5-Fu solutions with different concentration, which were diluted in different multiples; (b) 5-Fu Standard curve with linear correlation between UV-vis spectra peak intensity and 5-Fu concentration; UV-vis spectra for AlgNB hydrogel and AlgNB/MoS2 hydrogel without or

with NIR irradiation (1 W cm−2 , 10 min) at various time points of (c) 0.5 h, (d) 2 h, (e) 4 h, (f) 48 h, and (g) 72 h, respectively, all the groups were diluted in 50 multiples; (h) 5-Fu releasing measurement and NIR application strategy diagram.

Figure S4. In vivo thermal images of intra-tumorly injected AlgNB/MoS2 mice under 808 nm NIR irradiation (1.0 W/cm2 ) for varied durations.