Electronic Supporting Information

Magnetic BiFeO3 Nanoparticles: A Robust and Efficient Nanocatalyst for the Green One-Pot Three-Component Synthesis of Highly Substituted 3,4-Dihydropyrimidine-2(1H)-one/thione Derivatives

Safa Hanifi, Mohammad G. Dekamin*, Mohammad Eslami

Pharmaceutical and Biologically-Active Compounds Research Laboratory, Department of Chemistry, Iran University of Science and Technology, Tehran 16846-13114, Iran

Tel: +98-21-77240640-50; fax: +98-21-73021584; e-mail: mdekamin@iust.ac.ir

| Page | Contents |
| --- | --- |
| S1 | Title page |
| S4 | Figure S1. Typical examples of biologically active 3,4-dihydropyrimidine-2(1H)-one/thione derivatives (DHPMs/DHPMTs) |
| S4 | Figure S2. Synthesis of diverse 3,4-dihydropyrimidine-2(1H)-one/thione derivatives using the magnetic bismuth ferrite nanoparticles (BFO MNPs) in H2O: EtOH solvent system. |
| S4 | Figure S3. Schematic preparation of the BFO MNPs for the Green One-Pot Three-Component Synthesis of Highly Substituted 3,4-Dihydropyrimidine-2(1H)-one/thione Derivatives (DHPMs/DHPMTs) |
| S5 | Figure S4. 1H NMR of ethyl-6-methoxy-4-(3-nitrophenyl)2-oxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4b) |
| S6 | Figure S5. 1H NMR ethyl 4-(3,4-dichlorophenyl)6-methyl-2-oxo-1,2,3,40tetrahydropyrimidine-5-carboxylate (4f) |
| S7 | Figure S6. 1H NMR of ethyl 4-(3,4-dimethoxyphenyl)-6-methyl-2-oxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4l) |
| S8 | Figure S7. 1H NMR of ethyl 6-methoxy-2-oxo-4-(thiophen-2-yl)-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4q) |
| S9 | Figure S8. 1H NMR of ethyl 6-methyl-4-phenyl-2-thioxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4v) |
| S9 | Preparation of the magnetic bismuth ferrite nanoparticles (BFO MNPs) |
| S10 | Figure S9. Fourier-transform infrared spectrum (FT-IR) of bismuth ferrite nanoparticles (BFO MNPs) (a). FTIR spectrum of the as-synthesized spherical monodisperse Bi2O3 nanoparticles(b). FTIR graph of α-Fe2O3 calcined at 300oC. |
| S10 | Figure S10. SEM images of BiFeO3 nanoparticles; a) scale of 3 μm, b) scale of 500 nm. |
| S11 | Figure S11: EDS elemental mapping analysis of BFO MNPs. |
| S11 | Figure S112: Elemental analysis by energy-dispersive X-ray spectroscopy (EDS) for BFO MNPs. |
| S12 | Figure S13: X-ray diffraction pattern of BFO MNPs. |
| S12 | Figure S14: Hysteresis diagram of magnetic bismuth ferrite nanoparticles (BFO MNPs). |
| S12 | Table S1: Nitrogen adsorption-desorption isotherms of BFO MNPs. |
| S13 | Table S2. Exploring optimal conditions for the one-pot three-component Biginelli reaction involving benzaldehyde (1h), ethyl acetoacetate (2), and urea (3a).a |
| S14 | Table S3. Expanding the optimized method: synthesis of ethyl 4-(aryl/heteroaryl)-6-methyl-2-oxo-4,3,2,1-tetrahydropyrimidine-5-carboxylate using BiFeO3 magnetic nanoparticles for various aromatic and heteroaromatic carbonyl compounds.a |
| S17 | Figure S15. Proposed mechanism for the synthesis of 3,4 dihydropyrimidine-2(1H)-one/thione derivatives in the presence of magnetic bismuth ferrite nano catalyst (BFO MNPs). |
| S17 | Figure S16: The results of recyclability and reusability of the BFO MNPs nanoparticles in the model reaction. |
| S18 | Table S4. Comparison of the model reaction for the synthesis of Ethyl 6-methyl-2-oxo-4-phenyl-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4h) in the presence of BiFeO3 in terms of time and product yield with recent reports. |

Figure S1. Typical examples of biologically active 3,4-dihydropyrimidine-2(1H)-one/thione derivatives (DHPMs/DHPMTs).

Figure. S2. Synthesis of diverse 3,4-dihydropyrimidine-2(1H)-one/thione derivatives using the magnetic bismuth ferrite nanoparticles (BFO MNPs) in H2O: EtOH solvent system.

Figure S3. Schematic preparation of the Magnetic BiFeO3 Nanoparticles for the Green One-Pot Three-Component Synthesis of Highly Substituted 3,4-Dihydropyrimidine-2(1H)-one/thione Derivatives (DHPMs).

Figure S4: 1H NMR of ethyl-6-methoxy-4-(3-nitrophenyl)2-oxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4b).

Ethyl 6-methyl-4-(3-nitrophenyl)-2-oxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate; White solid, M.P: 220-221 oC, 1H NMR (500 MHz, d6-DMSO, δ = ppm) δ: 1.10 (t, J = 7.5 Hz, 3H, CH3), 2.28 (s, 3H, CH3), 4.00 (q, J = 7.0 Hz, 2H, CH2), 5.31 (d, J = 3.0 Hz, 1H, CH), 7.66 (t, J = 8.0 Hz, 1H, Ar-H), 7.70 (d, J = 7.5   Hz, 1H, Ar-H), 7.90 (brs, 1H, NH), 8.09 (s, 1H, Ar-H), 8.14 (d, J = 8.0 Hz, 1H, Ar-H), 9.37 (s, 1H, NH).

Figure S5: 1H NMR ethyl 4-(3,4-dichlorophenyl)6-methyl-2-oxo-1,2,3,40tetrahydropyrimidine-5-carboxylate (4f).

Ethyl 4-(3,4-dichlorophenyl)-6-methyl-2-oxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate; White solid, M.P: 228-230 oC, 1H NMR (500 MHz, d6-DMSO, δ = ppm) δ: 1.01 (t, J = 7.0 Hz, 3H, CH3), 2.30 (s, 3H, CH3), 3.90 (q, J = 7.0 Hz, 2H, CH2), 5.60 (s, 1H, CH), 7.32 (d, J = 8.5 Hz, 2H, Ar-H), 7.42 (d, J = 8.0   Hz, 2H, Ar-H), 7.57 (s, 1H, Ar-H), 7.57 (s, 1H, NH), 9.34 (s, 1H, NH).

Figure S6: 1H NMR of ethyl 4-(3,4-dimethoxyphenyl)-6-methyl-2-oxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4l).

Ethyl 4-(3,4-dimethoxyphenyl)-6-methyl-2-oxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate; White solid, M.P: 173-175 oC, 1H NMR (500 MHz, d6-DMSO, δ = ppm) δ: 1.12 (t, J = 7.0 Hz, 3H, CH3), 2.25 (s, 3H, CH3), 3.77 (s, 6H, 2 OCH3), 4.00 (q, J = 6.5 Hz, 2H, CH2), 5.11 (s, 1H, CH), 6.73 (d, J = 8.0 Hz, 1H, Ar-H), 6.85 (s, 1H, Ar-H), 6.90 (d, J = 8.0 Hz, 1H, Ar-H), 7.67 (s, 1H, NH), 9.15 (s, 1H, NH).

Figure S7: 1H NMR of ethyl 6-methoxy-2-oxo-4-(thiophen-2-yl)-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4q).

Ethyl 6-methyl-2-oxo-4-(thiophen-2-yl)-1,2,3,4-tetrahydropyrimidine-5-carboxylate; White solid, M.P: 214-216 oC, 1H NMR (500 MHz, d6-DMSO, δ = ppm) δ: 1.17 (t, J = 7.0 Hz, 3H, CH3), 2.23 (s, 3H, CH3), 4.07 (q, J = 7.0 Hz, 2H, CH2), 5.42 (d, J = 3.0 Hz, 1H, CH), 6.89 (m, 1H, Het Ar-H), 6.94 (t, J = 4.0 Hz, 1H, Het Ar-H), 7.33 (d, J = 5.0 Hz, 1H, Ar-H), 7.90 (s, 1H, NH), 9.31 (s, 1H, NH).

Figure S8: 1H NMR of ethyl 6-methyl-4-phenyl-2-thioxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4v).

Ethyl 6-methyl-4-phenyl-2-thioxo-1,2,3,4-tetrahydropyrimidine-5-carboxylate; White solid, M.P: 211-213 oC, 1H NMR (500 MHz, d6-DMSO, δ = ppm) δ: 1.10 (t, J = 7.0 Hz, 3H, CH3), 2.30 (s, 3H, CH3), 4.00 (q, J = 7.0 Hz, 2H, CH2), 5.19 (s, H, CH), 7.23 (d, J = 7.0 Hz, 2H, Ar-H), 7.28 (t, J = 7.5 Hz, 1H, Ar-H), 7.35 (t, J = 8.0 Hz, 2H, Ar-H), 9.65 (s, 1H, NH), 10.33 (s, 1H, NH).

Preparation of the magnetic bismuth ferrite nanoparticles (BFO MNPs)

Preparation of BFO MNPs was carried out through the solid-state thermal decomposition method33,34. Initially, a 100 ml round-bottom flask was charged with glycine (8.0 mmol), Fe(NO3)3 (4.0 mmol), Bi(NO3)3 (4.0 mmol), and deionized water (40.0 ml) and the obtained mixture was heated at 120 oC for one h. Subsequently, HNO3 (2.80 ml) was added dropwise to the reaction mixture. The reaction mixture was subjected to heating at 120 °C, resulting in the formation of a brown solid. Finally, the brown solid was placed in the oven for one h at 350 oC and further one h at 550 oC to prepare bismuth ferrite nanoparticles (BFO MNPs).

Figure S9: Fourier-Transform infrared spectrum (FT-IR) of BFO MNPs.

Figure S10: FESEM images of BiFeO3 nanoparticles; a) 3 μm and b) 500 nm scales.

Figure S11: EDS elemental mapping analysis of BFO MNPs.

Figure S112: Elemental analysis by energy-dispersive X-ray spectroscopy (EDS) of the BFO MNPs.

Figure S13:  X-Ray diffraction pattern of BFO MNPs.

Figure S14: Hysteresis diagram of the magnetic bismuth ferrite nanoparticles (BFO MNPs).

| BET Plot |  |
| --- | --- |
| BET Surface Area | 24.8109 [m2g-1] |

Table S1: The result of nitrogen adsorption-desorption isotherms of BFO MNPs.

| Table 1. Exploring optimal conditions for the one-pot three-component Biginelli reaction involving benzaldehyde (1h), ethyl acetoacetate (2), and urea (3a).a |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry. | Catalyst loading (mg) | Solvent | Temperature (oC) | Time (min) | Yield (%)b | TON |
| 1 | - | H2O | r.t | 360 | Trace | - |
| 2 | - | H2O | Reflux | 360 | Trace | - |
| 3 | Fe3O4 (2.0 mg) | H2O | r.t | 45 | Trace | - |
| 4 | MnFe2O4 (2.0 mg) | H2O | r.t | 45 | 30 | 34.6 |
| 5 | CuFe2O4 (2.0 mg) | H2O | r.t | 45 | 27 | 32.3 |
| 6 | ZnFe2O4 (2.0 mg) | H2O | r.t | 45 | 31 | 37.4 |
| 7 | NiFe2O4 (2.0 mg) | H2O | r.t | 45 | 25 | 29.3 |
| 8 | BiFeO3 (2.0 mg) | H2O | r.t | 45 | 40 | 62.6 |
| 9 | BiFeO3 (2.0 mg) | MeOH | r.t | 45 | 44 | 68.9 |
| 10 | BiFeO3 (2.0 mg) | EtOH | r.t | 45 | 59 | 92.3 |
| 11 | BiFeO3 (2.0 mg) | EtOAc | r.t | 45 | 53 | 82.9 |
| 12 | BiFeO3 (2.0 mg) | CH3CN | r.t | 45 | 50 | 78.2 |
| 13 | BiFeO3 (2.0 mg) | H2O: EtOH | r.t | 45 | 60 | 93.9 |
| 14 | BiFeO3 (2.0 mg) | H2O: EtOH | r.t | 45 | 67 | 104.9 |
| 15 | BiFeO3 (4.0 mg) | H2O:EtOH | r.t | 20 | 84 | 68.9 |
| 16 | BiFeO3 (4.0 mg) | H2O:EtOH | Reflux | 10 | 93 | 72.8 |
| aReaction conditions: aldehyde (1a, 1.0 mmol), ethyl acetoacetate (2, 1.0 mmol), urea (3a, 1.1 mmol) and 3 mL of H2O: EtOH mixture (4.0 ml, 3:1) as a solvent. bThe yield of the products is related to the isolated yield. |  |  |  |  |  |  |

| Table 2. Synthesis of diverse ethyl 4-(aryl/heteroaryl)-6-methyl-2-oxo-4,3,2,1-tetrahydropyrimidine-5-carboxylate using BFO MNPs nanocatalyst and various aromatic and heteroaromatic carbonyl compounds.a |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry. | Aldehyde (1a-s) | Urea/Thiourea (3a-b) | Product (4a-y) | Time (min) | Yield b (%) | M.p (oC) |
| 1 | 1a | Urea 3a |  | 10 | 96 | 211-2139 |
| 2 | 1b | Urea 3a |  | 10 | 91 | 220-2219 |
| 3 | 1c | Urea 3a |  | 15 | 90 | 205-20750 |
| 4 | 1d | Urea 3a |  | 10 | 93 | 219-22151 |
| 5 | 1e | Urea 3a |  | 15 | 90 | 209-2109 |
| 6 | 1f | Urea 3a |  | 10 | 97 | 228-23051 |
| 7 | 1g | Urea 3a |  | 10 | 94 | 210-21352 |
| 8 | 1h | Urea 3a |  | 10 | 93 | 201-20353 |
| 9 | 1i | Urea 3a |  | 15 | 90 | 231-23354 |
| 10 | 1j | Urea 3a |  | 15 | 95 | 200-20151 |
| 11 | 1k | Urea 3a |  | 20 | 94 | 258-26055 |
| 12 | 1l | Urea 3a |  | 15 | 92 | 173-17551 |
| 13 | 1m | Urea 3a |  | 15 | 90 | 205-20756 |
| 14 | 1n | Urea 3a |  | 10 | 88 | 232-23351 |
| 15 | 1o | Urea 3a |  | 20 | 90 | 241-24357 |
| 16 | 1p | Urea 3a |  | 15 | 88 | 205-20758 |
| 17 | 1q | Urea 3a |  | 15 | 93 | 214-2169 |
| 18 | 1r | Urea 3a |  | 15 | 90 | 199-2019 |
| 19 | 1a | Urea 3a |  | 15 | 95 | 207-20959 |
| 20 | 1d | Thiourea 3b |  | 15 | 91 | 181-18360 |
| 21 | 1g | Thiourea 3b |  | 15 | 89 | 189-19061 |
| 22 | 1h | Thiourea 3b |  | 20 | 98 | 211-21362 |
| 23 | 1n | Thiourea 3b |  | 15 | 90 | 217-21862 |
| 24 | 1s | Thiourea 3b |  | 20 | 94 | 208-21063 |
| 25 | 1j | Thiourea 3b |  | 20 | 92 | 207-20864 |
| a Reaction conditions: aromatic or heteroaromatic aldehyde (1a-s, 1.0 mmol), ethyl acetoacetate (2, 1.0 mmol), urea/thiourea (3a-b, 1.1 mmol), BiFeO3 (4.0 mg), 3.0 ml of H2O: EtOH (4.0 ml, 3:1) under reflux conditions. b The yield of products is related to the purified product. |  |  |  |  |  |  |

Figure S15: Proposed mechanism for the synthesis of 3,4 dihydropyrimidine-2(1H)-one/thione derivatives in the presence of magnetic BFO MNPs nanocatalyst.

Figure S16: The results of recyclability and reusability of the BFO MNPs nanoparticles in the model reaction.

| Table 4. Comparison of the model reaction for the synthesis of Ethyl 6-methyl-2-oxo-4-phenyl-1,2,3,4-tetrahydropyrimidine-5-carboxylate (4h) in the presence of BiFeO3 in terms of time and product yield with recent reports. . |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry | Catalyst (loading) | Solvent | Temperature (oC) | Time (min) | Yield (%) | Ref. |
| 1 | 5-Hf(OTf)4, 1.0 mol | - | 80 | 20 | 95 | 57 |
| 2 | Zwitterionic MSI and TRIP, 10 mol% | Solvent-Free | 30 | 72 | 99 | 32 |
| 3 | Niobium/Fe3O4, 1.5 mg | EtOH | 80 | 720 | 99 | 24 |
| 4 | Polyanilin-FeCl3, 200.0 mg | CH3CN |  | 24 | 90 | 58 |
| 5 | Bead-CDNS, 30.0 mg | H2O | Ultrasonic, 120 W | 15 | 100 | 59 |
| 6 | Coconut husk ash twisted graphene, 100.0 mg | Solvent-Free | 130 | 14 | 94 | 21 |
| 7 | IRMOF-3, 4.0 mol | Solvent-Free | Reflux | 300 | 90 | 60 |
| 8 | Coordination polymer Zn, 5.0 mol% | Solvent-Free | 100 | 5 | 99 | 35 |
| 9 | Wng Resin-Supported Sulfonic Acid, 30.0 mg | EtOH | 100 | 30 | 96 | 61 |
| 10 | Fe3O4@Nb2O5-0.1mol% | EtOH | 80 | 12 | 99 | 24 |
| 11 | Nb2O5/T, 5.0 mol% | Solvent-Free | 130 | 1 | 94 | 62 |
| 12 | BiFeO3 NPs, 4.0 mg | H2O:EtOH | Reflux | 10 | 93 | This Work |