Supplementary Information

# Formation and saturation of β-phase of PVDF in DMF solvent: a comprehensive study

# Satyasadhan Dowarah#, Parswajit Kalita#, Divya Pratap Singh, Sanjeev Kumar*

The %β/α has been calculated as follows -

The lattice parameters of the monoclinic structure of α-phase are:

a = 0.496nm, b = 0.964nm, c = 0.462nm; α = 90°, β = 97°, γ = 90°

The lattice parameters of the orthorhombic structure of β-phase are:

a = 0.856nm, b = 0.491nm, c = 0.256nm; α = 90°, β = 90°, γ = 90°

The Structure Factor can be mathematically expressed as-

fhkl =k=jnfjei(a**xj*h+b**yj*k+c**zj*l)

where h, k, l are the miller indices; a*, b*, c* are the reciprocal lattice vectors; x, y, z are the intercepts on x, y & z direction. fj is the atomic number of the atom.

We know that,

a* = 2πb×csinQabc,     Q is the angle between the lattice vectors

b* = 2πa×csinQ(abc),

c* = 2πa×bsinQ(abc)

And after determining the (𝑓ℎ𝑘𝑙) value we take the modulus square of it. As shown below:

|fhkl|2= ((real part)2+(imaginary part)2 )2

The data from the .cif file (available online) for the α-phase and β-phase has been used to calculate the fraction of the α and β phase under the deconvoluted α-peak from Fig 8.

The α-phase corresponds to the plane (020) and we have

f020 =k=124fjei(b**yj*2)

k = 1 to 24 means 8 C atoms, 8 F atoms and 8 H atoms.

=> f020 =k=124fjei(b**yj*2)

= 6ei4πb*yjsin97+ 9ei4πb*yjsin97+ 1 ei4πb*yjsin97

= 36ei4πb*yjsin97 + 72ei4πb*yjsin97 + 8ei4πb*yjsin97

= 6{ei4πb ⨯ 0.182021⨯bsin97+ei4πb ⨯0.181210⨯bsin97+ ... +ei4πb ⨯0.318790⨯bsin97}8terms + 9{ei4πb ⨯0.169112 ⨯bsin97 + ei4πb ⨯ 0.036797 ⨯ bsin97 ... + ei4πb ⨯ 0.463203 ⨯ bsin97}8terms + 1{ei4πb ⨯0.177500 ⨯ bsin97+ ei4πb ⨯ 0.073665 ⨯ bsin97 + ... + ei4πb ⨯0.426335 ⨯ bsin97}8terms

...............................................

Proceeding in this way, we get

|f020|2 = 372.16

Now, the α-phase fraction under the α-peak is-

αx = Area under the α peak |f020|2

The β-phase corresponds to the plane (200), hence

f200 =k=112fjei(a**xj*2)

k = 1 to 12 means 4 C atoms, 4 F atoms and 4 H atoms.

=>  f200 =k=112fjei(a**xj*2)

= 6ei4πb*yjsin97 + 9ei4πb*yjsin97 + 1ei4πb*yjsin97

= 6{ei4πa ⨯ 0⨯asin90 + .... + ei4πa ⨯ 0.5⨯asin90}4terms + 9{ei4πa ⨯ 0.5⨯asin90 + ... + ei4πa ⨯ 0.5⨯asin90}4terms + 1{ei4πa ⨯ 0 ⨯ asin90 + ... + ei4πb ⨯ 0⨯bsin90}4terms

= 64

Hence,   |f200|2 = 4096

Thus, the β-phase fraction under the α-peak is-

βx = Area under the β peak |f200|2

Therefore, we have,

%β/α = βxαx ⨯ 100